## Slide 1: Transistor and IC design for 50GHz and above
Mark Rodwell, UCSB
Short Course, July 26, 2017, Qualcomm San Diego
mm-wave systenms: Prof. U. Madhow & group: UCSB
mm-wave ICs S-K Kim, R. Maurer, A. Ahmed, H. Yu, H-C. Park, T. Reed, UCSB Prof. J. Buckwalter & group, UCSB J. Hacker, Z. Griffith: Teledyne Scientific and Imaging M. Seo: Sungkyunkwan University
mm-Wave Transistors : J. Rode, P. Choudhary, B. Markman, Y. Fang, J. Wu, A.C. Gossard, B. Thibeault, W. Mitchell: UCSB M. Urteaga, B. Brar: Teledyne Scientific and Imaging

## Slide 2: Why mm-wave wireless ?

## Slide 3
Overview

## Slide 4: mm-Waves: high-capacity mobile communications
Needs→ research: RF front end: phased array ICs, high-power transmitters, low-noise receivers IF/baseband: ICs for multi-beam beamforming, for ISI/multipath suppression, ...

## Slide 5: mm-Waves: benefits & challenges
Massive # parallel channels
Need mesh networks
Need phased arrays (overcome high attenuation)
5
Large available spectrum
line-of-sight MIMO
spatial multiplexing
(note high attenuation in foul weather)

## Slide 6: mm-Wave Wireless Needs Phased Arrays
isotropic antenna → weak signal →short range
highly directional antenna → strong signal, but must be aimed
no good for mobile
beam steering arrays → strong signal, steerable
32-element array → 30 (45?) dB increased SNR
must be precisely aimed →too expensive for telecom operators

## Slide 7: Millimeter-wave imaging
235 GHz video-rate synthetic aperture radar
10,000-pixel, 94GHz imaging array→ 10,000 elements
Golcuk: Trans MTT, Aug 2014
1 transmitter, 1 receiver 100,000 pixels 20 Hz refresh rate 5 cm resolution @ 1km 50 Watt transmitter (tube, solid-state driver)
Demonstrated: SiGe (UCSD/Rebeiz) ~1.3kW: 10,000 elements Lower-power designs: InP, CMOS, SiGe (UCSB, UCSD, Virginia Poly.)

## Slide 8: mm-wave imaging radar: TV-like resolution
What you see in fog
What 10GHz radar shows
What you want to see
goal: ~0.2o resolution, 103-106 pixels
Large NxN phased array
Frequency-scanned 1xN array
mm-waves → high resolution from small apertures
ultimate: ~400 GHz; intermediate: ~140 GHz

## Slide 9
mm-wave systems

## Slide 10: Target Systems
10

## Slide 11
arrays

## Slide 12: Antenna & array basics

## Slide 13: Electronic Beamsteering, a.k.a. phased array

## Slide 14: Reminder: Multipath Propagation

## Slide 15: Fading vs Intersymbol interference

## Slide 16: Beamforming can suppress ISI
1 Gbaud with 10o array beamwidth : multipath mostly causes fading not much ISI
10 Gbaud with 10o array beamwidth : significant fading and significant ISI
Solution 1: larger arrays narrower beamwidth
Solution 2: multiple arrays multiple receivers to handle fading ? can sum these to form narrow nulls! also handles fading and ISI

## Slide 17: Optimum array size for low system power
At optimum-size array, target PA output power is typically 10-200 mW

## Slide 18: How big should be the array ?
Large arrays: more directive→ less PA power needed more channels→ cost, DC power
Large arrays: more directive→ less SNR loss with NLOS nulling eases multipath equalization

## Slide 19: Data delay equalization in large arrays

## Slide 20
systems

## Slide 21: mm-Wave LOS MIMO: multi-channel for high capacity
Torklinson : 2006 Allerton Conference Sheldon : 2010 IEEE APS-URSI Torklinson : 2011 IEEE Trans Wireless Comm.

## Slide 22: Spatial Multiplexing: massive capacity RF networks
multiple independent beams each carrying different data each independently aimed # beams = # array elements
Hardware: multi-beam phased array ICs

## Slide 23: 100-1000 GHz Wireless Needs Mesh Networks
Object having area ~lR will block beam.
Blockage is avoided using beamsteering and mesh networks.
...high-frequency signals are easily blocked.
...this is easier at high frequencies.

## Slide 24
mm-wave propagation

## Slide 25: Fair-Weather Propagation
Wiltse, 1997 IEEE Int. APS Symposium, July
Fair weather
2-5 dB/km
75-110 GHz
200-300 GHz
125-165 GHz
9km elevation
4km elevation
sea level

## Slide 26: Foul Weather Propagation
Extreme Fog (1g/m3) ~(25 dB/km)x(frequency/500 GHz)
Rain: 10-3: 25mm/hr, 11dB/km 10-4: 50-85mm/hr, 19dB/km 10-5: 100+mm/hr: 30dB/km
Olsen, Rogers, Hodge, IEEE Trans Antennas & Propagation Mar 1978 Liebe, Manabe, Hufford, IEEE Trans Antennas and Propagation, Dec. 1989 Liebe, IEEE Trans Ant and Pro, Vol 31, No. 1, Jan 1983 Karasawa, Maekawa, IEEE Proc, Vol 85 , #6 , June 1997
35oC, 95% Humidity loss (dB/km)~(frequency/60GHz)2 11 dB/km@200 GHz, 5.5dB/km@140GHz
Rosker; Wallace, 2007 IEEE IMS

## Slide 27: Atmospheric Attenuation: Implications
Worst-case attenuation roughly constant over 50-250 GHz. 10-5 outage rate: equal losses over 50-300 GHz 10-3 outage rate: equal losses over 50-200 GHz
target should be 50-250 GHz links. Exclusive use of VLSI Si processes forces use of 50-180GHz

## Slide 28
detailed link analysis

## Slide 29: Example Link budgets (60 GHz)
Note various margins allocated. Rain losses calculated from rain rate.
array: 16 elements (2x8) 4.5 x 1.0 inches 11.5 x 2.54 cm

## Slide 30: Example Link budgets (140 GHz)
Note various margins allocated. Rain losses calculated from rain rate.
array: 16 elements (2x8) 1.9 x 0.43 inches 4.9 x 0.11 cm

## Slide 31
hardware: rough numbers

## Slide 32: 140 GHz, 10 Gb/s Adaptive Picocell Backhaul

## Slide 33: 140 GHz, 10 Gb/s Adaptive Picocell Backhaul
350 meters range in 50mm/hr rain
PAs: 24 dBm Psat (per element)
LNAs: 4 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 34: 340 GHz, 160 Gb/s MIMO Backhaul Link
→ 1o beamwidth; 8o beamsteering

## Slide 35: 340 GHz, 160 Gb/s MIMO Backhaul Link
600 meters range in five-9's rain
1o beamwidth; 8o beamsteering
PAs: 21 dBm Psat (per element)
LNAs: 7 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 36: 60 GHz, 1 Tb/s Spatially-Multiplexed Base Station
2x64 array on each of four faces.
Each face supports 128 users, 128 beams: 512 total users.
Each beam: 2Gb/s.
200 meters range in 50 mm/hr rain
PAs: 20 dBm Pout , 26 dBm Psat (per element)
LNAs: 3 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 37: mm-Wave Wireless Transceiver Architecture
custom PAs, LNAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.

## Slide 38: 400 GHz frequency-scanned imaging radar
What you see with X-band radar
What your eyes see-- in fog
What you would like to see
38

## Slide 39: 400 GHz frequency-scanned imaging car radar
39

## Slide 40: 400 GHz frequency-scanned imaging car radar
Image refresh rate: 60 Hz
Resolution 64×512=32,800 pixels
Angular resolution: 0.10 degrees
Aperture: 12" by 12"
Angular field of view: 9 by 97 degrees
Component requirements: 10 mW peak power/element, 3% pulse duty factor 6.5 dB noise figure, 5 dB package losses 5 dB manufacturing/aging margin
Range: see a basketball at 300 meters (10 seconds warning) in heavy fog (10 dB SNR, 28 dB/km, 1 foot diameter target, 65 MPH)
40

## Slide 41
Transistors and IC technologies

## Slide 42: Production Semiconductor Processes for mm-Wave
Silicon Germanium BiCMOS Processes |  |  | 
foundry | process | nominal fmax | useful range
IBM (GF !) | 9HP | 320 GHz | ~170 GHz
TowerJazz | SBC13H3 | 270 GHz | ~140 GHz
TowerJazz | SBC18H4 (near release) | 350 GHz | ~180 GHz
ST Microelectronics | S9MW | 270 GHz | ~140 GHz
ST Microelectronics | SB55 (development) | 340 GHz | ~180 GHz
"Useful (frequency) range" means those frequencies at which acceptable-performance IC blocks can be realized, not the highest frequency of a published research result.

## Slide 43: Production Semiconductor Processes for mm-Wave
VLSI CMOS Processes |  |  | 
foundry | process | nominal fmax | useful range
various (IBM, GF, TSMC) | 65nm bulk CMOS | ~~250GHz | ~130GHz
IBM (GF !) | 45nm PD-SOI (high leakage power) | ~~300 GHz | ~150 GHz
IBM (GF !) | 32 nm UTB-SOI | ~~300 GHz | ~150 GHz
ST Microelectronics | 28 nm UTB-SOI | similar to above | 
various | 22nm, ~14nm UTB-SOI | poorer than above | 
Intel, IBM/GF | 22nm, ~14nm finFET | likely poorer than above, | 
Generations beyond 28/32nm: progressively poorer performance in 100+ GHz ICs progressively lower transmitter power at all frequencies

## Slide 44: Semiconductor Processes for mm-Wave
Production III-V foundries |  |  | 
foundry | process | nominal fmax | useful range
Northrop-Grumman (low-volume) | 600nm InP HBT: 4V: higher-power transmitters | >300GHz | ~150 GHz
Northrop-Grumman (low-volume) | 100nm InP HEMT (FET) for very low noise receivers | >350GHz | ~200 GHz
Qorvo (Tri-Quint) | TQP13 HEMT power amps, low-noise -amps | ~~150GHz | 100 GHz
These processes are best for single-stage add-on power amps, low-noise amps; both to increase system range.

## Slide 45: Research Semiconductor Processes
Research institutions with some "foundry-like" access |  |  | 
foundry | process | nominal fmax | useful range
Teledyne | 250nm InP HBT | 700GHz | ~250 GHz
Teledyne | 130nm InP HBT | 1100 GHz | ~450 GHz
IHP | 130nm SiGe BiCMOS | 500GHz | ~250 GHz
microwave GaN HEMT is a production technology mm-wave GaN HEMT may become a production technology mm-wave InP HBT may become a production technology

## Slide 46: mm-wave CMOS (examples)
260 GHz amplifier: 65nm bulk CMOS, Over-neutralized to reach Gmax, 9.2 dB, 4 stages Momeni ISSCC, March 2013
150 GHz amplifier: 65 nm bulk CMOS, 8.2 dB, 3 stages (250GHz fmax) Seo et al. (UCSB), JSSC, December 2009
300 GHz fmax

## Slide 47: mm-Wave CMOS won't scale much further
Gate dielectric can't be thinned → on-current, gm can't increase
Tungsten via resistances reduce the gain
Inac et al, CSICS 2011
Shorter gates give no less capacitance dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz.
Present finFETs have yet larger end capacitances

## Slide 48: III-V high-power transmitters, low-noise receivers
Cell phones & WiFi: GaAs PAs, LNAs
mm-wave links need high transmit power, low receiver noise
0.47 W @86GHz
0.18 W @220GHz
1.9mW @585GHz
M Seo, TSC, IMS 2013
T Reed, UCSB, CSICS 2013
H Park, UCSB, IMS 2014

## Slide 49
InP Bipolar Transistors

## Slide 50: Why InP Bipolar Transistors ?
InP better electron transport than Si collectors higher electron velocity 3.5 vs 1.0 × 107 cm/s plus wider bandgap→ higher breakdown field
InGaAs base, base-emitter heterojunction: very low base sheet resistances
Implications: ~3:1 higher (ft, fmax) at a given scaling node higher breakdown* at a given (ft, fmax) but...InP HBT not a production technology
*Breakdown is too complicated to summarize with BVCEO. BVCBO vs. BVCEO vs. safe operating area ? Bottom line: look at Vce used in published IC data for a given IC technology.

## Slide 51
Transistor scaling laws: ( V,I,R,C,t ) vs. geometry
Bulk and Contact Resistances
Depletion Layers
Thermal Resistance
Fringing Capacitances
Available quantum states to carry current
→ capacitance, transconductance contact resistance

## Slide 52: Bipolar Transistor: Structure & Models

## Slide 53: Base-Collector Distributed RC Parasitics

## Slide 54: RbbCcb Time Constant, Fmax , Simple Hybrid-p model
Vaidyanathan & Pulfrey IEEE Trans. Elect. Dev. Feb. 1999

## Slide 55
BJT Space-Charge-Limited Current (Kirk effect)

## Slide 56: InP: Electron velocity modulation
More collector voltage→ less distance before scattering→ more transit time
✘
✘
more collector voltage
less collector voltage
light G valley
heavy L valley
heavy X valley
(ft, fmax) decrease with increased Vce. Ccb is modulated by Ic.

## Slide 57: Reduced gm at extreme current densities
Boltzmann
Fermi-Dirac
Highly Degenerate
Problem in InP, not silicon: silicon has larger electron effective mass, more valleys
High currents→ transconductance less than qI/kT → bandwidth decreases
130nm InP HBT

## Slide 58
Bipolar Transistor Design
58

## Slide 59
Bipolar Transistor Design: Scaling
59

## Slide 60: Energy-limited vs. field-limited breakdown
band-band tunneling: base bandgap impact ionization: collector bandgap
60

## Slide 61: Making faster bipolar transistors
to double the bandwidth: | change
emitter & collector junction widths | decrease 4:1
current density (mA/mm2) | increase 4:1
current density (mA/mm) | constant
collector depletion thickness | decrease 2:1
base thickness | decrease 1.4:1
emitter & base contact resistivities | decrease 4:1
Narrow junctions. Thin layers High current density Ultra low resistivity contacts
Teledyne: M. Urteaga et al: 2011 DRC

## Slide 62: Refractory Contacts to In(Ga)As
Refractory: robust under high-current operation / Low penetration depth: ~ 1 nm / Performance sufficient for 32 nm /2.8 THz node.
32 nm (2.8THz) node requirements
Baraskar et al, Journal of Applied Physics, 2013
Why no ~2THz HBTs today ? Problem: reproducing these base contacts in full HBT process flow
62

## Slide 63: THz HBTs: The key challenges
Obtaining good base contacts in HBT vs. in contact test structure (emitter contacts are fine)
Baraskar et al, Journal of Applied Physics, 2013
RC parasitics along finger length metal resistance, excess junction areas

## Slide 64: THz HBTs: double base metal process
Blanket surface clean (UV O3 / HCl) strips organics, process residues, surface oxides
Blanket base metal no photoresist; no organic residues Ru refractory diffusion barrier 2 nm Pt : penetrates residual oxides
Thick Ti/Au base pad metal liftoff thick metal→ low resistivity
Rode et al., IEEE TED, Aug. 2015

## Slide 65: Reducing Emitter Length Effects
small base post undercut
large base post
before
after
large base post undercut
small base post
65
Rode et al., IEEE TED, Aug. 2015
large emitter end undercut
small emitter end undercut

## Slide 66: Reducing Emitter Length Effects
before
after
thicker Au base metal
narrower collector junction
66
Rode et al., IEEE TED, Aug. 2015

## Slide 67
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 68: 130nm /1.1 THz InP HBT: ICs to 670 GHz
614 GHz fundamental VCO
340 GHz dynamic frequency divider
620 GHz, 20 dB gain amplifier
M Seo, TSC IMS 2013
also: 670GHz amplifier J. Hacker , TSC IMS 2013 (not shown)
M. Seo, TSC / UCSB
M. Seo, UCSB/TSC IMS 2010
204 GHz static frequency divider (ECL master-slave latch)
Z. Griffith, TSC CSIC 2010
300 GHz fundamental PLL
M. Seo, TSC IMS 2011
220 GHz 180 mW power amplifier
T. Reed, UCSB CSICS 2013
600 GHz Integrated Transmitter PLL + Mixer
M. Seo TSC
Integrated 300/350GHz Receivers: LNA/Mixer/VCO
M. Seo TSC
81 GHz 470 mW power amplifier
H-C Park UCSB IMS 2014

## Slide 69: Towards a 3 THz InP Bipolar Transistor
Extreme base doping→ low-resistivity contacts→ high fmax
Extreme base doping→ fast Auger (NP2) recombination→ low b.
Solution: very strong base compositional grading→ high b

## Slide 70: 1/2-THz SiGe HBTs
500 GHz fmax SiGe HBTs Heinemann et al. (IHP), 2010 IEDM
16-element multiplier array @ 500GHz (1 mW total output) U. Pfeiffer et. al. (Wuppertal / IHP) , 2014 ISSCC

## Slide 71: Towards a 2 THz SiGe Bipolar Transistor
 | InP | SiGe | 
emitter |  |  | 
junction width | 64 | 18 | nm
access resistivity | 2 | 0.6 | W-mm2
base |  |  | 
contact width | 64 | 18 | nm
contact resistivity | 2.5 | 0.7 | W-mm2
collector |  |  | 
thickness | 53 | 15 | nm
current density | 36 | 125 | mA/mm2
breakdown | 2.75 | 1.3? | V
ft | 1000 | 1000 | GHz
fmax | 2000 | 2000 | GHz
Similar scaling InP: 3:1 higher collector velocity SiGe: good contacts, buried oxides
Key distinction: Breakdown
InP has: thicker collector at same ft, wider collector bandgap
Key requirements:
low resistivity Ohmic contacts note the high current densities
Assumes collector junction 3:1 wider than emitter.
Assumes SiGe contacts no wider than junctions

## Slide 72
InP Field-Effect Transistors

## Slide 73
State of the art in InP HEMTs
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process

## Slide 74: HEMTs: Key Device for Low Noise Figure
Hand-derived modified Fukui Expression, fits CAD simulation extremely well.
2:1 to 4:1 increase in ft → greatly improved noise @ 200-670 GHz.
Better range in sub-mm-wave systems; or use smaller power amps.
or enable yet higher-frequency systems

## Slide 75
FET Design

## Slide 76
FET Design: Scaling

## Slide 77
FET Design: Scaling
2:1
2:1
constant
2:1
2:1
2:1
2:1
2:1
2:1
2:1
2:1
constant
constant
2:1
2:1
constant
2:1
2:1
4:1
constant
constant

## Slide 78
FET Scaling Laws (these now broken)
fringing capacitance does not scale → linewidths scale as (1 / bandwidth )
78
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1

## Slide 79
FET Scaling Laws (these now broken)
Gate dielectric can't be much further scaled. Not in CMOS VLSI, not in mm-wave HEMTs
gm/Wg (mS/mm) hard to increase → Cend / gm prevents ft scaling.
Shorter gate lengths degrade electrostatics → reduced gm /Gds → reduced fmax/ ft
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1

## Slide 80
Why THz HEMTs no longer scale
HEMTs: gate barrier also lies under S/D contacts → high S/D access resistance
As gate length is scaled, gate barrier must be thinned for high gm, low Gds
HEMTs: High gate leakage when gate barrier is thinned→ cannot thin barrier

## Slide 81
FET scaling laws; 2:1 higher bandwidth | change
gate length | decrease 2:1
current density (mA/mm), gm (mS/mm) | increase 2:1
transport mass | constant
gate-channel capacitance density | increase 2:1
contact resistivities | decrease 4:1
Towards at 2.5 THz HEMT
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process
Need thinner dielectrics, better contacts

## Slide 82: Record III-V MOS
S. Lee et al., VLSI 2014
Vertical Spacer
N+ S/D
Lg~25 nm
record for III-V
= best UTB SOI silicon

## Slide 83: Excellent III-V gate dielectrics
61 mV/dec Subthreshold swing at VDS=0.1 V
Negligible hysteresis
2.5nm ZrO2 1nm Al2O3
2.5nm InAs
V. Chobpattanna, S. Stemmer FET data: S Lee, 2014 VLSI Symp.

## Slide 84: III-V MOS @ Lg = ???
Image courtesy of S. Kraemer (UCSB)
Huang et al., 2015 DRC

## Slide 85: Towards at 2.5 THz HEMT
C. Y. Huang et al., DRC 2015
VLSI III-V MOS
THz III-V MOS

## Slide 86
mm-wave measurements

## Slide 87
Agilent, Rhode/Schwarz network analyzer,
Oleson Microwave Lab or Virginia Diodes frequency extenders
micro-coax wafer probes with waveguide connections GGB Industries, Cascade Microtech University of Virgina.
Internal bias Tee’s in probes
Mostly on-wafer calibration standards.
On-Wafer Network Analysis: 750+ GHz

## Slide 88: On-Wafer Through-Reflect-Line (TRL) Calibration
Through
Reflect
Line
Device Under Test
225um
reference plane
ΔL
ΔL= 90 deg @center frequency. l/8<ΔL<3l/8
DUT
open
short
Either open or short needed. Standards need not be accurate. "Open" must have G closer to that of open than that of short. Ports 1 & 2 must be symmetric.
Through line should be long for large probe separation. Minimizes probe-probe coupling. Measurements normalized to the line characteristic impedance.
225um
225um
225um
225um
225um
Please see also: http://www.ece.ucsb.edu/Faculty/rodwell/publications_and_presentations/publications/204vg.ppt

## Slide 89: On-Wafer Line Reflect Linie Calibration
Extended Reference planes transistors placed at center of long on-wafer line LRL standards placed on wafer large probe separation → probe coupling reduced still should use the best-shielded probes available
Problem: substrate mode coupling method will FAIL if lines couple to substrate modes → method works very poorly with CPW lines need on wafer thin-film microstrip lines
CPW

## Slide 90: Difficulties with >100 GHz On-Wafer Calibration
Data on two layouts of 65 nm MOSFET
MAG/MSG, dB
U < 0 (!)
10*log10|U| (?)
"Unilateral gain", dB
"Unilateral gain", linear
Measured Y-parameters correlate reasonably with expected device model. Small errors in measured 2-port parameters result in large changes in Unilateral gain and Rollet's stability factor; neither measurement is credible.
Y12 appears to be the key problem. IC Sij measurements are fine. Transistor fmax measurements are hard.
( K<1 )

## Slide 91
Packaging and antennas

## Slide 92: The Antenna Feed Loss Problem
array elements are many l long overall array can be very big → high feed line losses
One solution: waveguide-fed arrays of slots
Use distribution amplifiers ?
Use to feed array tile: overall array needs steering

## Slide 93: Using lenses to reduce feed loss
Lenses on individual array elements.
...or on the overall array.
Here the challenge is maintaining constant beamwidth over wide steering angles.

## Slide 94: mm-wave interfaces: packaging
Wire-bonds: With care, >60GHz can be coupled over wire-bonds. Coupling of multiple lines remains problematic .
Flip-chip bonds Standard C4 bonds very capacitive; tuning OK @ 60GHz. Possibly higher. Option: more highly scaled bonds. Must contact vendors. Heat removal problematic in flip-chip ICs
Flexible polyimide interconnect substrate Used in Cascade micotech multi-signal probes, in some 60GHz products. Ground integrity, low inductance mm-wave connections. Must identify vendor.
https://www.cmicro.com/products/probe-cards/the-technology/thin-film-technology/cascade-microtech-s-thin-film-technology

## Slide 95: mm-wave interfaces: packaging
Through-silicon vias for RF grounding (TowerJazz, also IBM/GF) very low ground inductance low losses, low crosstalk in mm-wave IC-package connections

## Slide 96
mm-wave IC Design

## Slide 97
Reactively-Tuned IC Design: Concepts

## Slide 98: What's the most gain we can get ? Do we care ?
A. Singhakowinta & A. R. Boothroyd, International Journal of Electronics, Volume 21, Issue 6, 1966, pages 549-560, DOI:10.1080/00207216608937931 O. Momeni and E. Afshari, 2011 IEEE Custom Integrated Circuits Conference (CICC), San Jose, CA, 2011, pp. 1-4, doi: 10.1109/CICC.2011.6055322

## Slide 99: What's the most gain we can get ? Do we care ?
Low-noise amplifiers designed for low noise figure, fairly high IP3
Power amplifiers designed for high Psat, PAE, sufficiently low IM3
IF amplifiers designed for low noise figure, high IP3.
Practical amplifiers are rarely designed for highest gain.
Real-world relevance of Gma, Gms, Gmax,S is not clear.
Practical designs would benefit from new theory Quantities similar to Gma, Gms, Gmax,S above But under constraints of high-power or low-noise tuning. I know of no such published work.

## Slide 100: RF-IC Design: Simple & Well-Known Procedures
1: (over)stabilize at the design frequency guided by stability circles
3: Tune remaining port for maximum gain
2: Tune input for Fmin (LNAs) or output for Psat (PAs)
4: Add out-of-band stabilization.
There are many ways to tune port impedances: microstrip lines, MIM capacitors, transformers Choice guided by tuning losses. No particular preferences.
For BJT's, MAG/MSG usually highest for common-base.
Common-base gain is however reduced by: base (layout) inductance emitter-collector layout capacitance.
100

## Slide 101: Low-Noise Amplifier Design
Inductive emitter/source degeneration simultaneous S11 and noise match reduces gain, improves IP3
Additional in-band stabilization (output port) as needed Input tuning for Fmin Output match Out-of-band stabilization

## Slide 102: Power Amplifier Design (Cripps method)
parasitic C's and R's represented
by external elements...
For maximum saturated output power,
& maximum efficiency
device intrinsic output must see optimum loadline set by:
breakdown, maximum current, maximum power density.
ammeter monitors intrinsic junction current without including capacitive currents
...(Vcollector-Vemitter ) measures voltage internal to series parasitic resistances...

## Slide 103: PAs with corporate combining
W-band InP HBT power amplifier - UCSB
34 GH InP HBT power amplifier - J. Hacker Teledyne
34 GH InP HBT power amplifier - J. Hacker Teledyne

## Slide 104: Power amplifier design: combiners
Even-mode equivalent circuit

## Slide 105
mm-wave IC Interconnects

## Slide 106: Transmission Lines
A pair of wires with regular spacing, dielectric loading along the length. These have inductance per unit length and capacitance per unit length. Forward and reverse waves propagate. Reflections will occur if lines are not terminated in Zo

## Slide 107: Transmission Lines for On-Wafer Wiring
H
W
microstrip line
coplanar waveguide
0V
0V
0V
+V
0V
+V
geometry
voltages
currents
I
I
H
W
W+2S
I
0
I/2
I/2

## Slide 108: Skin loss
H
W
~W +2H

## Slide 109: Lateral Modes (1)

## Slide 110: Lateral Modes (2)

## Slide 111: Lateral Modes (3)→ Junction Parasitics

## Slide 112: Substrate Modes

## Slide 113: Substrate Mode Coupling: Microstrip

## Slide 114: Substrate Mode Coupling: CPW
kz

## Slide 115: Transmission lines: the problem

## Slide 116: III-V MIMIC Interconnects -- Classic Substrate Microstrip
kz
Strong coupling when substrate approaches ~ld / 4 thickness
H
W
Thick Substrate → low skin loss
Zero ground inductance in package
High via inductance
12 pH for 100 mm substrate -- 7.5 W @ 100 GHz
TM substrate mode coupling
Line spacings must be ~3*(substrate thickness)
lines must be widely spaced
ground vias must be widely spaced
all factors require very thin substrates for >100 GHz ICs → lapping to ~50 mm substrate thickness typical for 100+ GHz
No ground plane breaks in IC

## Slide 117: Coplanar Waveguide
kz
Parasitic slot mode
-V
0V
+V
0V
No ground vias No need (???) to thin substrate
Parasitic microstrip mode
+V
+V
+V
0V
Hard to ground IC to package
substrate mode coupling or substrate losses
ground plane breaks → loss of ground integrity
Repairing ground plane with ground straps is effective only in simple ICs In more complex CPW ICs, ground plane rapidly vanishes → common-lead inductance → strong circuit-circuit coupling
40 Gb/s differential TWA modulator driver note CPW lines, fragmented ground plane
35 GHz master-slave latch in CPW note fragmented ground plane
175 GHz tuned amplifier in CPW note fragmented ground plane
poor ground integrity
loss of impedance control
ground bounce
coupling, EMI, oscillation
III-V: semi-insulating substrate→ substrate mode coupling
Silicon conducting substrate → substrate conductivity losses

## Slide 118: If It Has Breaks, It Is Not A Ground Plane !
signal line
signal line
ground plane
coupling / EMI due to poor ground system integrity is common in high-frequency systems whether on PC boards ...or on ICs.

## Slide 119: No clean ground return ? → interconnects hard to model
35 GHz static divider interconnects have no clear local ground return interconnect inductance is non-local interconnect inductance has no compact model
InP 8 GHz clock rate delta-sigma ADC
8 GHz clock-rate delta-sigma ADC thin-film microstrip wiring every interconnect can be modeled as microstrip some interconnects are terminated in their Zo some interconnects are not terminated ...but ALL are precisely modeled

## Slide 120: III-V MIMIC Interconnects -- Thin-Film Microstrip
fewer breaks in ground plane than CPW
narrow line spacing → IC density
... but ground breaks at device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
H
W
...need to flip-chip bond
no substrate radiation, no substrate losses
InP 34 GHz PA (Jon Hacker , Teledyne)

## Slide 121: III-V MIMIC Interconnects -- Inverted Thin-Film Microstrip
No breaks in ground plane
narrow line spacing → IC density
... no ground breaks at device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
...need to flip-chip bond
Some substrate radiation / substrate losses
InP 150 GHz master-slave latch
InP 8 GHz clock rate delta-sigma ADC

## Slide 122: VLSI mm-wave interconnects with ground integrity
negligible breaks in ground plane
narrow line spacing → IC density
negligible ground breaks @ device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
...need to flip-chip bond
no substrate radiation, no substrate losses
Also: Ground plane at *intermediate level* permits critical signal paths to cross supply lines, or other interconnects without coupling. (critical signal line is placed above ground, other lines and supplies are placed below ground)

## Slide 123: Modeling Interconnects, Passives in Tuned IC's
Interconnects are tuning elements
Narrow bandwidths→ precision is critical
Initial IC simulation uses CAD-systems' library of passive element models.
Second design cycle: 2.5-Dimensional electromagnetic simulation of: lines, junctions, stubs, capacitors, resistors, pads.
Third design cycle: 2.5-D simulation of entire IC wiring (if possible); otherwise, of large blocks (gain stages)
150-200 GHz HBT amplifier, Urteaga et al, IEEE JSSCC , Sept. 2003
185GHz HBT amplifier, Urteaga et al, IEEE IMS, May. 2001
1-180GHz HBT amplifier, Agarwal et al, IEEE Trans MTT , Dec.. 1998

## Slide 124: ICs in Thin-Film (Not Inverted) Microstrip
Note breaks in ground plane at transistors, resistors, capacitors

## Slide 125: ICs in Thin-Film (Not Inverted) Microstrip
Note breaks in ground plane at transistors, resistors, capacitors

## Slide 126: ICs in Thin-Film Inverted Microstrip
100 GHz differential TASTIS Amp. 512nm InP HBT

## Slide 127: Power supply problems
local resonances between bypass cap and supply interconnects global LC standing-wave resonances on supply bus
Detuning of individual stages Coupling, feedback via supply→ oscillation, loss of path isolation

## Slide 128: Power supply problems
The supply impedance will detune individual stages.

## Slide 129: Power supply problems
Here, the supply is terminated by 50 Ohms through a bias T. This avoids resonances. More generally, we must simulate system for wide range of external supply impedance.
Model the supply in all simulations. "If it is on the {IC, PCB, probe station}, put it in the simulation."

## Slide 130: Transmission-lines in 500+ GHz ICs
Inverted microstrip: the problem is ground via inductance

## Slide 131: Transmission-lines in 500+ GHz ICs
Grounded CPW: lower ground inductance, metal 3 ground plane suppresses ground bounce
J. Hacker , Teledyne IMS 2013

## Slide 132: Differential mm-wave stages
Common-emitter
M. Seo, Teledyne
Common-base
M. Seo, 2013 IMS
Virtual ground→ avoids ground via inductance  Avoids power-supply coupling  Potential problems with common mode ✘

## Slide 133: mm-wave common-mode instability
In all amplifiers, stability must be ensured from DC-fmax. Differential & common-mode stability must be ensured from DC-fmax Simple LNA inductive tuning is, for example, problematic

## Slide 134: Pseudo-Differential Stages
No common-mode instability problem. Power-supply is virtual ground. No supply detuning of output network Improved power-supply isolation (oscillation, unwanted signal coupling)

## Slide 135
20+ GHz digital & mixed-signal design

## Slide 136: Modeling Interconnects: Digital & Mixed-Signal IC's
longer interconnects: lines terminated in Zo → no reflections.
Shorter interconnects: lines NOT terminated in Zo . But they are *still* transmission-lines. Ignore their effect at your peril !
If length << wavelength, or line delay<<risetime, short interconnects behave as lumped L and C.
Modeling: 2.5D, library Tline, or L-C

## Slide 137: Design Flow: Digital & Mixed-Signal IC's
All interconnects: thin-film microstrip environment. Continuous ground on one plane.
2.5-D simulations run on representative lines. various widths, various planes same reference (ground) plane.
Simulation data manually fit to CAD line model effective substrate er , effective line-ground spacing.
Width, length, substrate of each line entered on CAD schematic. rapid data entry, rapid simulation.
Resistors and capacitors: 2.5-D simulation→ RLC fit RLC model used in simulation.

## Slide 138: High Speed ECL Design
Followers associated with inputs, not outputs Emitters never drive long wires. (instability with capacitive load)
Double termination for least ringing, send or receive termination for moderate-length lines, high-Z loading saves power but kills speed.
Current mirror biasing is more compact. Mirror capacitance→ ringing, instability. Resistors provide follower damping.

## Slide 139: High Speed ECL Design
Layout: short signal paths at gate centers, bias sources surround core. Inverted thin film microstrip wiring.
Example: 8:1 205 GHz static divider in 256 nm InP HBT.
Key: transistors in on-state operate at Kirk limited-current. → minimizes Ccb/Ic delay.
205 GHz divider, Griffith et al, IEEE CSIC, Oct. 2010
Key: transistors designed for minimum ECL gate delay*, not peak (ft , fmax). *hand expression, charge-control analysis

## Slide 140: Differential stages: schematic vs. floorplan

## Slide 141: Example: 40 GS/s S/H clock buffer
Itail=6 mA
Itail=12 mA

## Slide 142: Example: 40 GS/s S/H clock buffer

## Slide 143: Example: 40 GS/s S/H clock buffer

## Slide 144: 20GHz Op-Amps for Linear 2 GHz Amplification
Even for 2 GHz operation, loop bandwidths must 20-40 GHz.
need very fast transistors
physically small feedback loop;
bias components surround active core.
Griffith et al, IEEE IMS, June. 2011
input power, dBm
output power, dBm
linear response
2-tone intermodulation
increasing feedback
Reduce distortion with
strong negative feedback
R. Eden

## Slide 145
86 GHz Power Amplifier

## Slide 146: mm-Wave Power Amplifier: Challenges
needed: High power / High efficiency / Small die area ( low cost)
Extensive power combining
Compact power-combining
Efficient power-combining
Class E/D/F are poor @ mm-wave insufficient fmax , high losses in harmonic terminations
Goal: efficient, compact mm-wave power-combiners

## Slide 147: Parallel Power-Combining
Output power: POUT = N x V x I Parallel connection increases POUT
Load Impedance: ZOPT = V / (N x I) Parallel connection decreases Zopt
High POUT→ Low Zopt
Needs impedance transformation: lumped lines, Wilkinson, ...
High insertion loss Small bandwidth Large die area

## Slide 148: Series Power-Combining & Stacks
Parallel connections: Iout=N x I Series connections: Vout=N x V
Local voltage feedback: drives gates, sets voltage distribution
Design challenge: need uniform RF voltage distribution need ~unity RF current gain per element
...needed for simultaneous compression of all FETs.
Output power: Pout=N2 x V x I Load impedance: Zopt=V/I Small or zero power-combining losses Small die area How do we drive the gates ?
Shifrin et al., 1992 IEEE-IMS; Rodwell et al., U.S. Patent 5,945,879, 1999; Pornpromlikit et al., 2011 CSICS

## Slide 149: Ideal Tri-axial Line
Two separate transmission lines (m3-m2, m2-m1)
 E, H fields between m3 and m1 perfectly shielded

## Slide 150: Sub-λ/4 Baluns for Series Combining
Sub-l/4 balun : stub→ inductive tunes transistor Cout ! short lines→ low losses short lines → small die
Standard l/4 balun : long lines → high losses → large die
Balun combiner: 2:1 series connection each source sees 25 W → 4:1 increased Pout
Park et al., 2013 CSICS, 2014 IEEE-IMS

## Slide 151: Baluns in Real ICs
  1) M1 as a GND
  2) Slot-type transmission lines (M1-M2), AC short (2 pF MIM)
  3) Microstrip line (M2-M3), E-field shielding NOT negligible
  4) Sidewalls between M3-M1 (Faraday cages), l/16 length
1)
2)
3)
4)

## Slide 152: Two-Stage PA IC Test Results (86GHz)
  Gain: 17.5 dB
  PSAT: >200 mW @ 3.0 V
  PAE: >30 %
  Power density (power/die area)
  = 307 mW/mm2 (including RF pads) = 927 mW/mm2 (core area)
Large signal measurements
  IC size: 825 x 820 um2
[H. Park et al, CSICS 2013] 30% PAE W-Band InP Power Amplifiers Using Sub-Quarter-Wavelength Baluns for Series-Connected Power-Combining

## Slide 153: 4:1 series-connected 81GHz power amplifier
17 dB Gain 470 mW Psat 23% PAE Teledyne 250 nm InP HBT 2 stages, 1.0 mm2(incl pads)
Park et al., 2014 IEEE-IMS

## Slide 154
IC example: 220 GHz power amplifier

## Slide 155: Millimeter-wave imaging
235 GHz video-rate synthetic aperture radar
10,000-pixel, 94GHz imaging array→ 10,000 elements
Golcuk: Trans MTT, Aug 2014
1 transmitter, 1 receiver 100,000 pixels 20 Hz refresh rate 5 cm resolution @ 1km 50 Watt transmitter (tube, solid-state driver)
Demonstrated: SiGe (UCSD/Rebeiz) ~1.3kW: 10,000 elements Lower-power designs: InP, CMOS, SiGe (UCSB, UCSD, Virginia Poly.)

## Slide 156: 90 mW, 220 GHz Power Amplifier
Reed (UCSB) and Griffith (Teledyne): CSIC 2012 Teledyne 250 nm InP HBT
active area, 1.02 x 0.85 mm die: 2.42 x 1.22 mm
156
Notes: when you show the IBM FET, you say:
"because we want a device with the geometry taken for granted in silicon VLSI"
..source/drain pitch at most a few times the gate length.

## Slide 157: 214 GHz InP HBT Power Amplifier
UCSB/Teledyne
Gain: 25dB S21 Gain at 220GHz
Saturated output power: 164mW at 214GHz
Output Power Density:0.43 W/mm
PAE: 2.4%
Technology: 250 nm InP HBT
(no die photo) 2.5mm x 2.1 mm
Reed et al, 2014 CSICS http://ieeexplore.ieee.org/xpls/abs_all.jsp?arnumber=6659187&tag=1

## Slide 158: 214 GHz 180mW Power Amplifier (330 mW design)
2.3 mm x 2.5 mm
Reed, Griffith CSICS2013 Teledyne 250 nm InP HBT
158
Reed et al, 2014 CSICS http://ieeexplore.ieee.org/xpls/abs_all.jsp?arnumber=6659187&tag=1

## Slide 159: 220 GHz power amplifiers; 256nm InP HBT

## Slide 160: ICs in Thin-Film (Not Inverted) Microstrip
Note breaks in ground plane at transistors, resistors, capacitors

## Slide 161: 220 GHz measurement

## Slide 162: Power combined modules
Slide from Z. Griffith IMS 2016 Presentation

## Slide 163
mm-Wave power

## Slide 164: Teledyne: 1.9 mW, 585 GHz Power Amplifier
Output Power
12-Stage Common-base
2.8 dBm Psat
>20 dB gain up to 620 GHz
What limits output power in sub-mm-wave amplifiers ?
S-parameters
M. Seo et al., Teledyne Scientific: IMS2013

## Slide 165: Sub-mm-wave PAs: need more current !
common-base HBT
base
emitter
collector
ground plane
HBTs with microstrip combiner
3 mm max emitter length (> 1 THz fmax) 2 mA/mm max current density Imax= 6 mA Maximum 3 Volt p-p output Load: 3V/6mA= 500 W
Combiner cannot provide 500 W loading

## Slide 166: Multi-finger HBTs: more current, lower fmax
More current → lower cell load resistance
one-finger common-base HBT
two-finger power cell
four-finger power cell: parasitics
base
emitter
collector
ground plane
base
emitter
collector
base
emitter
collector
unequal emitter inductances
emitter-collector capacitance
Reduced fmax, reduced RF gain: common-lead inductance→ Z12 feedback capacitance→ Y12 phase imbalance between fingers.
Worse at higher frequencies: less tolerant of cell parasitics less current per cell higher required load resistance Can optimum load be reached ?

## Slide 167: Sub-mm-wave transistors: need more current
InP HBTs: thinner collector→ more current hotter→ improve heat-sinking or: longer emitters→ thicker base metal
GaN HEMTs: much higher voltage 100+ GHz: large multi-finger FETs not feasible Need high current to exploit high voltage.
Need more mA/mm or longer fingers
Example: 2mA/mm, 100 mm max gate width, 50 Volts 200mA maximum current 50 Volts/200mA= 250 W load→ unrealizable.

## Slide 168
50-500GHz Wireless

## Slide 169
IC example: 150 GHz CMOS amplifier

## Slide 170: 3-stage 150-GHz Amplifier; IBM 65 nm CMOS
Acknowledgement: IBM
M. Seo, B. Jagannathan, J. Pekarik, M. Rodwell, IEEE JSSCC, Dec. 2009
Dummy-prefilled microstrip lines

## Slide 171
IC example: 140 GHz spatial multiplexing

## Slide 172: Massive Spatial Multiplexing
Two applications: Spatially multiplexed networks multiple independent beams carrying independent data → spectral re-use for massive capacity
mm-wave line-of-sight MIMO spatial multiplexing for increased capacity
These use similar signal processing hardware

## Slide 173: Arrays for single-beam links
Single-beam arrays: steerable, high gain, for mm-wave links.
Simple hardware: one RF port for IC, one phase-shifter for each element

## Slide 174: Multi-beam links: hardware design
multiple independent beams each carrying different data each independently aimed # beams = # array elements
Hardware: multi-beam phased array ICs

## Slide 175: Multi-Beam Links: Analog Beamformer Matrix
I/Q matrix at baseband
varying coefficients → track/aim beams
Designs: March tapeout GF (ex IBM) 45nm SOI 16 beams: 32 x 32 matrix 1024 matrix elements area: 2.25 mm2 power: 2.25W bandwidth: ~5 GHz ? aggregate ~160 Gb/s. Also for tapeout 140 GHz front-ends for these

## Slide 176: Multi-Beam Links: Analog Beamformer Matrix

## Slide 177: Multi-Beam Links: Analog Beamformer Matrix
I/Q matrix at baseband
varying coefficients → track/aim beams
Designs: March tapeout GF (ex IBM) 45nm SOI 16 beams: 32 x 32 matrix 1024 matrix elements area: 2.25 mm2 power: 2.25 W bandwidth: ~5 GHz ? aggregate ~160 Gb/s. Also for tapeout 140 GHz front-ends for these later: RF for 38GHz, 60 GHz
array
cell
switched gm block

## Slide 178
140 GHz MIMO receiver front-end
LO
RF
RF
RF
RF
Ch.1
Ch.2
Ch.3
Ch.4
Size: 1075 x 1760 um2
Power div.
Single-channel layout

## Slide 179
Single-ended vs differential
 | Single-ended | Differential
Gain | - | -
Power consumption | Low | High
Design complexity | Low | High (Balun is required)
Isolation (S12) & Stability | Low | High (Cgd cancellation)
Power supply (VDD & VSS) immunity | Poor | Good
Power supply immunity is critical  differential structure

## Slide 180
Low noise amplifier
LNA design:
3-stage differential CS amplifier
Cgd cancellation
Transformers for matching networks and sing.-to-diff.
24 x 1um

## Slide 181
SGF vs PGF
Simulation results includes BSIM model and PEX results
(PEX  capacitance and resistance due to PC, CA and M1)
*PC: poly, CA: connection between poly and metal 1, M1: metal 1

## Slide 182
FET footprint
Series gate feeding
Parallel gate feeding
Gate
Gate
(M1)
Gate
(M2)
Drain
(M2)
Source
(M1)
Drain
(M2)
Source
(M2)

## Slide 183
FET footprint - PGF
PGF
- PGF and SGF have similar performances (MSG, NF)
- SGF is hard to extract the inductance of the gate
feeding line
- Source can directly connect to ground
(M1 is the ground plane)
SGF
Gate
Gate

## Slide 184
FET modeling
Parallel Gate Feeding
Gate
(M2)
Drain
(M2)
Source
(M1)
LB
M1
BEOL: M1-M2-M3-C1-C2-B1-B2-B3-UA-UB-LB
Transistor modeling:
BSIM + PEX + EM simulation
(BSIM & PEX from the foundry)

## Slide 185: FET differential pair layout
Cgd cancellation
: MOM Cap
M1 ground plane
Cgd cancellation – better isolation & gain
Gate+
(LB)
Gate-
(LB)
Drain+
(LB)
Drain-
(LB)
BEOL: M1-M2-M3-C1-C2-B1-B2-B3-UA-UB-LB

## Slide 186
Matching networks
VDD: M2-M3-C1-C2
Gate bias: M2
UB-LB
M1 ground plane
For matching:
Optimize transistor size & transformer diameter
Center-tapped transformer for DC biasing (VDD, VGS)
BEOL: M1-M2-M3-C1-C2-B1-B2-B3-UA-UB-LB

## Slide 187
LNA layout
Size: 315 x 170 um2

## Slide 188
Gain & NF
Gain 19.2 dB (peak gain 20 dB @ 145 GHz)
NF: 5.2 dB

## Slide 189
Linearity
IIP3: -5.84 dBm, Input P1dB: -13.87 dBm

## Slide 190
Summary - LNA
Gain | 19.2 dB (Peak 20 dB @ 145 GHz)
NF | 5.2 dB
IIP3 | -5.8 dBm
Input P1dB | -13.87 dBm
Power consumption | 41 mA @ 1 V
Size | 315 x 170 um2

## Slide 191
Down-conversion mixer
Mixer design:
Single-balanced active I/Q mixer
CS buffer for testing (buffer gain ≈ 1)
Size: 140 x 230 um2
LO_I
LO_Q
I/Q mixer

## Slide 192
Mixer core layout
RF input
(LB)
LO +
(LB)
LO –
(LB)
IF output
(C1)
M1 ground plane
FET
BEOL: M1-M2-M3-C1-C2-B1-B2-B3-UA-UB-LB

## Slide 193
LO distribution network:
Wilkinson power divider
Quadrature hybrid (I/Q generation)
Four-channel receiver
(12 dBm)

## Slide 194
Layout
LO
RF
RF
RF
RF
Ch.1
Ch.2
Ch.3
Ch.4
Size: 1075 x 1760 um2
Power div.
Single-channel layout
Wilkinson power divider

## Slide 195
Conversion gain & NF (single-channel)
Gain 17 dB (single-channel IF_I output)
NF : 5.8 dB (dsb)

## Slide 196
Linearity (single-channel)
IIP3: -10.7 dBm, Input P1dB: -18.74 dBm

## Slide 197
Summary - receiver
Gain | 17 dB (Single-channel IF_I output)
NF | 5.8 dB
IIP3 | -10. 7 dBm
Input P1dB | -18.7 dBm
Power consumption | 41 mA (LNA) + 2 mA (I/Q mixer) + 14 mA (IF-I/Q buffers) @ 1 V (Single-channel)
Size | 1075 x 1760 um2

## Slide 198
IC example: 94 GHz low-power-array

## Slide 199: Millimeter-wave imaging
10,000-pixel, 94GHz imaging array→ 10,000 elements
Golcuk: Trans MTT, Aug 2014
Demonstrated: SiGe (UCSD/Rebeiz) ~1.3kW: 10,000 elements Lower-power designs: InP, CMOS, SiGe (UCSB, UCSD, Virginia Poly.)
System concept: Bruce Wallace DARPA. 1st ICs (SiGe) Rebeiz, UCSD.

## Slide 200: Millimeter-wave imaging
10,000-pixel, 94GHz imaging array→ 10,000 elements
Golcuk: Trans MTT, Aug 2014
Demonstrated: SiGe (UCSD/Rebeiz) ~1.3kW: 10,000 elements Lower-power designs: InP, CMOS, SiGe (UCSB, UCSD, Virginia Poly.)
100 pixel × 100 pixel image→ 10,000 array elements. ~130 mW DC power per element → 1.3 kW system power requirement. Problem: required size and weight of heat sink.

## Slide 201: 94 GHz low-power IC design: transistors
At 1mW dissipation, ~17 dB gain is feasible→ low power ICs.
Teledyne: 130nm InP HBT: high-fmax bias
Teledyne: M. Urteaga et al: 2011 DRC
Teledyne: 130nm InP HBT: low-power bias
130nm × 3 mm emitter

## Slide 202: 94 GHz low-power IC design: transistors
BJTs
FETs

## Slide 203: Phased array
IC can transmit on vertical (V) or horizontal (H) polarizations (one at a time) IC can receive on vertical (V) and horizontal (H) polarizations (simultaneously) Each mode has phase-shifter, VGA. Signal distribution on backplane. InP IC: requires low-speed CMOS digital control IC
1770 um x 1550 um

## Slide 204: Low-power, low-voltage mm-wave design
Extensive use of current mirrors, translinear techniques
Gain & switching
Low-power T/R switching
VGA / switch
Multiplier→ mixer, modulator, phase-shifter

## Slide 205: Low-power, low-voltage mm-wave design
Antenna switch
LNA
backplane T/R switch
PA & V/H switch

## Slide 206: Phase-shifter and control circuits
760 um x 640 um

## Slide 207: Phase-shifter measurement results (1 V)
Power consumption: 4.2 mA @ 1 V

## Slide 208: Low-noise amplifier
Noise matching for input
Conjugate matching for inter-stage
Gain matching for output
Power consumption: 2 mA @ 1.5 V
660 um x 510 um

## Slide 209: LNA Measurement results (1 V)
Power consumption: 2.0 mA @ 1 V
Gain: 16.3 dB @ 94 GHz (peak gain)

## Slide 210: Noise measurement setup
Calibration
Measurement
-1 dB
-1 dB
Loss before the DUT: compensated using the NFA’s internal function
therefore, measured gain should be subtracted by -1 dB
Noise source
Mixer
(LO @ 94 GHz)
W-band
Amp.

## Slide 211: Transceiver measurement results

## Slide 212: Receiver noise

## Slide 213: 94 GHz transceiver: performance summary
 |  |  | @Vcc=1.5V | @Vcc=1.0V
Power Amplifier + V/H SW | Output Power P3dB | dBm | 6.9 | 3.5
 | Power Gain @P3dB | dB | 14 | 14
 | PAE | % | 17 | 12.7
 | Pdiss @ P3dB | mW | 27.2 | 16.9
 | Pdiss (small-signal) | mW | 22.5 | 16.4
 | Pdiss (core exclude bias ckt) | mW | 17.55 | 11.45
 | Size (exclude Pads) | µm | 475*475 | 475*475
VGA | Power Gain (Rx/Tx) | dB | 12.5/10.9 | 13.4/11.5
 | NF (max gain) | dB | 4.8/7.8 | 4.6/7.7
 | NF (max gain - 6dB) | dB | 7.1/9.4 | 6.6/9.3
 | Input P1dB | dBm | -12.4/-9.6 | -15.9/-15
 | OIP3 | dBm | 6.7/7.6 | -1.8/-3
 | Pdiss | mW | 9 | 6.4
 | Pdiss (core exclude bias ckt) | mW | 6.9 | 4.6
 | Size (exclude Pads) | µm | 530*900 | 530*900
LNA | Power Gain | dB | 15.1 | 16.3
 | NF | dBm | 5 | 5
 | Input P1dB | dBm | -21.9 | -24.5
 | OIP3 | dBm | -1.7 | -3
 | Pdiss | mW | 4.95 | 3.95
 | Pdiss (core exclude bias ckt) | mW | 3.5 | 2
 | Size (exclude Pads) | µm | 480*280 | 480*280
Phase Shifter | Power Gain (Rx/Tx) | dB | -5±1.5 | -5±1.5
 | NF | dB | 14.9 | 14.6
 | Input P1dB | dBm | 9 | 6
 | OIP3 | dB | 10.9 | 2
 | Pdiss | mW | 6.5 | 4.2
 | Pdiss (core exclude bias ckt) | mW | 6.5 | 4.2
 | Size (exclude Pads) | µm | 660*340 | 660*340
SPDT Antenna T/Rx SW | Loss | dB | 2 | 1.8
 | Isolation | dB | 19.5 | 18.5
 | P1dB | dBm | 14 | 14
 | Pdiss | mW | 6.8 | 4.8
 | Pdiss (core exclude bias ckt) | mW | 4.8 | 2.8
 | Size (exclude Pads) | µm | 200*680 | 200*680
Rx Channel | Power Gain | dB | 21 | 22.7
 | NF | dB | 8.5 | 8
 | Fractional BW | % | 7.6 | 7.5
 | Input P1dB | dBm | -22.9 | -27.9
 | IIP3 | dBm | -16.3 | -24.3
 | Pdiss | mW | 19.2 | 12.9
 | Pdiss (core exclude bias ckt) | mW | 17.25 | 11
Tx Channel | Power Gain | dB | 22.2 | 22.4
 | Pout (P3dB) | dBm | 3.8 | 0.1
 | Fractional BW | % | 6.7 | 6.7
 | Output P1dB | dBm | 0.8 | -3.4
 | OIP3 | dBm | 10 | 3.8
 | Pdiss | mW | 39.7 | 28.7
 | Pdiss (core exclude bias ckt) | mW | 31.5 | 20.5
Simulation

## Slide 214
IC example: 1-25 GHz dual-conversion receiver

## Slide 215: Dual Conversion: Wide Tuning
Low (2GHz) IF→ image & LO responses close to RF carrier
High (100GHz) IF→ image & LO responses far from RF carrier
Dual conversion: a standard approach in RF receivers.
Modern THz IC processes→ 100 GHz IF easily feasible → Image-response-free 1-50 GHz receiver

## Slide 216: W-band Waveguide Filters
1 GHz filter bandwidth is easy; 100 MHz should be just feasible.
our effort: design the ICs, purchase the filter.

## Slide 217: Choice of Frequency Plan
Distribution Statement
LO below IF: triplers have residual output @ 2fin → maximum 1.5:1 tuning ratio → maximum 67-100 GHz LO tuning ~1-33 GHz RF tuning Need 67-100GHz LO driver PA present designs (lower-risk)
217
LO above IF: maximum 100-150 GHz LO tuning ~1-50 GHz RF tuning Need 100-150GHz LO driver PA At ~200-300mW output power higher-risk.

## Slide 218: Full receiver configuration: 2 chips to ease testing

## Slide 219: Receiver: down-conversion block
5240 um x 1160 um

## Slide 220: Receiver: up-conversion block
4300 um x 1160 um
1 GHz -25 GHz

## Slide 221: Mixer
Diode mixer: High dynamic range. base-collector diodes: no saturation series-connected→ high IP3 requires high LO drive power
Baluns: tri-plane design some are sub-quarter-wavelength

## Slide 222: 9:1 LO Multiplier
2500 um x 1160 um
simulation
measured

## Slide 223: Differential LO Driver Amplifier: 67-100GHz
Ultra-broadband LO driver limited by 67GHz substrate mode ? data shows otherwise.
High Power required by high-IP3 mixer >100mW over full bandwidth > 250mW at most frequencies.
Topology 4:1 series connected by baluns compact, efficient, ultra-broadband 2 cascaded stages

## Slide 224: Differential LO Driver Amplifier: 67-100GHz

## Slide 225: High dynamic range IF amplifier
low noise figure high third-order intercept
low/moderate gain
Common-emitter
Pseudo-differential Strong inductive degeneration high IP3. partly converges noise & S11 tuning

## Slide 226: First IF Amplifier
Distribution Statement
226
5.5-6 dB gain
6.5 dB noise figure
95-105GHz
WITHOUT PADS: 551 um X 575 um, 100 mW DC power
20.7dBm IIP3 (26.7dBm OIP3)
baluns for probe testing only
Simulations

## Slide 227: IF Amplifier measurement results
Power consumption: 94 mA @ 2 V Peak gain: 4.3 dB @ 95 GHz, 4.0 dB @ 100 GHz
Low-gain (high-IIP3) design
Power consumption: 97 mA @ 2 V
Peak gain: 5.9 dB @ 95 GHz, 5.7 dB @ 100 GHz
Low-gain (high-IIP3) design

## Slide 228: IF Amplifier measurement results

## Slide 229: Performance: upconversion block

## Slide 230: Upconversion measurement: Gain, IM3
Coupler
Power
sensor
1
Harmonic
mixer
Spectrum
analyzer
Power meter
Signal
generator
(Multiplier, LO)
Signal
generator (RF)
Frequency measurement: Harmonic mixer
Power measurement: power meter
Harmonic mixer
LO = (RF+IF)/n
In our test:
n=10 and IF = 1 GHz
*Harmonic mixer LO frequency was
adjusted to measure LO feedthrough
(Harmonic mixer IF =1 GHz)

## Slide 231: Downconversion measurement: IP3

## Slide 232
mm-Wave Wireless

## Slide 233: mm-Wave Wireless Electronics
Mobile communication @ 2Gb/s per user, 1 Tb/s per base station
Requires: large arrays, complex signal processing, high Pout , low Fmin
VLSI beamformers VLSI equalizers III-V LNAs & PAs (?)

## Slide 234
(backup slides follow)