## Slide 1: Making better transistors: beyond yet another new materials system
Mark Rodwell, University of California, Santa Barbara
Dagstul Worshop, Feb 6-11, 2017.
Notes: Making better transistors: beyond yet another new materials system.
In ~55 years of IC development, industry has concentrated on making switches smaller; universities have mostly concentrated on the complementary role of making them from new materials. Thus has university electron device research progressed from silicon to germanium and SiGe, the arsenide, phosphide and then antimonide III-V's, then carbon nanotubes, and today 2D semiconductors. Beyond SiGe, there seems but little hope that these more recent materials might benefit transistors in computer ICs.
Perhaps we should focus instead on improving their shape ? Corrugating a FET channel, in the style of a folded piece of paper, produces a device with transport distance much larger than its footprint; we can use this to improve electrostatics and suppress source-drain tunneling currents in few-nm-footprint transistors. Corrugating the channel in the perpendicular direction increases the drive current per unit IC area, which we then might trade for lower-voltage, lower-power operation. With FETs, making low-resistance yet small contacts is as much a problem as is making short gates: should we corrugate the metal-semiconductor interface to reduce the interface resistance ?
Or, should we change their band structure ? In tunnel FETs, we can add several heterojunctions, and so increase the desired on-state tunneling currents while decreasing the unwanted off-state leakage currents. Yet, I can offer nothing beyond this single example, albeit one that I presently find of great interest.
Finally, perhaps we might change their function ? One focus of this workshop is to explore the merging of logic and memory. We might do this at either within the transistor or within low-level logic design. It is not yet clear to this circuit designer that a logic-plus-memory transistor would be markedly more useful than, for example, simple merged logic using pass transistors and gate capacitances. I will do my best to examine their potential utility.

## Slide 2: What does VLSI need ?
Small transistors: plentiful, cheap
Small transistors→ short wires small delay CVDD /I low switching energy CVDD2/2
Low supply voltages low energy CVDD2/2
Large on-currents small delay CVDD /I
Low leakage current thermal: Ioff > Ion*exp(-qVDD/kT) want low VDD yet low Ioff.
Ion

## Slide 3: Transistor Research
Make the switch smaller (scaling)
Make it from different materials
Change its shape
Change its internal operation: bandgap engineering
Change what we do with it.

## Slide 4: We can't make MOSFETs much smaller
Tunneling: can't make gate insulator any thinner
→ smaller devices have poor electrostatic control, don't turn off
Tunneling: can't make channel much shorter
→ smaller devices have high source-drain tunneling, don't turn off
Expensive lithography: EUV, multiple patterning

## Slide 5: New Materials: III-V semiconductors ?
S. Lee et al., VLSI Symp. 2014
Vertical Spacer
N+ S/D
Lg~25 nm
record for III-V
= best UTB SOI silicon

## Slide 6: New Materials: 2-D semiconductors ?
Silicon
MoS2
Phosphorene
Does 1-atom-thick channel help ? 2D or 3D: the gate oxide won't scale the oxide sets a minimum gate length 1-atom-thick channels don't help much
If oxides won't scale, we must make fins with 2D, can we make fins ? later, will need to make nanowires...
Ballistic drive currents don't win either high m*, and/or high DOS mobility sufficient for ballistic ?

## Slide 7: When it gets crowded, build vertically
2-D integration: wire length # gates1/2
Los Angeles: sprawl
Manhattan: dense
3-D integration: wire length #gates1/3
LA is interconnect-limited
1) Chip stacking (skip) 2) 3D transistors: corrugation (change the shape)

## Slide 8: Corrugated surface→ more surface per die area

## Slide 9: Corrugated surface→ more current per unit area
Cohen-Elias et al., UCSB 2013 DRC
J .J. Gu et al., 2012 DRC, Purdue 2012 IEDM

## Slide 10: Corrugation: same current, less voltage, less CV2

## Slide 11: Forming tall fins by sidewall regrowth (ugly)
Cohen-Elias et al., 2013 DRC

## Slide 12: Confined Epitaxial Lateral Overgrowth
Semiconductor regrowth into hollow glass boxes formed on wafer surface Semiconductor thicknesses controlled by ALD layer thickness: atomic precision
L. Czornomaz et. al, (IBM) 2015 & 2016 VLSI Symposia

## Slide 13: CELO: Can we grow 3-D structures ?
With a few process tricks, can we make growth templates for 3-D structures ?

## Slide 14: Fixing source-drain tunneling by increasing mass ?
Source-drain tunneling leakage:
Fix by increasing effective mass ?
This will decrease the on-current:
?
!
long gate→ big
shorter gate→ smaller
less current
wider→ more current
big again !
(also increases transit time)

## Slide 15: Fixing source-drain tunneling by corrugation
Transport distance > gate footprint length Only small capacitance increase
CY Huang et al, 2015 DRC

## Slide 16: Fixing source-drain tunneling by corrugation ?
CELO growth over ridge
3D structure
transport length >> footprint
improves electrostatics ...like finFET
improves S/D tunneling ...unlike finFET
Gate oxide is SiOxNy , not HfO2 → thinner @ given leakage How to reduce gate footprint below ~5nm ?

## Slide 17: Changing the band structure: tunnel FETs
TFET: bandgap of p-type source truncates source thermal distribution:
Problem: 4-6nm tunnel barriers→ ~3% tunneling probability→ very low current.

## Slide 18: [110] gives more on-current than [100]
high confinement mass low transport mass
low confinement mass high transport mass
P. Long et al., EDL 3/2016
valence band

## Slide 19: Add more Heterojunctions: much more current.
Added heterojunctions→ greater built-in potential→greater field→ thinner barrier → higher tunneling probability (~80%)→ 30:1 more current.
Source HJ: S. Brocard, et al., EDL, 2/2014; Channel HJ: P. Long et al., EDL 3/2016

## Slide 20: 3HJ still have higher ON/OFF ratio than GaAsSb/InAs
3HJ 516A/m
GaAsSb/InAs 75A/m
3HJ still have higher ON/OFF ratio than GaAsSb/InAs when acoustic and non-polar optical phonon scattering are considered.
P. Long, J. Huang, M. Povolotski: Purdue, Unpublished

## Slide 21: Changing the function: ferroFETs ?
This won't work
need tri-state driver
why not this ?
or this ?
or an input switch.

## Slide 22: Multiple Supplies for Low-Power Logic
Given 200 mV swings on long interconnects,
Line receivers provide 0.1 mA/mm output with 0.1 mA/mm leakage
Line drivers, and logic gates provide 3 mA/mm output with 0.1 mA/mm leakage
Is cost in added die area acceptable ?

## Slide 23
(backup slides follow)

## Slide 24: Record III-V MOS
S. Lee et al., VLSI 2014
Vertical Spacer
N+ S/D
Lg~25 nm
record for III-V
= best UTB SOI silicon

## Slide 25: Vertical FETs ????
Can have a smaller footprint.
No clue how to make it !
III-V nanowire growth: much too big

## Slide 26: 3D→shorter wires→less capacitance→less CV2
All three have same drive current, same gate width
Tall fin, "4-D": smaller footprint→ shorter wires

## Slide 27: Minimum Dielectric Thickness & Gate Leakage
→ 0.5-0.7nm minimum EOT constrains on-current electrostatics degrades with scaling → fins, nanowires
High-er materials have lower barriers
Thin dielectrics are leaky

## Slide 28: Quick check: scaling limits
finFET: 5 nm physical gate length. Channel: <100> Si, 0.5, 1, or 2nm thick dielectric: er=12.7, 0.5 or 0.7 nm EOT
NEMO ballistic simulations
Given EOT limits, ~1.5-2nm body is acceptable.
Source-drain tunneling often dominates leakage.
simulation
Notes: N+ S/D: 5*1012/cm2

## Slide 29: TEM images of Lg~12 nm devices
N+InGaAs
InP spacer
InAlAs
Barrier
Lg~12nm
~ 8nm
29
tch~ 2.5 nm
(1.5/1 nm InGaAs/InAs)
Top View
Ni
Cross-setion
N+InP

## Slide 30: ID-VG and ID-VD curves of 12nm Lg FETs
30
Ioff~1.3 nA/μm
Ion~1.1 mA/μm
Ion/Ioff > 8.3∙105
Lg-12nm

## Slide 31
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 32: 130nm /1.1 THz InP HBT: ICs to 670 GHz
614 GHz fundamental VCO
340 GHz dynamic frequency divider
620 GHz, 20 dB gain amplifier
M Seo, TSC IMS 2013
also: 670GHz amplifier J. Hacker , TSC IMS 2013 (not shown)
M. Seo, TSC / UCSB
M. Seo, UCSB/TSC IMS 2010
204 GHz static frequency divider (ECL master-slave latch)
Z. Griffith, TSC CSIC 2010
300 GHz fundamental PLL
M. Seo, TSC IMS 2011
220 GHz 180 mW power amplifier
T. Reed, UCSB CSICS 2013
600 GHz Integrated Transmitter PLL + Mixer
M. Seo TSC
Integrated 300/350GHz Receivers: LNA/Mixer/VCO
M. Seo TSC
81 GHz 470 mW power amplifier
H-C Park UCSB IMS 2014