## Slide 1: 100-340GHz Systems: Transistors and Applications
M.J.W. Rodwell1, Y. Fang1, J. Rode1,2, J. Wu1,3, B. Markman1, S. T. Suran Brunelli1, J. Klamkin1, M Urteaga4
1University of California, Santa Barbara 2Now with Intel 3Now with GlobalFoundries 4Teledyne Scientific and Imaging

## Slide 2: Why 100-340GHz Wireless ?
Wireless networks: exploding demand.
Immediate industry response: 5G. 28, 38, 57-71(WiGig), 71-86GHz increased spectrum, extensive beamforming
Next generation (6G ??): above 100GHz. greatly increased spectrum, massive spectral multiplexing
Plus, TV-like imaging/sensing/radar: cars, airplanes, drones

## Slide 3: 100-340GHz: Benefits & Challenges

## Slide 4: 100-340GHz: Potential Applications
MIMO hub: 128 beams/face, 1Gb/s/user 140 GHz
Point-point MIMO: 340GHz: Tb/s links massive spatial multiplexing
220, 340GHz imaging: drive/fly in fog/rain/snow 300m, 512×64 image, 60Hz, 15dB SNR
Ultra-compact imaging: drones unlike visible: image through fog/smoke/rain

## Slide 5: 140 GHz Spatially Multiplexed Base Station
Each face supports 128 beams @ 1Gb/s/beam.
225 meters range in 50 mm/hr rain
PAs: 16 dBm Pout (per element)
LNAs: 3 dB noise figure
Realistic packaging loss, operating & design margins (20dB total)

## Slide 6: 340 GHz 640 Gb/s MIMO Backhaul
1.6m MIMO array: 8-elements, each 80 Gb/s QPSK; 640Gb/s total 4 × 4 sub-arrays → 8 degree beamsteering
500 meters range in 50 mm/hr rain; 29 dB/km
PAs: 82mW Pout (per element)
LNAs: 4 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 7: Millimeter-Wave Wireless Transceiver Architecture
custom PAs, LNAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.

## Slide 8: 100-1000 GHz Transistors and ICs
 | fmax GHz | Good ICs to (GHz) | complexity | LNAs | PAS | increased bandwidth ?
CMOS | 350 | 150/200 | transceivers | ok | poor: 1-5 mW | not easy
Production SiGe | 300 | 200/250 | transceivers | good | OK: 20-100 mW | depends on $$
R&D SiGe | 700 | 300/500 | transceivers | good | OK: 20-100 mW | 2-3THz
R&D InP HBT | 1150 | 400/650 | PA, converters | poor | good: 100-200 mW | 2-3THz
R&D InP HEMT | 1500 | 500/1000 | LNA | great | weak: 20-50 mW | 2-3THz
R&D GaN | 400 | 120/140 | PAs | good | excellent: 0.1-1W | 600GHz
ICs with useful performance, hero experiments |  |  |  |  |  | 
There are THz transistors today; their bandwidth will increase
Challenge: reducing costs, increasing market size

## Slide 9: Gallium Nitride Power Technologies
N-polar GaN: Mishra, UCSB
GaN is the leading high-frequency power technology

## Slide 10: 130nm / 1.1THz InP HBT Technology
Teledyne: M. Urteaga et al: 2017 IEEE Proceedings
Integrated ~600GHz transmitter
220 GHz, 0.18W power amplifier
UCSB/Teledyne: T. Reed et al: 2013 CSICS
325 GHz, 16mW power amplifier
UCSB/Teledyne: A. Ahmed, 2018 EuMIC Symp.
1.1THz fmax HBT, 3.5 V breakdown
Teledyne/UCSB: M. Urteaga et al: 2011 DRC

## Slide 11
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 12: THz Transistor Measurements
Simple pads: Substrate coupling: need small pads, narrow CPW Ambiguity in pad stripping order. UCSB 130nm HBTs: order not important. Add through & load to remove ambiguity
On-wafer through-reflect-line: No ambiguity from pad stripping. Calibration to line Zo Still must avoid substrate resonances CPW does not work. needs thin-film microstrip or ~25 mm substrate with TSV's
(publication used parallel elements outside)

## Slide 13: Bipolar Transistor Scaling Laws
Narrow junctions. Thin layers High current density Ultra low resistivity contacts

## Slide 14: Challenges at the 64nm/2THz & 32nm/3THz Nodes
Baraskar et al, Journal of Applied Physics, 2013
Need high base contact doping >1020/cm3 for good contacts high Auger recombination very low b.
Need moderate contact penetration Pd or Pt contacts react with 3++ nm of base penetrate surface contaminants too deep for thin base
Solution: base regrowth: thin, moderately-doped intrinsic base thick, heavily-doped extrinsic base
Rode et al., IEEE TED, Aug. 2015

## Slide 15: Regrown-Base InP HBTs: Images
Cross-section
Dry-etched TiW emitter contact
100nm emitter after base regrowth

## Slide 16: Regrown-Base InP HBTs: DC Data
0.1× 5mm emitter
0.2× 5mm emitter
0.2× 5mm emitter
0.4× 5mm emitter
Good b, low Rex, high-current operation

## Slide 17: Regrown-Base InP HBTs: Base Resistance
0.9W-mm2 resistivity for GaAs/metal contact 294W sheet resistivity for regrown base 
1.0W-mm2 resistivity for InGaAs/GaAs contact 4300W/ sheet resistivity for intrinsic base ✘
Base contact resistivity sufficient for 64nm/2THz node. Improvements: anneal after regrowth, grade interface
Regrowth: base contacts suitable for 64nm/2THz & 32nm/3THz nodes

## Slide 18: FETs (HEMTs): key for low noise
2:1 to 4:1 increase in ft : improved noise less required transmit power smaller PAs, less DC power
or higher-frequency systems
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process

## Slide 19
Towards faster HEMTs: MOS-HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, place N+ layer on InAs channel Target ~10nm node ~0.3nm EOT, 3nm thick channel 1.2 to 1.5 THz ft.
1st demonstration: Fraunhofer IAF

## Slide 20: Towards Faster HEMTs: MOS-HEMTs
Double regrowth modulation-doped access regions N+ contacts
High-K gate dielectric: 3 nm ZrO2.
Highly scaled 5nm InAs channel, 10-30nm gate lengths
Jun Wu, UCSB, IEEE EDL, 2018

## Slide 21: 100-340GHz Wireless Systems:
100-340 GHz wireless systems massive capacities via spatial multiplexing compact, high-resolution imaging systems short range: few 100 meters
Many challenges spatial multiplexing: computational complexity, dynamic range packaging: fitting signal channels in very small areas
IC Technology All-silicon for short ranges below 250 GHz. III-V LNAs and PAs for longer-range links. Just like cell phones today III-V frequency extenders for 340GHz and beyond
Device opportunity: better PAs, LNAs for 140, 220, 340GHz.

## Slide 22
In case of questions

## Slide 23: Towards faster HEMTs: next step
No N- material between channel and contacts reduced source/drain access resistance
Sacrificial layer reduces parasitic gate-channel overlap less gate-source capacitance
2.5nm ZrO2 dielectric, 3nm InAs channel higher gm , lower gds

## Slide 24: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1
Gate dielectric can't be much further scaled.
gm/Wg hard to increase→ Cend / gm prevents ft scaling.
Shorter Lg→ poor electrostatics→ reduced gm /Gds

## Slide 25
Towards faster HEMTs: MOS-HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, place N+ layer on InAs channel Target ~10nm node ~0.3nm EOT, 3nm thick channel 1.2 to 1.5 THz ft.
1st demonstration: Fraunhofer IAF