## Slide 1: Self-Aligned InGaAs Channel MOS-HEMTs for High Frequency Applications
Logan Whitaker
UCSB Department of Electrical and Computer Engineering
June 28th, 2023
Advisor: Prof. Mark Rodwell
Funding: SRC & DARPA

## Slide 2: Motivation – Beyond 5G
Industry currently introducing 5G (20-80 GHz)
Beyond 5G requires 100-300 GHz communication systems
  More bandwidth
  Higher data rates
Requires transistors operate “easily” at these frequencies:
Reprinted with permission of Mark Rodwell

## Slide 3: FETs – Reduce Noise Figure
Reprinted with permission of Mark Rodwell
Increase in ft :
Current frequency
  Improved noise
higher-frequency systems
  Same noise

## Slide 4: Why not HEMT?
Increasing ft by reducing CGS,i
Reduced CGS /CGD hurts gds
Scaling laws say thin gate insulator
InAlAs – InGaAs CBO ~ 0.5 eV
High gate leakage

## Slide 5: MOS-HEMTs
Add gate dielectric
Improve CGS /CGD
Improve gds
Institution | Lg (nm) | gm,e (mS/µm) | gds,e (mS/µm) | CGS (fF/um) | CGD (fF/um) | fτ (GHz) | fmax (GHz)
Markman et al. | 40 | 2.9 | 0.15 | 0.8 | 0.2 | 403 | 594
Reprinted with permission of Brian Markman

## Slide 6: MOS-HEMTs
Ft, fmax limited by CGS, CGD
Fringe capacitance from gate-link overlap
  T-gate filling
  Gate alignment
Extra capacitance from thick link
Institution | Lg (nm) | gm,e (mS/µm) | gds,e (mS/µm) | CGS (fF/um) | CGD (fF/um) | fτ (GHz) | fmax (GHz)
Markman et al. | 40 | 2.9 | 0.15 | 0.8 | 0.2 | 403 | 594
Reprinted with permission of Brian Markman

## Slide 7: MOS-HEMTs
Ft, fmax limited by CGS, CGD
Fringe capacitance from gate-link overlap
  T-gate filling
  Gate alignment
Extra capacitance from thick link
Need:
  Self aligned process
  Structure that’s easier to fill
  Thinner Link
Institution | Lg (nm) | gm,e (mS/µm) | gds,e (mS/µm) | CGS (fF/um) | CGD (fF/um) | fτ (GHz) | fmax (GHz)
Markman et al. | 40 | 2.9 | 0.15 | 0.8 | 0.2 | 403 | 594
Reprinted with permission of Brian Markman

## Slide 8: MOS-HEMTs 2.0
Self aligned
  Removes gate-link overlap
  Reduces CGS,f
V-Gate
  Easier to fill with metal
  Better Lg scaling
Thin link
  More є0
  Less єS
  Reduces CGS,f

## Slide 9: What is my variable?
Link thickness
  3 nm minimum (source starvation)
  20 nm maximum (maximized mobility)

## Slide 10: Rs breakdown

## Slide 11: Capacitance
Create model in HFSS
Find capacitance of the model
Vary Lg
Find y intercepts
Divide by 2 to find CGS
Repeat with variations on the model

## Slide 12: Cgs end vs Link Thickness
Vary the thickness of the link
  Assume channel is perfectly conducting (pessimistic)
  Assume topside link doping is a perfect insulator (optimistic)
  Results in a STRONG linear relationship between link thickness and end capacitance
Thinner (low mobility) links could be better?

## Slide 13: So What?
Ideal: Transit Time

## Slide 14: So What?
Ideal: Transit Time

## Slide 15: So What?
Ideal: Transit Time

## Slide 16: Process Flow
Epi + Regrowth 1
Regrowth 2
c) Digital etch, high-k, and gate metal
d) high-k etch, sidewall, sacrificial etch, mesa isolation, and contacts

## Slide 17: DC results – Lg = 22 nm

## Slide 18: RF results vs Gate Length

## Slide 19: Mixed Results – Lg = 20 nm

## Slide 20: Mixed Results – Lg = 36 nm

## Slide 21: TEM – Lg = 18 nm

## Slide 22: Acknowledgements
Funding Support: SRC, DARPA (ComSenTer, JUMP)
Nanofab: Cleanroom staff
MOCVD Growth: Klamkin Group and MOCVD staff
HFM Testing Lab: Matt Guidry and Christopher Clymore
Lund University: Erik Lind and Lars-Erik Wernersson
Special Thanks: Brian Markman

## Slide 23: Self-Aligned InGaAs Channel MOS-HEMTs for High Frequency Applications
Logan Whitaker
UCSB Department of Electrical and Computer Engineering
June 28th, 2023
Advisor: Prof. Mark Rodwell
Funding: SRC & DARPA

## Slide 24: References
[1] M. Egard et al., IEEE-EDL, vol. 33, no. 3, p. 369, (2012).
[2] B. Markman et al., DRC, (2021).
[3] D. F. William et al., IEEE-TSAT, vol. 3, no. 4, p. 433, (201).
[4] S. Kee et al., IEEE-EDL, vol. 35, no. 6, p. 621, (2014).
[5] S. Lee et al., IEEE Microw. Guid. Wave Lett., 1997.
[6] W. S. Park & H. B. Jo et al., IEEE-IEDM, (2022).