## Slide 2
Si
SiO2
SiN
InP
SCH
QW
n-InP contact
Gold
Aluminum
Other metal
PR

## Slide 3: WG etch
1um
0.7um
Delay
SOA/SA
Isolation between SOA/SA

## Slide 4: VC etch

## Slide 5: SiO2/SiN protect
0.7 um
1 um

## Slide 6: SiO2/SiN protect etch

## Slide 7: Bond

## Slide 8: InP substrate removal
~2.5 um
~1.7 um

## Slide 9: Gap fill

## Slide 10: Open III-V
1 um

## Slide 11: P-TLM litho

## Slide 12: Thin P metal deposition
137 nm

## Slide 13: Liftoff
P-TLM

## Slide 14: Mesa hard mask deposition

## Slide 15: Mesa hard mask definition
1 um
1 um
0.3 um

## Slide 16: Mesa hard mask etch

## Slide 17: Metal etch

## Slide 18: PR strip and mesa etch

## Slide 19: QW etch
Aspect ratio exaggerated

## Slide 20: Remove mesa hard mask

## Slide 21: P and N metal (one mask)

## Slide 22
Anneal and TLM measurements

## Slide 23: Thin p isolation etch

## Slide 24: Implant

## Slide 25: Implant HM and N-layer etch

## Slide 26: Via
SU8

## Slide 27: Probe pad
SU8

## Slide 28: Remove III-V under gap*
SU8