## Slide 1: Optical Isolator Update
Jason
5/4/2010

## Slide 2: Outline
Device fabrication and issues
Magneto-optical material characterization
Concept of uni-directional ring laser

## Slide 3: NRPS in microdisk resonator
BOX
MO
B
Disks with smaller radius push the optical mode outward and thus increase confinement factor of MO.
Trade-off between the bend loss and confinement factor of MO
One step litho and no need to etch MO
Oxide hardmask is used to prevent mode overlap with the top MO, which increases optical loss
Si

## Slide 4: Fabrication process- disk isolator
BOX
Si
BOX
Si
Ebeam lithography
Waveguide and disk etch
Ce:YIG MO sputtering
thermal annealing for crystallization
waveguide
disk

## Slide 5: Mask layout
Disk diameters: 3um, 4um, 5um, and 10um
Thickness: 700 nm
Waveguide width: 350 nm
Disk-waveguide gap: 100nm ~ 250 nm, step: 25nm
D=3um
D=4um
D=5um
Gap= 100nm
Gap= 250nm

## Slide 6: Issues
Waveguides are fragile for polishing
  Rectangular waveguides instead of rib waveguides
  No SU8 or polyimide as a protection layer
  Solutions:
    Deposit oxide as a protection layer (CeYIG for real devices)
    Leave ~100nm Si not etched
    Taper out the waveguide for the fiber coupling region

## Slide 7: CeYIG:500C
500C
Ar/O2=50/0.25sccm
Power: 300W
Pressure: 6mT
Time: 2hr
chamber pressure: 1.6e-6 -> 7.8e-7
RTA annealing:
800C, 850C, and 900C 10 min
Ramp: 5 min
(400)
(420)
Si sub.

## Slide 8: CeYIG:520C
520C
Ar/O2=50/0.25sccm
Power: 300W
Pressure: 6mT
Time: 2hr
chamber pressure: 1.4e-6 -> 6.3e-7
RTA annealing:
800C, 850C, and 900C 10 min
Ramp: 5 min
(400)
(420)

## Slide 9: CeYIG: 550C
550C
Ar/O2=50/0.25sccm
Power: 300W
Pressure: 6mT
Time: 2hr
chamber pressure:
RTA annealing:
800C, 850C, and 900C 10 min
Ramp: 5 min
Si substrate

## Slide 10: CeYIG: 600C
600C
Ar/O2=50/0.25sccm
Power: 300W
Pressure: 6mT
Time: 2hr
chamber pressure: 5e-6 -> 2e-6
RTA annealing:
800C, 850C, and 900C 10 min
Ramp: 5 min
(400)
(420)
(620)
(444)
Si sub.

## Slide 11: Higher annealing temperature
When the annealing temperature is higher than 950C, X-ray diffraction shows stronger peaks. But, speckle-like patterns pop out on the surface of the film.
 May be due to the outgassing of the film

## Slide 12: Chamber condition
1st time target installed
2nd time target installed
Same recipe, but the target which was taken out of the chamber and reinstalled gives different results

## Slide 13: Chamber pressure
7.5e-7 Torr
1.1e-5 Torr
For high temperature sputtering process, the material on the sample holder may evaporate and affect the film quality

## Slide 14: Annealing time
10 min of annealing time is sufficient for crystallization

## Slide 15: Conclusions
Reproducibility of film quality
  Preheat the sample holder to evaporate contaminations before loading the sample
  Run a dummy run after changing the target
    Clean the surface of the target
Annealing temperature higher than 900C creates surface speckle
  may be due to outgasing of the film
Best result so far
  500C of sputtering temperature with 900C 10 min post-annealing

## Slide 16: Uni-directional ring laser
SOI wafer
Non-reciprocal ring resonator
III-V gain medium
BOX
MO
III-V gain medium
Cross-sectional view
Nonreciprocal ring resonator with different gain/loss in different directions
Bonded III-V material provides the required gain.
Lasing only happens in either clockwise or counterclockwise direction
x
y
III-V gain medium

## Slide 17: Uni-directional ring laser
BOX
MO
x
y
P contact
N contact
Based on Di’s ring laser structure
More optical confinement for small ring laser
Cavity is defined by III-V region