## Slide 1: Silicon Photonics Meeting - Ring Isolator with Bonded YIG
7/12/2010
Jason Tien

## Slide 2: Nonreciprocal propagation constant in ring resonators
B
YIG
Si
BOX
Si
I
YIG
Metal wire
B
Top view
Cross-section
y
x
Magnetic field with radial direction is required!
y0
y1

## Slide 3: How to apply radial magnetic field?
Si
BOX
CeYIG
Si
Permanent magnet
1.6 mm
0.8 mm
CeYIG
Ring resonator
The diameter of the ring matches that of the cylinder magnet
- magnet: 1.6 mm
- ring: 1.8mm
Material of ring can be silicon (or SiN?)
Better quality of Ce:YIG can be bonded to ring resonator

## Slide 4: Ring resonators with horizontal YIG film
Si
BOX
Si
GGG
a-Si
a-Si
GGG
Approach 1)
Wafer bond YIG-film on to Si ring resonators
Approach 2)
Fabricate a-Si ring resonators on the GGG substrate with YIG
Low-loss a-Si waveguide is required.
YIG-Si bonding needs to be developed.

## Slide 5: Ce:YIG bonded to SOI
CeYIG
Si
BOX
GGG
A’
A
A’
A
0.5um CeYIG on GGG substrate
Bond CeYIG to SOI Si waveguide
Si waveguide: 0.6um * 0.2um
Resonance wavelength split: 0.37nm

## Slide 6: Faraday Effect
Resonance wavelength shift 0.37nm as Ce:YIG is 0.5 um thick
10X larger than that in Si disk

## Slide 7: Coupling calculation by FIMMPROP
0.5um CeYIG on GGG substrate
Bond CeYIG to SOI Si waveguide
Si waveguide: 0.6um * 0.2um
Radius : 1 mm

## Slide 8: Device layout
4mm
4mm
5mm
CeYIG on GGG
Magnet
1.6mm
1.8mm

## Slide 9: Conclusions
Advantages:
  > 10X wavelength split than that on Si disks
  Better CeYIG quality because of lattice match, similar thermal expansion coefficient, and same crystal structure
Challenge:
  Bonding between CeYIG and silicon waveguides
Potential issue:
  A large ring is not a resonator anymore if the waveguide loss is too high (loss > 10 dB/cm for 1-mm-radius ring)