## Slide 1: WGUTC process flow

## Slide 2: Starting wafer
Si
BOX
Handle wafer
Device layer

## Slide 3: Implant alignment etch
SiO2 mask from Si thinning by wet oxidation - ~1um thick
Mask used for standard Cl/BCl3 ICP etch – alignment marks only in corners of die
Not removed after etch
Si
BOX
Alignment marks
Most areas

## Slide 4: N++ implant
SiO2 mask from Si thinning by wet oxidation - ~1um thick
Si
BOX
Alignment marks
Device areas
PD layout – top view
N++

## Slide 5: N implant
New PECVD SiO2 mask
Followed by:
Strip SiO2, clean, dep 50nm SiO2, 5’ RTA at 900C in graphite susceptor
Then Ge growth
Si
BOX
Alignment marks
Device areas
PD layout – top view
N++
N

## Slide 6: Material after growth
Si
BOX
Ge
Device area
Elsewhere
Doped Si
PD layout – top view
N++
N

## Slide 7: Waveguide etch
WG etch (SF6/O2 in ICP1 with Cr/SiO2 hardmask)
Etch 300nm into Si
Final WG dimensions achieved using this process have already been verified
Si
BOX
Device area
WG
PD layout – top view
Optical input

## Slide 8: Deep etch
Deep etch (self-aligned to previous step - similar to what Hui-Wen used to do)
Without this step, minimum bend radius becomes huge, MMI design becomes difficult
Si
BOX
Device area
WG
PD layout – top view
No change in PD area

## Slide 9: Self-aligned implant
Cross-section: device during implant
Implant: N-type for contact layer
Anneal: strip PR, then waveguide hardmask, then clean again and deposit SiO2 before 600C 5 min anneal
Si
BOX
Device area
WG
PR

## Slide 10: P-metal
Very thin (150nm), mostly protects device during subsequent steps
Si
BOX
Device area
WG

## Slide 11: Mesa wet etch
2:2:15 H2O2:HCL:DI
Mask: SiO2
  Would prefer SiN so PR is easier to remove
  PR removal actually important, it tends to build up around the waveguide edges and cause issues during this step (Ge strings that don’t get etched)
Si
BOX
Device area
WG
PD layout – top view

## Slide 12: Passivation dep/via etch
500nm to protect waveguides and passivate PD sidewalls, via etch to open n-contacts and PD mesa
Si
BOX
Device area
WG
PD layout – top view
3 rectangles: 2n, 1p

## Slide 13: N-metal
Not too thick (~500nm), want to be below p-metal
Forms ground plane for microstrip lines
Mesa-Nmet spacing 1um
Si
BOX
Device area
WG
PD layout – top view
Opening to make liftoff easier

## Slide 14: Heater metal dep
Only shown on this slide
Si
BOX
Device area
WG
PD layout – top view
No change in PD area

## Slide 15: Cap deposition
MIS cap
Blanket dep of 20nm SiN in ALD
  Should be pinhole-free, but may not grow on metal-covered areas
Then do contact/heater anneal
Then liftoff to form cap upper contacts
Si
BOX
Cap area
P-metal
N-metal
Large* via
SiN
Cap metal

## Slide 16: BCB/planarization
Spin on 4um, immediately cover with thin SiN
Cap dielectric covers everything – protects BCB surface from damage (for better adhesion later) and is patterned in the same steps
Si
BOX
Device area
WG

## Slide 17: BCB vias
Pattern w/PR – vias are quite large and have sloped sidewalls
  Makes sidewall coverage easier
Si
BOX
Device area
WG

## Slide 18: Via 2
200 nm of SiN. Via pattern pulled in 200nm from edge of PD
Si
BOX
Device area
WG

## Slide 19: Probe metal
1um
Probe-Nmet overlap 2um in some places, 0um in others
Si
BOX
WG
PD layout – top view
Device area

## Slide 20: Total mask layers (lithographies)
Implant alignment
N++ implant
N implant
- Ge growth -
Trench
Deep Si etch
Implant
P-metal
Mesa
Via etch (to n-contacts and p-contact metal)
N-metal
Heater metal
Capacitor (incl. top metal)
BCB vias
Via 2
Probe metal