## Slide 1: 2x2 E-PHI MMI Characterization
Geza Kurczveil

## Slide 2: Chip layout
Straight facet (1.0 μm wide WG @ input)
no AR coating
Top cladding: air
Passive WG
2x2 MMI (long ~300 μm)
11 devices, vary L in 5 μm steps
2x2 MMI (short ~100 μm)
11 devices, vary L in 2.5 μm steps
…
…

## Slide 3: Setup
ASE
DUT
BPF
4 nm centered on 1550 nm
PM

## Slide 4: Long 2x2 MMIs
Device #4 has lowest insertion loss
  Too few reference wageguides to be certain on absolute insertion loss
1
2
3
4

## Slide 5: Short 2x2 MMIs
Device #3 or 4 has lowest insertion loss
1
2
3
4

## Slide 6
Martin T. Hill et al., “Optimizing Imbalance and Loss in 2x2 3-dB Multimode Interference Couplers via Access Waveguide Width,” JLT 2003
Wa/W = 0.3 theoretically gives lowest imbalance and lowest insertion loss for 2x2 coupler.
  Long design: Wa/W = 4/15 = 0.266
  Short design: Wa/W = 2.5/9 = 0.277
Q: Why not always use Wa/W = 0.3?
A: For 2x2 coupler, access waveguides centered on W/3 and 2W/3. If Wa/W = 0.3, access WG separation is 0.033*W. Must be large enough to be resolved, and for light to not couple between WGs. This increases footprint.