## Slide 1: SiP Meeting – Isolator
Jason
2/16/2010

## Slide 2: Process flow –post LioniX
`
`
`
`
`
`
`
Si3N4/SiO2 waveguides
Pattern Cr as hardmask
Deep etch SiO2 and strip Cr hardmask
Sputter Ce:YIG or BIG magnetic material

## Slide 3: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 5um
Ce:YIG
Film thickness: 50nm
SiO2 cladding
Si3N4 core
Magnetic film
5um

## Slide 4
Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 5um
Ce:YIG
Film thickness: 100nm

## Slide 5: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 5um
Ce:YIG
Film thickness: 150nm

## Slide 6: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 5um
Ce:YIG
Film thickness: 200nm

## Slide 7: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 5um
Ce:YIG
Film thickness: 250nm

## Slide 8: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 6um
Ce:YIG
Film thickness: 50nm
SiO2 cladding
Si3N4 core
Magnetic film
6um

## Slide 9: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 6um
Ce:YIG
Film thickness: 100nm

## Slide 10: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 6um
Ce:YIG
Film thickness: 150nm

## Slide 11: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 6um
Ce:YIG
Film thickness: 200nm

## Slide 12: Optical mode profile
SiN core: 80nm
SiO2 cladding: 4um
Etch depth : 6um
Ce:YIG
Film thickness: 250nm

## Slide 13: Optical modes in Si3N4 waveguides
Thicker magnetic film will suck optical field from Si3N4 (n=2) core to Ce:YIG (n=2.22) layer.
Shallower etch causes leak mode to the horizontal magnetic film, which doesn’t contribute to Faraday effect but extra optical loss!
6 um etch
5 um etch
Magnetic film thickness : 150 nm
Magnetic film
Si3N4 core

## Slide 14: Design plot for magnetic film thickness
MO material : Ce:YIG
  refractive index =2.22
  Loss: 20 cm-1

## Slide 15: Design of Si waveguide
W
H=0.7um
Slab height
Ce:YIG
MO material : Ce:YIG
  refractive index =2.22
  Loss: 20 cm-1
  thickness: 200nm

## Slide 16: Comparison between confinement factor and wavelength splitting
W=0.3um
W=0.4um
W=0.5um
W=0.6um
FIMMWAVE calculation
Analytic calculation
(rectangular waveguide like)

## Slide 17: Process plan
Ce:YIG target will arrive this week.
Material sputtering test
  X-ray diffraction
Deep oxide etch
  Photomask design
  Etch test using Cr as hardmask