## Slide 1: Heterogeneous Integration for Reduced Phase Noise and Improved Reliability of Semiconductor Lasers
Sudharsanan Srinivasan
Ph.D. Defense
Electrical and Computer Engineering Department
University of California, Santa Barbara

## Slide 2: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 3: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 4
Linewidth  160kHz
Tunable Lasers
Mode-locked Lasers
Linewidth  <100kHz
14dB phase noise reduction
8dB phase noise reduction
Chart: Wavelength (nm)
| 1235 | 1237 | 1241 | 1243 | 1245 | 1247 | 1249 | 1251 | 1253 | 1255 | 1258 | 1261 | 1262 | 1264 | 1266 | 1268 | 1270 | 1272 | 1274 | 1275 | 1277 | 1278 | 1281 | 1283 | 1285 | 1288 | 1290 | 1292
 | 52 | 74 | 66 | 50 | 92 | 62 | 55 | 63 | 55 | 73 | 91 | 92 | 75 | 72 | 58 | 61 | 63.3 | 85 | 58 | 96 | 56 | 68 | 63 | 82 | 55 | 94 | 63 | 57

## Slide 5
Evanescent coupling for gain/loss
Transition to silicon guides
MTTF >40000 hrs
Processed die of 300 DFB lasers

## Slide 6: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 7: Introduction
High Speed Communications
Sensing
Metrology
High speed & high ENOB ADC
Spectral efficiency in telecom
Wind LIDAR
Oil & Gas Sensing
Pipeline Monitoring
Spectroscopy
Frequency standards
Low phase noise
microwave and laser sources
Notes: Thermal, mechanical and acoustic sensors.

## Slide 8: Introduction
Low phase noise microwave and laser sources
Requirements
Low cost
Small Size
Mechanically stable
Low power consumption
Enabled by INTEGRATION!
Notes: Thermal, mechanical and acoustic sensors.

## Slide 9: Introduction
Silicon Photonics
Ultra-small size
Low cost
Convergence with electronic devices
InP Photonics
Lasers, optical amplifiers
Wavelength conversion
Ultra-fast modulators and switches
Hybrid Silicon Platform
DFB/EAM/PD Array
Optical preamplifier PD array
Optical buffer
Hybrid Silicon Photonic Integrated Circuit Technology
M. J. R. Heck et al. JOURNAL OF SELECTED TOPICS IN QUATUM ELECTRONICS, vol. 19(4), 2013.

## Slide 10: Introduction
Heterogeneous Integration of III-V material to Silicon
Cross-section of
the hybrid laser

## Slide 11: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 12: Phase Noise of an Oscillator
Frequency
Ideal Oscillator
Frequency
Real world Oscillator
Time
Time
Total Oscillator noise is the sum of amplitude and phase noise.
Close to the true carrier frequency phase noise dominates.
ASE is dominant source of noise in semiconductor lasers.
Semiconductor Laser Linewidth

## Slide 13: Noise Dilution - Analogy
W1
A
B
W2
A
B
For a fixed W1

## Slide 14: Current Injection Semiconductor Laser
Photon density Carrier density
ΔNp ΔN
Carrier Density (N)
Photon Density of Lasing Mode (Np)
Carrier leakage
Non-radiative recombination
Input current
Spontaneous emission into other wavelengths
Absorption
Spontaneous emission into lasing mode
Stimulated emission into lasing mode
Laser output

## Slide 15: Negative Optical Feedback
Mirror reflectivity
Frequency
Frequency Mirror reflectivity/Feedback strength Photon density Carrier density ref. index  Frequency
Δν ΔR ΔNp ΔN Δn Δν
ΔνFR
Δνo
β
ΔνFB

## Slide 16: ASE Noise Dilution
W1
A
B
W2
A
B
Laser confinement factor
L
W
N Wells
t
Lx
Ly
Lz
Carrier confined volume
Optical mode volume

## Slide 17: Long Laser Cavity
Fundamental cavity
Harmonic cavity
  Linewidth reduction is inversely proportional to the square of the cavity length.
<αi>  internal loss
Short cavity
Long cavity
Cavity loss

## Slide 18: Harmonic Cavity Mode-Locking
50mm absorber
Directional coupler
Multi-Mode
Interference
Coupler – 50:50
4cm cavity length
1.5mm
7mm
90:10

## Slide 19: Characterization
RF Peak Power
SMSR
SOA current: 220mA
SA voltage: -0.5V
Optical
spectrum
RBW-3MHz
Electrical
spectrum
RBW-20MHz

## Slide 20: Optical Linewidth
Chart: Mode Number
| -2 | -1 | 0 | 1 | 2
Fundamental cavity | 14.3333 | 10.5 | 10.1 | 13.4667 | 16.8
Harmonic cavity | 1.1333 | 1.1158 | 1.1225 | 1.475
10x
Fiber Laser
DUT
OSA
ESA
Fundamental cavity
Harmonic cavity
Linewidth improvement 10MHz  1MHz (10x)

## Slide 21: Microwave Linewidth
Linewidth improvement – 1.5MHz  52kHz (30x)
2G cavity with filter -220mA, -0.5V
20G cavity –
188mA, 0 V
Fundamental cavity
Harmonic cavity
SOA lengths 900mm and 1.4mm respectively.
Absorber length 50mm in both cases

## Slide 22: Microwave Phase Noise
Passive locking
5x
14dB
Fundamental cavity
Harmonic cavity
Integrated jitter (100kHz100MHz)
reduced from 4.3ps to 1.3ps

## Slide 23: Coupled Cavity Mode-Locking
Advantages
Lower threshold
Better slope efficiency
Laser acts as the filter
Le
1/2α
Δν
0

## Slide 24: Transverse Confinement
Laser confinement factor
Reduce number of MQW to reduce transverse confinement
Five QW
Three QW

## Slide 25: Characterization
Three QW
Five QW
Three QW
Five QW
7.7ps pulsewidth
4ps pulsewidth

## Slide 26: Characterization
Three QW
Five QW
8dB reduction in phase noise

## Slide 27: Longitudinal Confinement
Laser confinement factor
Amplitude control
Phase
control

## Slide 28: Feedback Cavity
Three QW
Five QW
Optimum bias

## Slide 29: Longitudinal Confinement
RF linewidth (kHz) measured @ | Without feedback | With feedback
 | Three QW device | 
3dB | 44 | 29
10dB | 103 | 60
20dB | 292 | 159
 | Five QW device | 
3dB | 200 | 136
10dB | 607 | 409
20dB | 2010 | 1356
Three QW
Five QW
Three QW
Integrated jitter (100kHz100MHz)
reduced from 2.7ps to 1.2ps
6dB

## Slide 30: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 31: Coupled Cavity Tunable Laser
Filter response
Front mirror – 10%
Rear mirror – 60%
Laser SOA Length – 1.2mm
Feedback SOA Length - 560μm

## Slide 32: Coupled Cavity Tunable Laser
Chart: Wavelength (nm)
| 1235 | 1237 | 1241 | 1243 | 1245 | 1247 | 1249 | 1251 | 1253 | 1255 | 1258 | 1261 | 1262 | 1264 | 1266 | 1268 | 1270 | 1272 | 1274 | 1275 | 1277 | 1278 | 1281 | 1283 | 1285 | 1288 | 1290 | 1292
 | 52 | 74 | 66 | 50 | 92 | 62 | 55 | 63 | 55 | 73 | 91 | 92 | 75 | 72 | 58 | 61 | 63.3 | 85 | 58 | 96 | 56 | 68 | 63 | 82 | 55 | 94 | 63 | 57
54+ nm tuning
>45 dB SMSR
~30 mA threshold current
10+ mW output power
Without coupled cavity

## Slide 33: Relative Intensity Noise
RIN <-150dBc/Hz from 10MHz18GHz except from 1GHz3GHz

## Slide 34: Modulation Response
Photon-photon resonance

## Slide 35: Coupled Ring Resonator Mirrors
SOA
Thermal tuners

## Slide 36: Cavity Length Enhancement
Cavity appears longer as we tune into resonance

## Slide 37: Characterization
29 nm tuning
>40 dB SMSR
160kHz linewidth
50-60× lower than natural linewidth
We only predict
~(1+3)2=16×

## Slide 38: Negative Optical Feedback
Linewidth is narrowest before mode-hop
ΔνFR
Δνo
β
ΔνFB
Free-running
Output
Noise dilution
Negative feedback

## Slide 39: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 40: Bonding Defect Propagation
D. Liang, S. Srinivasan, J. Peters, A. Fang and J. Bowers, ECS Trans. volume 33,issue 4, 421-426 (2010)
Test integrity of MQW with aging

## Slide 41: Reliability Experiment
Strategy for pinning defects  strained super-lattice layers
D. Liang, S. Srinivasan, J. Peters, A. Fang and J. Bowers, ECS Trans. volume 33,issue 4, 421-426 (2010)

## Slide 42: Laser Characterization
300 DFB Lasers + 300 monitor photodiodes
×
10 dies with different interface super-lattice structures
Wafer level tested L-I curves

## Slide 43: Laser Packaging
Chart: Current (mA)
15°C to 65°C in steps of 5°C

## Slide 44: Results
Green  No super-lattice, Red  Strained super-lattice, Blue  Unstrained super-lattice

## Slide 45: Results
Time to reach 50% degradation in threshold current at 70°C is ~40,000hrs

## Slide 46: Cross-sectional TEM
Defects < 107 cm-2
No visible signs of MQW degradation

## Slide 47: On-chip Photodiode Dark Current
Before aging
After aging

## Slide 48: Outline
Preview
Introduction
Lowering phase noise of:
  Mode locked lasers
  Tunable lasers
Reliability of hybrid silicon DFB lasers
Conclusion and Future Work

## Slide 49: Conclusions
14dB microwave phase noise reduction at 20GHz using 10× mode-locked-laser cavity length and an intra-cavity filter.
8dB reduction in microwave phase at 17.36GHz with reduced number of quantum wells
<100kHz optical linewidth on a widely tunable o-band laser using coupled cavity tunable laser.
160kHz optical linewidth on a coupled ring resonator mirror based tunable laser using negative optical feedback.
No degradation seen in threshold current of DFB lasers after aging for 5000hrs at 70°C and 100mA.
MTTFestimate for hybrid silicon DFB lasers >40000hrs.

## Slide 50: Future Work
Coupled cavity laser limitations from waveguide loss and filter bandwidth. Low loss high aspect ratio silicon nitride waveguides can be used for longer delays and sharp filters. However, “Do not design for more Q than you can chew.”
Exploit on-chip negative feedback from ring resonator structures both within the cavity and external to the main laser cavity.
Remove optical amplifier in the feedback cavity to remove spontaneous emission noise. Passive solutions are quieter.

## Slide 51: Acknowledgement
Adviser: John Bowers (Doc) PILL  (P)assion to cure (I)gnorance (L)ethargy (L)assitude
Committee: Luke Theogarajan, Larry Coldren, Rod Alferness.
Faculty: Nadir Dagli, Dan Blumenthal, Dan Cohen, Milan, Petroff, Palmstrom, Van-de-Walle, Mark Rodwell.
Staff: Ceanna, Alyssa, Christine, Shannon, Val, Jon Magnani, Paul Gritt and many other lovely people in the ECE and Grad. Division who work magic with paperwork.
Aurrion friends: Alex, Byungchae, Jeff Wise, John Hutchinson, Eric Hall, Greg Fish, Erik Norberg, Alfredo.
Bowers Alumni: Anand, Andy, Sid, Di Liang, Geza, Molly, Ben, Jared B, Martijn, Daoxin, Yongbo, Hui-Wen, Tony (Chieh-Ting), Jon Doylend, Jock, Nick J.
Bowers group: Michael Davenport, Daryl, Chong, Jared H, Tin K, Eric, Alex S, Emmett, Minh, Lin, Tony H, Yichen, Alan, Justin.
Luke’s group: Aaron, Avantika.
Dan Blumenthal’s group: Kim, John Garcia, Erica, Wenzao, Henrik, Demis, Michael Belt, Renan.
Dagli’s group: Selim.
Larry Coldren’s group: John Parker, Rob Guzzon, Abi, Chinhan.
Engineers: Jon Peters, Andy.
Cleanroom Staff: Jack, Tom, Tony, Don, Mike, Adam, Aidan, Bill.
Interns: Alois, Bassem, Ardit, Sylvia, Rui.

## Slide 52: Acknowledgments
Collaborator at U Surrey: Prof. Sweeney, Graham Read, Nadir Hossain
Screening study group: Matt L, Joe Nedy, Jeong, Han-Wei.
Room-mates: Scott Dirkse, John Smith Mac-Donald, Shawn Owens, Dinesh, Aseem.
Volleyball crew: Keith, Hannah, Saiph, D Morales, Jacob Adams.
Indian friends through Raagmala and IASB: Karthick Santhanam, Karthikeyan, Tejaswi, Madhukar, Vineeth, Karthik Malasani, Kumar Bhargav, Sandeep & Malavika, Ramya, Dilip.
Last but not the least  My Parents.
THANK YOU ALL!

## Slide 53
Phase Noise is Important!
Original Image
Phase Switched
Amplitude Switched

## Slide 54: Back-up

## Slide 55: Hybrid Locking
Hybrid locking with RF signal generator
SOA current: 206mA
SA voltage: -1.4V
OSA
ESA

## Slide 56: Characterization
RF Peak Power
SMSR
SOA current: 220mA
SA voltage: -0.5V
Optical
spectrum
RBW-3MHz
Electrical
spectrum
RBW-20MHz

## Slide 57: Coupled Opto-Electronic Oscillator
Electro-Optic Feedback
~20m feedback fiber delay
40dB gain

## Slide 58: Coupled-Cavity Tunable Laser

## Slide 59: External Cavity Multi-Moding
Complex Plane
Decreasing loss in ext. cavity
For higher SOA bias currents the coupled cavity starts to multi-mode

## Slide 60: Cavity Mode Locations

## Slide 61: Heater Cross-Talk