## Slide 1: Ce:YIG characterization
Jason Tien
8/24/2010

## Slide 2: Sputtered Ce:YIG
Si
Box
Sputter Ce:YIG for 2 hours in AJA#3 followed by 900C RTA annealing
Cleave and dip in BHF before SEM
Ce:YIG

## Slide 3: Sputtered Ce:YIG
Vertical-to-lateral thickness: 2:1
Deposition rate: 90 nm/hr

## Slide 4: XRD of Sputtered Ce:YIG on Si
(400)
(420)
Film was sputtered on a bare silicon chip
10min
5 min

## Slide 5: XRD of Sputtered Ce:YIG on Si (Cont.)
1min
1 min

## Slide 6: XRD of Sputtered Ce:YIG on GGG
Room temperature sputtering + 900C annealing gives the strongest XRD

## Slide 7: E-beam Litho
Resist
Developed area
Stitch error?
600um
ZEP positive E-beam resist
Coat with Au to avoid charging
Smaller sample holder without atuo-height correction
Smaller sample holder with atuo-height correction
No observable stitch error under 150X microscope
Two possible reasons:
Wrong e-beam focus plan
Stage over movement

## Slide 8: Plan for the next
Measure the waveguide loss and estimate the Q for large-radius ring resonators
Fabricate large-radius ring resonators
Add Im-balance MZI structure to distinguish the material properties

## Slide 9: Imbalanced MZI Test Structure
L1
L2
ΔL=290um
Δn=7e-4  Δλ~0.5nm
External magnetic field
As a test pattern to measure Faraday coefficient
Easy to apply external magnetic field
Waveguide loss doesn’t matter