## Slide 1: BCB Planarization Process Using EPHI SOA Masks
Jared Hulme
6/2/12

## Slide 2: Process for BCB SOA Mask Run
Si Substrate
SiO2
Si Substrate
SiO2
Resist
Si Substrate
SiO2
Si Substrate
1. Silicon wafer
2. Deposit Hardmask 400nm SiO2
3. Spin AZ4210
4. Hardmask Litho
Si Substrate
Si Substrate
8. Remove Hard Mask
7. Mesa Etch
6. Remove PR
5. Hardmask Etch
Si Substrate
Si Substrate
9. Deposit 200nm SiN Sticking Layer
10. Spin 2 layers SF11PMGI+AZ4210
11. N-metal Litho
12. SiN Dry Etch
13. N-metal Deposition
14. Liftoff
15. Apply BCB
16. BCB Ash-back
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
BCB
Si Substrate
Si Substrate

## Slide 3
25. Spin on AZ4210
26. Via Litho
27. SiN Dry Etch
28. BCB Ash
32. Probe Metal Deposition
30. Spin 2 layers SF11PMGI+AZ4210
23. SU-8 Via Litho
22. Spin on SU-8
20. P-metal Deposition
19. P-Metal Lithography
17. Nitride Removal (Dry)
18. Spin 2 layers SF11PMGI+AZ4210
21. Liftoff
24. Deposit 30nm SiN Sticking Layer
29. Strip PR
31. Probe Metal Litho
33. Liftoff
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate

## Slide 4: Hard Mask Dep & Lithography
Measure Si wafer thickness: = _______um
Prepare an additional test piece to recharacterize Si etch rate (ICP1 - #157)
Hard Mask Deposition
  Clean - ACE/ISO/DI
  Deposit Oxide
    PlasmaTherm PECVD 5000A
  Measure Oxide Thickness in Ellipsometer: = _______nm
P-Mesa Lithography
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 30s, 300mT, 100W
  Spin HMDS (5000rpm, 30s) (let sit for 30s on chip before spinning)
  Spin AZ4210 (4000rpm, 30s)
  Pre-Exposure Bake (95C, 1min)
  Lithography
    Use P-Mesa Mask – EPHI-dev-2-1 – Quadrant I
      Put Quadrant I in the bottom right of the mask holder
    Litho Tool: Autostepper
      Program: JAREDH\PROT
      Exposure: 1sec
      Focus Offset: 0
    NO POST-EXPOSURE BAKE
    Develop (AZ400K 1:4 diluted, 120sec)
    DI Rinse
  Inspect in microscope
  Dektak PR height: = ______nm
Si Substrate
Si Substrate
SiO2
Si Substrate
SiO2
Resist
Si Substrate
SiO2
I
II
III
IV

## Slide 5: Hardmask Etch and Inspect
Hardmask Etch - SiO2 Etch target 500nm
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 250nm/min = 4.16nm/s) over etch by 20% => Etch for 2’30”
Inspect in microscope
Dektak height: = ______nm
Strip PR
  ACE/ISO/DI Rinse
  1165 Soak at 80C in covered bath - 10min
  ISO/DI Rinse
  PEII - O2 Descum (100W, 300mTorr, 60-120sec)
Inspect in microscope
Dektak height: = ______nm
Si Substrate
Si Substrate

## Slide 6: Mesa Etch and Inspect
Si Etch target 2200nm
  Characterize etch rate:
    Etch Tool: ICP#2
    Switch gas CF4->SF6
    Clean: O2 Clean, 5min (10’ if last etch was Cl-based)
    Season (Recipe, Time): Si etch # 124, 5’ (400W, 50W RF, 30/10sccm SF6/O2, 1Pa)
    Etch Test Piece 1: Si etch # 124, 6’30” at ~333nm/min
    BHF dip (300nm/min): Dip for 2 min
      Dektak measure etch depth _____ nm/min
    Etch Sample: (Si etch # 124) 2200nm based on characterized etch rate
    Switch gas SF6->CF4
    Clean: O2 Clean, _______ min
Inspect in microscope
Dektak height: = ______nm
Remove Oxide (~500nm)
  BHF dip (~300 nm/min) => Dip for 2 min
  DI Rinse
Inspect in microscope
Sticking Layer Deposition
  Clean - ACE/ISO/DI
  Deposit SiN
    PlasmaTherm PECVD 200A
Si Substrate
Si Substrate
Si Substrate

## Slide 7: N-metal Litho for Nitride
N-metal Lithography
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 30s, 300mT, 100W
  Spin on resists
    PMGI SF-11: 4000rpm/1 min
      Bake 170C/1min
    PMGI SF-11: 4000rpm/1min
      Bake 170C/2min
    AZ4210 Resist: 4000rpm/30sec
    Pre-Exposure Bake (95C, 1min)
  Lithography
    Use N-Metal Mask – EPHI-dev-2-2 – Quadrant II
      Put Quadrant II in the bottom right of the mask holder
    Litho Tool: Autostepper
      Program: JAREDH\PROT
      Align to center of P-Mesa Vernier (closest to the top left of the die)
        Vernier center is (1.264325,.317175) from top left
      Exposure: 1sec
      Focus Offset: 0
    NO POST-EXPOSURE BAKE
  Develop Resist
    AZ400K 1:4 diluted, 120sec
    DI Rinse
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 70sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  Inspect in microscope
  Repeat DUV and develop as needed
  Dektak height: ____nm
Si Substrate
Si Substrate
I
II
III
IV

## Slide 8
Nitride Etch - SiN Etch target 20nm
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 310nm/min = 5.16nm/s) => Etch 10”
Inspect in microscope
Dektak height: = ______nm
Pre-metal clean
  O2 Descum 30s, 300mT, 100W)
  BHF dip
E-beam 3 metal deposition
  Ni: 50Å @.2Å/sec
  Ge: 300Å @ .5Å/sec
  Au: 300Å @
  Ni: 200Å @
  Au: 1.5um @ 2/5 Å/sec for 200/remainder
Liftoff
  1165 soak @ 80˚C for 20min
  Gently agitate with pipette
  ISO/DI rinse
Inspect in microscope
Repeat liftoff steps as needed
Nitride Etch & N-Metal Deposition
Si Substrate
Si Substrate
Si Substrate

## Slide 9: BCB Application and Cure
NOTES:
  There must not be any pauses from sample surface preparation to loading the spun sample w/ BCB into the Blue oven
  Any delays will allow increased surface oxide to regenerate on the semiconductor, increasing leakage currents
  Oxygen contaminates BCB and prolonged exposure will compromise the cure and ruin the sample
  If oven temperature is above room temperature, BCB will bubble during the cure
  Program sequence for HARD CURE (Total time in oven: ~7 hours)
    (a) 5 min ramp to 50_C, 5 min soak
    (b) 15 min ramp to 100_C, 15 min soak
    (c) 15 min ramp to 150_C, 15 min soak
    (d) 60 min ramp to 250_C, 60 min soak
    (e) Natural cool down (NOTE TIME OF COOL DOWN: ~3.5 Hours)
    (f) Oven off
BCB application
  Prepare the ‘Blue Oven’
    Check that the oven is ~25C before beginning
    Confirm program sequence is correct for Program 5
    Place Aluminum Baking Table in ‘Blue Oven’
    Run N2 through chamber at 100%
    Set alarm temperature to greater than 250C
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 30s, 300mT, 100W
  Apply BCB 3022-46 (Let sit on surface for 30 sec) – thickness ~3-4 μm
    Spin (500 rpm, 100 rpm/s, 5 sec)
    Spin (1500 rpm, 150 rpm/s, 30 sec)
BCB Cure
  Place sample on Aluminum Baking Table
  Reduce N2 flow to 60% after 3 min
  Load and run Program 5
  Wait for natural cool-down to 25C
  Remove sample and inspect under the microscope
  Turn off the ‘Blue Oven’
BCB
Si Substrate

## Slide 10
Wafer planarization ash back
  Clean carrier wafer
    ICP1 ash (Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 7 min
  Load sample on carrier wafer
    ICP1 ash(Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 2 min
    Ash rate ~ 400nm/min (it does take some time to heat up the sample before the full rate kicks in)
  Inspect sample in Microscope/Dektak/FEI SEM to see if both large and small mesas are exposed
  Repeat as needed
    Carrier clean (7min), ash (1 min), inspection
    Variation in BCB height should be under 200nm
Nitride Etch - SiN Etch target 20nm
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 310nm/min = 4.16nm/s) => Etch 10”
Inspect in microscope
Dektak height: = ______nm
P-Mesa Exposure
Si Substrate
Si Substrate

## Slide 11
P-metal Lithography
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 60s, 300mT, 100W)
  Spin on resists
    PMGI SF-11: 4000rpm/1min
      Bake 170C/2min
    AZ4210 Resist: 4000rpm/30sec
    Bake 95C/1min
  Lithography
    Use P-Metal Mask – EPHI-dev-2-2 – Quadrant III
      Put Quadrant III in the bottom right of the mask holder
    Litho Tool: Autostepper
      Program: JAREDH\PROT
      Align to P-Mesa Vernier (closest to the top left of the die)
        Vernier center is (1.264325,.317175) from top left
      Exposure: 1sec
      Focus Offset: 0
    NO POST-EXPOSURE BAKE
  Develop Resist
    AZ400K 1:4 developer 120sec
    DI Rinse
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  Inspect in microscope
  Repeat DUV and develop as needed
  Dektak height: ____nm
Sticking layer & P-Metal Lithography
Si Substrate
Si Substrate
I
II
III
IV

## Slide 12
Pre-metal clean
  O2 Descum 60s, 300mT, 100W)
Remove Native Oxide
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 250nm/min = 4.16nm/s) => Etch 5 sec
E-beam 3 metal deposition
  Pd: 30Å @1Å/sec
  Ti: 170Å @ 1Å/sec
  Pd: 170Å @ 1Å/sec
  Au: 1000Å @ 2/5 Å/sec for 200/remainder
Liftoff
  1165 soak @ 80˚C for 20min
  Gently agitate with pipette
  ISO/DI rinse
Inspect in microscope
Repeat liftoff steps as needed
RTA (Rapid Thermal Anneal)
  360˚C / 30s
Inspect in microscope
P-Metal Deposition & Anneal
Si Substrate
Si Substrate

## Slide 13
Si Substrate
Clean
  ACE/ISO/DI (3 min each)
  Dehydration bake: Hotplate 120C,3min
  O2 Descum 30s, 300mT, 100W
Spin-coat SU-8 2002 (~2um)
  10s@500rpm (ramp 100rpm/s)
  30s@3000rpm(ramp 500rpm/s)
  Bake 95C 3min
SU-8 Lithography
  Litho Tool: Autostepper
    Use Via Mask(negative) – EPHI-dev-2-3 – Quadrant II
      Put Quadrant II in the bottom right of the mask holder
    Program: JAREDH\PROT
    Align to P-Mesa Vernier (closest to the top left of the die)
      Vernier center is (1.264325,.317175) from top left
    Exposure: .4sec
    Focus Offset: -10
  Post-exposure bake:
    65C, 1min
    95 C, 2min
  Develop (SU-8 Developer)
    60s dip and shake + 15s pipette flush
    ISO/DI rinse and N2 dry
    Inspect vernier tips are open
    Repeat using 30s dip and shake + 10s pipette flush until vernier tip open
    Inspect via’s are open over contacts
  Hard Bake (Hotplate)
    95 C Starting point
    Ramp to 150 C, hold 5 min
    Ramp to 205 C, hold 5 min
    Ramp to 260 C, hold 30 min
    Ramp down 205 C, hold 5 min
    Ramp down 150 C, hold 5 min
    Ramp down 95 C, remove from hot plate
    Color should be dark red
Apply SU-8
Si Substrate
I
II
III
IV

## Slide 14: Via Lithography
Si Substrate
Sticking Layer Deposition
  Clean - ACE/ISO/DI
  Deposit Oxide
    PlasmaTherm PECVD 300A
  Oxide Thickness: = _______nm
Via Lithography
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 30s, 300mT, 100W)
  Spin HMDS (5000rpm, 30s) (let sit for 30s on chip before spinning)
  Spin AZ4210 (4000rpm, 30s)
  Pre-Exposure Bake (95C, 1min)
  Litho Tool: Autostepper
    Use Via Mask (positive) – EPHI-dev-2-3 – Quadrant I
      Put Quadrant I in the bottom right of the mask holder
    Program: JAREDH\PROT
    Align to center of P-Mesa Vernier (closest to the top left of the die)
      Vernier center is (1.264325,.317175) from top left
    Exposure: 1sec
    Focus Offset: 0
    Develop (AZ400K 1:4 diluted, 120sec)
    DI Rinse
  Inspect in microscope
  Dektak height: = ______nm
I
II
III
IV
Si Substrate
Si Substrate

## Slide 15
Sticking Layer Etch - SiO2 Etch target 30nm
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 250nm/min = 4.16nm/s) => Etch for 20 sec
Inspect in microscope
Dektak height: = ______nm
BCB Ash – target ~1000nm
  Clean carrier wafer in Panasonic ICP #1 (Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 7 min
  Load sample on carrier wafer
    ICP ash (Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 2 min
    Ash rate BCB ~ 400nm/min
  Inspect sample in Microscope/Dektak to check that N-metal is exposed
  Repeat as needed
    Carrier clean (7min), sample ash (1 min), inspection
Strip PR
  1165 soak @ 80˚C for 20min
  Gently agitate with pipette
  ISO/DI rinse
Inspect in microscope
Repeat liftoff steps as needed
Via Etch
Si Substrate
Si Substrate
Si Substrate

## Slide 16: Probe Metal Litho
Probe-metal Lithography
  Clean
    ACE/ISO/DI
    Dehydration bake: Hotplate 150C, 2-5min
    O2 Descum 60s, 300mT, 100W)
  Spin on resists
    PMGI SF-11: 4000rpm/1 min
      Bake 170C/1min
    PMGI SF-11: 4000rpm/1min
      Bake 170C/2min
    AZ4210 Resist: 4000rpm/30sec
    Bake 95C/1min
  Lithography
    Use Probe-Metal Mask – EPHI-dev-2-3 – Quadrant III
      Put Quadrant III in the bottom right of the mask holder
    Litho Tool: Autostepper
      Program: JAREDH\PROT
      Align to P-Mesa Vernier (closest to the top left of the die)
        Vernier center is (1.264325,.317175) from top left
      Exposure: 1sec
      Focus Offset: 0
    NO POST-EXPOSURE BAKE
  Develop Resist
    AZ400K 1:4 developer 120sec
    DI Rinse
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 70sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  Inspect in microscope
  Repeat DUV and develop as needed
  Dektak height: ____nm
Si Substrate
Si Substrate
I
II
III
IV

## Slide 17
Pre-metal clean
  O2 Descum 60s, 300mT, 100W)
E-beam 4 metal deposition
  Ti: 50Å @.2Å/sec
  Pt: 200Å @ .5Å/sec
  Au: 1.5um @ 2/5 Å/sec for 200/remainder
Liftoff
  1165 soak @ 80˚C for 20min
  Gently agitate with pipette
  ISO/DI rinse
Inspect in microscope
Repeat liftoff steps as needed
Si Substrate
Probe-Metal Deposition
Si Substrate

## Slide 18: P-Mesa Vernier
(1264.325.,-317.175)
Vernier Center when This mask quadrant is in the lower right.

## Slide 19: Mask Layout EPHI-dev-2-1
P-Mesa (Positive)
Si-Waveguide
QW-Etch2
QW-Etch1

## Slide 20: Mask Layout EPHI-dev-2-2
N-Substrate
VCs
P-Metal
(Positive)
N-Metal
(Positive)

## Slide 21: Mask Layout EPHI-dev-2-3
Via-Etch
Positive
Implant
Probe-Metal
Positive
Via-Etch
Negative

## Slide 22: Questions
Double check all metal stacks
How long to develop AZ4210 (70s or 2min)
Fix E-beam 4 dep rate info on slide 17
Is this a good SU8 thickness?

## Slide 23
http://www.microchem.com/pdf/SU-82000DataSheet2000_5thru2015Ver4.pdf