## Slide 1: Sweeper Run#2B Grating Process Report
Jock Bovington

## Slide 2: Sweeper Chip Layout
S2B#1
S2B#2

## Slide 3: Etch Targets (S2B#2)
Dicing and grating etch.
75 nm
50 nm

## Slide 4: Current State of Sweeper Chips
S2B#1a2
S2B#1
S2B#2
S2B#1b
S2B#1c
S2B#2a
S2B#2b
S2B#2c
S2B#1a1
ON HOLD
32nm
54nm
43nm
105nm
All etch depths are approximate and from a single measurement of a 50% DC Grating on the first column of the die.
75nm

## Slide 5: Etch Results
Chart: AFM Etch Depth of 50% DC Grating
| 10 | 40 | 23 | 68 | 49
Run#2 | 32 | 54 | 43 | 105 | 75
Run#1 | 83
 | SWEEPER RUN#2B |  | 
 | Sample | Etch time (s) | Ech Depth (nm)
 | S2B#1a1 | 10 | 32
 | S2B#1a2 | 40 | 54
 | S2B#2a | 23 | 43
 | S2B#2b | 68 | 105
 | S2B#2a | 49 | 75
Reference from Run#1 |  |  | 
 | S1#1 | 35 | 83

## Slide 6: Before Cleaning Polymer
Note that the horns are much higher that the flat top

## Slide 7: After Cleaning Polymer with Gasonics
Note that the horns are basically removed. Further cleaning would improve this.

## Slide 8
1
3 (left side)
2 (left side)
4 (bottom-most grating in this group)
1. 50 % dc
2. 20% dc (left)
3. Smallest width
4. 80% dc
5. 50% dc for comparison across the die.
5 (bottom-most grating in this group)

## Slide 9: Characteristic AFM Data
All data was taken on S2B#1a2
The following 5 scans are representative of all of the data collected on this sample.
Note that there is evidence that this sample will look better if cleaned further as it was simply stripped and O2 Descummed for 30s. See data at position #4.

## Slide 10: Characteristic AFM Data Position #1

## Slide 11: Characteristic AFM Data Position #2

## Slide 12: Characteristic AFM Data Position #3

## Slide 13: Characteristic AFM Data Position #4
Note peak of this tooth to the gap is much higher that the typical etch depth. This suggests that this is simply polymer.

## Slide 14: Characteristic AFM Data Position #1

## Slide 15: Characteristic SEM Data

## Slide 16: Characteristic SEM Data

## Slide 17: Characteristic SEM Data

## Slide 18: Measurement Recommendations
As I need further results for my thesis project, I can not take time to do the following analysis. However, I see it as vital to further understanding of the grating process.
There are 2 “optical die” which will not continue the process through the metal and other processing. Below are some recommended measurements:
A proper analysis of the proximity effects the would impact the duty cycle of the beginning vs. the middle of the grating. I have done this on a planer surface, but not on a patterned surface. This will give predictive capability of the pattern bias between the make and actual pattern.
Rough map of alignment error. Note that gratings were grouped into local and global alignment groups based on whether they had gratings narrower than the waveguide width. Martijn has the details.
AFM study of etch depth vs. pattern size. The data collected so far with Jonathan is not enough to be conclusive.
Cross-sectional SEMs of multiple duty cycles of the gratings.