## Slide 1: Hybrid Silica Platform
Jock Bovington

## Slide 2: Mask Layers and Polarity
  Waveguide (done by LioniX) Vertical Channels (P resist) Excess Epi Removal Window (N resist) P Mesa (P resist) N Metal (P resist) Excess Epi Removal Frame #1 (P resist) N Layer Taper (P resist) Excess Epi Removal Frame #2 (P resist) AlGaAs Oxidation Reveal (P resist) N Vias (P resist) P/Probe Metal (P resist)

## Slide 3: Process Summary
10 Lithography steps (2 Critical Taper Lithos)
3 PECVD Hardmask Steps
2 Metal Depositions
3 Oxide Dry Etches
2 GaAs Dry Etches
3 Oxide Wet Etches
1 GaAs Wet Etch, 3 Full Epi Cleanup Wet Etches
1 Spin-on-Glass Deposition and Cure at 425C
1 AlGaAs Thermal Oxidation 360C
2 CMPs

## Slide 5: Check wafer quality
LioniX wafer with thick top oxide

## Slide 6: Wafer Thinning
CMP down wafer to ~100-200nm
Clean thoroughly with ultrasonics in Ter:Iso:DI
Confirm <1nm RMS

## Slide 7: Vertical Channels PR Masking
AZ-4210 – Pos. PR – 4kRPM
Pre-bake 95C
Expose ~1s
AZ-400K (1:4) diluted

## Slide 8: Vertical Channels Etch
ICP#2 SiO2 Nano etch

## Slide 9: Vertical Channels PR Strip
1165 - 80C
PEII O2 Plasma – 1min

## Slide 10: Bonding Process
Confirm surface roughness <1nm RMS
Clean: ACE,ISO,DI,(Tergitol),PEII
(Ozone if Tergitol is used)
O2 Activate
Bond/Anneal

## Slide 11: III/V substrate removal
Lap substrate to ~100um
Spray etch off substrate (NH4OH:H2O2 1:20)
Stops on InGaP (or Al0.8Ga0.2As Layer, which is not compatible with P-mesa hardmask wet etching)

## Slide 12: III/V Edge Die Cleanup
Neg. PR (withstands wet etch)
???Any Suggestions???

## Slide 13: III/V Edge Die Cleanup
Wet etch epi
Strip PR

## Slide 14: P-mesa Hardmask - Deposition
PECVD – SiO2
  2 Depositions with air soak to prevent pinholes

## Slide 15: P-mesa Hardmask - Patterning
Thin Pos. PR
  Recommendation?

## Slide 16: P-mesa Hardmask - Patterning
ICP#2 SiO2 Nano etch
BHF under cut

## Slide 17: P-mesa Etch
RIE#5 or Unaxis (DOWN!!!)

## Slide 18: Frame Removal Pattern
Pos. PR
  Resistant to GaAs Wet etchs

## Slide 19: Frame Removal Etch
BHF Mask Etch (suggested)
AlGaAs Wet Etch

## Slide 20: Frame Removal Strip
Strip

## Slide 21: AlGaAs Oxidation Protection Deposition
PECVD Oxide
  Thick enough to be N taper hardmask

## Slide 22: AlGaAs Oxidation Protection Patterning
Pos. PR

## Slide 23: AlGaAs Oxidation Protection Patterning
ICP#2 SiO2 Nano etch (maybe)
BHF side wall cleanup - Etches the AlGaAs

## Slide 24: AlGaAs Oxidation Protection Strip
1165, PEII

## Slide 25: AlGaAs Oxidation Pre-Clean
Solvents, O2 Plasma
NH4OH:DI (1:10), 10s

## Slide 26: AlGaAs Oxidation
360C in Lindberg furnace

## Slide 27: Apertured Mesa Protection Hardmask Deposition
PECVD

## Slide 28: N Layer Taper Hardmask Patterning
Pos. PR

## Slide 29: N Layer Taper Hardmask Etch
ICP#2 SiO2 Nano etch
BHF Undercut

## Slide 30: N Layer Taper Strip
1165

## Slide 31: N Layer Taper Etch
RIE#5 or Unaxis
N Layer Wet Etch

## Slide 32: Frame Removal Etch #2 - Patterning
Pos. PR

## Slide 33: Frame Removal Etch #2 - Patterning
Pos. PR
Possibly PMGI

## Slide 34: Frame Removal Etch #2 - Patterning
N Layer/SL Wet Etching

## Slide 35: Frame Removal Etch #2 - Strip
1165, PEII

## Slide 36: N metal Patterning
Bi Layer lift-off PR
  AZ-4210, PMGI

## Slide 37: N metal Patterning
BHF Oxide etch
NH4OH:DI (1:10) GaAs Clean

## Slide 38: N metal Deposition
Ebeam - N Metal Stack
Lift-off

## Slide 39: Cladding Deposition
Cladding Layer Deposition
Spin On Glass

## Slide 40: Cladding Planarization
CMP

## Slide 41: Cladding Etch Back
Oxide Etchback

## Slide 42: N Vias Patterning
Pos. PR

## Slide 43: N Vias Etch
ICP#2 SiO2 Nano etch
BHF Clean-up

## Slide 44: N Vias Strip
1165
PEII

## Slide 45: P/Probe Metal Patterning
Bi Layer Lift-off
  AZ-4210, PMGI

## Slide 46: P/Probe Metal Pre-Depostion
Etch Stop Removal
NH4OH:DI (1:10) GaAs Surface Cleaning

## Slide 47: P/Probe Metal Depostion/Lift-off
Ebeam P-metal/Probe Metal
Lift-off

## Slide 49: Novel Electro-Mechanical Bond
Jock Bovington

## Slide 50: Alignment-free Selective Electro-mechanical Bonding
Using plasma assisted bonding it is possible to bond both to metal and semiconductor/dielectric surfaces with a semiconductor/dielectric surface. For example: would be especially useful for bonding a III-V semiconductor to CMOS circuit without the limitation of wafer alignment. By adding a thin contact metal stack on-top of a pre-existing CMOS circuit and then bonding III-V to both the oxide and metal and annealing under pressure covalent bonds will form between the oxide and III-V and interdiffusion will occur between the metal with the semiconductor. This process simply requires extremely low surface roughness of all surfaces which can be achieved with CMP or another smoothing process. Height profiles such as that shown above can be achieve with short post CMP etching. It has been shown that the metal contacts can both contract and expand during the duration of this process so the above configuration may be preferred, though is not the only configuration claimed.
Advantages: Not covered in prior art for electro mechanical bonding, no alignment required, compatible with CMOS as back end process, enables bottom contacting on SOI, Si, etc. Thermal regulation benefits.

## Slide 51: Metal-to-Metal Bonding in situ with Semiconductor Low Temp Plasma Assisted Wafer Bonding
PRIOR ART*
*Method for room temperature metal direct bonding
Qin-Yi Tong et al

## Slide 52: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Deposition
Ebeam Cr

## Slide 53: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Deposition
PECVD Si3N4

## Slide 54: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Patterning - PR
AZ-4210 – Pos. PR – 4kRPM
Pre-bake 95C
Expose ~1s
AZ-400K (1:4) diluted

## Slide 55: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Patterning - Nitride
ICP#2 SiO2 Nano etch

## Slide 56: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Patterning - Strip
1165 – 80C
Limit exposure to PEII to <1min (oxidizes Cr)

## Slide 57: Optional: Electrical Contact Addition Cr/Oxide Hard Mask Patterning - Cr
ICP#2 Cr Etch (known to undercut)

## Slide 58: Optional: Electrical Contact Addition Deep Oxide Etch
ICP#2 SiO2 Nano etch
Simultaneously etches nitride hardmask

## Slide 59: Optional: Electrical Contact Addition Metal Fill
Leave Cr
Ebeam Metal fill
  Au? Cu?
  What are Si Contact layer stacks? Ti/Pt/Au…

## Slide 60: Optional: Electrical Contact Addition Metal Planarization
CMP

## Slide 61: Optional: Electrical Contact Addition Eutectic Metal Deposition
Lift-off a eutectic metal stack for contact to n-type bonding layer.

## Slide 62: Optional: Electrical Contact Addition Eutectic Metal Encapsulation
Use PECVD Oxide to encapsulate metal

## Slide 63: Optional: Electrical Contact Addition Eutectic Metal Layer Planarization
CMP so both metal and Oxide are <1nm RMS
BHF over etch the oxide leave slight metal pillars. This ensures metal to semiconductor contact and will be consumed in eutectic process during bonding.
Following this is the standard bonding process potentially with a metal pretreatment such as H plasma.