## Slide 1
HSP- Silicon waveguide process development
6 splits.
Three different tools to deposit/grow oxide hardmask for waveguide definition i.e. Tystar oxidation furnace, Sputter4 AJA, Plasma-Therm PECVD.
Two different resist recipes. SPR955-0.9um and CEM+SPR955-0.9um

## Slide 2
PECVD
Sputter
Thermal
With CEM

## Slide 3
PECVD
Sputter
Thermal
With CEM

## Slide 4
Without CEM
PECVD

## Slide 5
PECVD
Sputter
Thermal
With CEM

## Slide 6
PECVD
Sputter
Thermal
Without CEM

## Slide 7
CEM - Thermal
No CEM - PECVD

## Slide 8
SUMMARY
Accuracy – Sputter(~5nm)>PECVD(10-15nm)>Thermal- dry(10-20nm).
Marginal(sputter) to no difference between various oxides. (Slide 4/5)
CEM has very good sidewall angle. (Slide 4/5)
Sidewall roughness, CEM = No CEM. (Slide 6)
CEM removes the constraint on design for overdose.
CEM leaves the oxide surface marginally cleaner. (Slide 6)
CEM process introduced tiny particles(streaks), or I am sloppy as a first timer, as all Coldren group students do not have a problem at all.