## Slide 1: Alternatives to SiOVert
ICP2 SiO2 etch roundup
Molly 4/2011

## Slide 2: 0.5Pa, 500W RF, 50W bias, 20 sccm CHF3 + 20 sccm CF4
3 minute etch time
PR removed in ACE/ISO only
Looks decent, but not very vertical
Si
Ge
SiO2
PR residue
SiO2
Ge
Si
Si
Ge
SiO2

## Slide 3: 0.5Pa, 500W RF, 50W bias, 20 sccm CHF3
5 min 45 sec etch
Clearly isotropic
Probably shouldn’t use this one
Ge
SiO2
SiO2
SiO2
Ge
Ge
Si

## Slide 4: 0.5Pa, 900W RF, 200W bias, 40 sccm CHF3
1 min 20 sec etch
Standard SiOvert
Tends to roughen Ge surface
SiO2
SiO2
SiO2
Ge
Ge
Ge
Si

## Slide 5: 0.5Pa, 900W RF, 50W bias, 10 sccm CHF3 + 30sccm CF4
Ben Curtin’s etch
Polymerization with SPR 220-3
  Probably – there’s some residue that forms in areas that have been etched that reacts with PRX-127, won’t come off in PEII (successive 30s descums), and comes off slowly/not completely in gasonics. It ends up leaving small pits (see last slide) on the bottom Si after the mesa etch (ICP2 BCl3/Cl2)
Ge
Ge
SiO2
SiO2

## Slide 6: Comparison
0.5Pa, 500W RF, 50W bias, 20 sccm CHF3 + 20 sccm CF4
0.5Pa, 500W RF, 50W bias, 20 sccm CHF3
0.5Pa, 900W RF, 200W bias, 40 sccm CHF3
0.5Pa, 900W RF, 50W bias, 10 sccm CHF3 + 30sccm CF4

## Slide 7: 0.5Pa, 900W RF, 50W bias, 10 sccm CHF3 + 30sccm CF4 – after mesa etch
Little pits – don’t seem to have huge impact on device performance?
Ge mesa
Streak: darker in optical microscope, pretty obvious to naked eye
Ge mesa
Si
Si
Si
Si

## Slide 8: Ben’s etch + Cr hardmask
0.5Pa, 900W RF, 50W bias, 10 sccm CHF3 + 30sccm CF4
After Cr etch and ACE/ISO – looks clean in optical scope, but there is PR on sides of Cr
Cr
SiO2
Cr
SiO2
Resist
After SiO2 etch (2 min + 15 sec) – angle >85 degrees

## Slide 9: Ben’s etch + Cr hardmask
Can remove the Cr before or the mesa etch or just not bother
Before: etch in ICP2 1’55” 23.3 Cl2, 6.8 O2, 1.37Pa, 500 ICP, 15RIE. 0.6nm/s
Ge is etched, but not too much (50-100nm)
Ge
Ge
SiO2
SiO2