## Slide 1: Selective Ge wet etching

## Slide 2: Goal/context
Proposed process follower
Advantages:
  PDs automatically aligned to waveguide
  Don’t have to find a dry etch for Ge that leaves top Si surface smooth
Si
Waveguide etch (dry)
Mesa etch (wet)
Si
Passive WG

## Slide 3: Options
Many solutions etch Ge with good Si selectivity:
  H202 alone (heated or at room temp)
  H2O2:NH4OH:DI
    NH4OH by itself will etch Si, so it is important to keep a large H2O2 concentration
  H2O2:HCl:DI
  H2O2:H2SO4:DI
    Very fast

## Slide 4: H2O2
Etch is not even, stops at Si/Ge interfacial layer, especially in large open areas
Surface left pretty smooth
Except when it isn’t:
Some Ge
Ge
Si

## Slide 5: NH4OH:H2O2:DI
Various concentrations tested, rates usually ~200nm/min
Etched surface rougher than as-grown surface
  Laser pointer test
Ge etches anisotropically
Ge
Si

## Slide 6: HCl:H2O2:DI
Leaves more SiGe than NH4OH:H2O2:DI
  Visible to naked eye, using color of surface
Etched surface clearly rougher than as-grown surface
Etches Ge isotropically
I think the pits are from the growth, not the wet etch
Si
Ge
Si
Ge

## Slide 7: More on pits
Looks like a thin damaged layer at Si surface

## Slide 8: Also tried
NH4OH:H2O2:DI+HF:HNO3:DI 1:1:50 1’
Could also try ICP1 ashing chamber CF4/O2 (50:200 sccm)

## Slide 9: Dry etch after wet etch
5 second Cl ICP etch after selective wet etch (wet etch was all the way to the Si)

## Slide 10: Dry etch only (point of reference)

## Slide 11: Wet + dry etching
Process:
  Wet etch 3-3.5 min. HCl:H2O2:DI 2:2:15
  Dry etch 5-20s in standard WG etch (SF6/O2 ICP)
3-die piece: 3.5 min wet etch
4-die piece: 3 min wet etch
+15s +2s dry etch
+8s +5s dry etch
+8s dry etch

## Slide 12: Summary
All images are the same scale, wet-only and wet+ dry are both flat, though dry-only is angled
Wet + dry works pretty well
Wet etch only
Dry etch only
Wet + dry
Si
Si
Si
Ge
Ge
Waveguide sidewall