## Slide 1: InGaAsP Wet Etch
4/20/2009

## Slide 3: InGaAsP Pre Etch
Measurement Site 1
Measurement Site 2
1997 nm Step
830 nm Step
2027 nm Step
Die 1

## Slide 4: AWG Die 2 Pre Etch

## Slide 5: InGaAsP Pre Etch
Measurement Site 1
Measurement Site 2
1997 nm Step
830 nm Step
2027 nm Step
Post 8.5 minute Etch in 1:1:10 H2SO4:H2O2:DI
Post 2270 nm – Pre 1960 nm = 310 nm loss
Post 2377 nm – Pre 2027nm = 350 nm loss

## Slide 6: Underetch Post 8.5 minutes. Edges cleared but 90% of area still underetched.