## Slide 1: Useful DQPSK experimental results
Data by Stefano and Kim
Compiled by Molly

## Slide 2: PIN Photodetector Epi Order
Layer | Composition | Doping Concentration | Thickness
Substrate | InP | P - 2-8x1018 cm-3 | 
Buffer | InP | N.I.D | 0.2 μm
P-contact layer | In0.53Ga0.47As | P - 1x1018 cm-3 | 0.1 μm
Absorption layer | In0.53Ga0.47As | N.I.D | 0.5 μm
N layer | InP | N - 1x1018 cm-3 | 200 nm
Super lattice | In0.794Ga0.206As0.145P0.855(3x) | N - 1x1018 cm-3 | 10 nm
 | InAs0.312P0.6873(3x) | N - 1x1018 cm-3 | 10 nm
N bonding layer | InP | N - 1x1018 cm-3 | 10 nm
Cap | In0.53Ga0.47As | N - 1x1018 cm-3 | 0.2 μm
We have 1 wafer of this left

## Slide 3: PD layout
General dimensions:
  Si waveguide: 2um wide
  Mesa: 11.5um wide, varying lengths
  Pads: GSG 125, 80 um center pad with 30um gap
Input WG
7o angled mesa
At input:
n-InP to mesa: 1um
Mesa edge to p-metal: 1um
On sides:
Mesa to n-metal: 4um

## Slide 4: Contact resistance – spin 1
P isn’t very highly doped, but this is implausibly high
Chart: Gap (um)
| 5 | 10 | 15 | 30
 | 841.2 | 1307.4 | 1591 | 2583
Chart: Gap (um)
| 5 | 10 | 15 | 30
 | 9.54 | 15.982 | 23.066 | 50.17
P
N
ρc=1e-3 Ωcm2, Lt=4um, Rsh=6.8kΩ/
ρc=negligible, Lt<1um, Rsh=165Ω/

## Slide 5: RF parameters – spin 2
For 11.5um wide PDs, from S11 data
P-contact resistance is at most 8e-5 Ωcm2
Parasitic C ~10fF (seems low…)
Transit time ~2.4ps (f3dB from transit time = 66GHz)
  Assuming:
  R and C come from S11 data, and H(jω) is the bandwidth (S21), so we can fit for tau.
  The PDs were mostly RC limited, so this number is not very accurate, though it agrees reasonably well with Silvaco simulations
Chart: PD length (um)
| 30 | 35 | 40 | 50 | 60
C | 95.5 | 106 | 128 | 157 | 187
Expected C | 84.879 | 99.0255 | 113.172 | 141.465 | 169.758
Expected C: d=550 | 77.163 | 90.0235 | 102.884 | 128.605 | 154.326
Chart: 
| 30 | 35 | 40 | 50 | 60
Rs | 20.4 | 19 | 14.4 | 14 | 10.9

## Slide 6: RF parameters – spin 2
Length | Series resistance (Ω) | Capacitance (fF) | -3dB bandwidth (electrical)
30 | 20.4 | 95.5 | 23
35 | 19 | 106 | 22
40 | 14.4 | 128 | 22
50 | 14 | 157 | 18
60 | 10.9 | 187 | 17

## Slide 7: Dark current – all HSP PDs ever
Hyundai (laser-like epi and structure, 100um long x 2um wide) 1V 6.20E-08 4V 4.22E-07 PIN (DQPSK fab run, ~25x10 um, probably) 3V 2.00E-05 UVA/PICO (UTC, 7x100um - 700nm thick i-region around 400nm away from the bonded interface) 5V 1.00E-09