## Slide 1: SiP Meeting – Isolator
Jason
3/30/2010

## Slide 2: Waveguide Design
Width of the ring | Resonance wavelength splitting | Confinement factor of Ce:YIG
200 nm | 173 pm | 65.42%
300 nm | 78 pm | 29.34 %
400 nm | 30.2 pm | 12.35 %
500 nm | 14.7 pm | 6.21 %
Si
BOX
700 nm
w
Ce:YIG
Ce:YIG
  Thickness: 200 nm
  n=2.22
  Faraday coefficient: 4500 deg/cm
Wavelength splitting is linearly proportional to confinement factor of MO !
Parameters used for the following calculation

## Slide 3: Definition of Isolation Ratio and Insertion Loss
Transmission (dB)
Wavelength (nm)
Isolation ratio
Insertion loss
Input
Output

## Slide 4: Coupling between the Ring and Waveguide
κWG/γring
Insertion loss (dB)
κWG/γring
Q=104
Q=105
Q=106
Isolation ratio (dB)
Single-ring isolator
κWG
γring
γring: round-trip loss
κWG: power coupling ratio between the WG and the ring
Larger coupling  larger isolation ratio and smaller insertion loss

## Slide 5: Influence of Q factor
Isolation ratio (dB)
Q factor
κWG=0.5γring
κWG= γring
κWG=2γring
Single-ring isolator
Higher Q  larger isolation ratio
 require smaller coupling to reach the same insertion loss

## Slide 6: Coupling between the Ring and Waveguide
κring/γring
Insertion loss (dB)
κWG=γring
κWG=2 γring
κWG=3 γring
κring/γring
Isolation ratio (dB)
κWG=γring
κWG=2 γring
κWG=3 γring
Q is assumed 105 for calculation
κWG
γring
κring
γring: round-trip loss
κWG: power coupling ratio between the WG and the ring
κring: power coupling ratio between the two rings
Double-ring isolator
Stronger inter-ring coupling  wider top flat band  smaller isolation ratio
 smaller insertion loss

## Slide 7: Influence of Q factor
κ=γring
κ=2 γring
κ=3 γring
κ=4 γring
κ=5 γring
Isolation ratio (dB)
Q factor
κ / γring | Insertion loss
1 | 7.96 dB
2 | 4.22 dB
3 | 2.85 dB
4 | 2.15 dB
5 | 1.73 dB
Q is assume 105 for calculation
κ= κWG =κring
Double-ring isolator
Higher Q  larger isolation ratio
Lager coupling  smaller isolation ratio but also smaller insertion loss

## Slide 8: Comparison between the Single- and Double-Ring
Isolation ratio (dB)
Q factor
Double-ring
Single-ring
Isolation ratio (dB)
Double-ring
Single-ring
Faraday coefficient (deg/cm)
Double-ring isolator can enhance isolation ratio!

## Slide 9: Influence of Confinement Factor
Isolation ratio (dB)
κring/γring
Г=10%
Г=20%
Г=30%
Г=40%
Г=50%
Loss=10 (1/cm)*ГMO
Wavelength splitting : 0.24nm*ГMO
Confinement factor has little effect on isolation ratio because:
larger ГMO  larger wavelength splitting but smaller Q

## Slide 10: Summary
Double-ring isolator has larger isolation ratio at the expense of increased insertion loss.
  Insertion loss can be compensated by stronger coupling.
Higher Q and larger Faraday coefficient is always better.
  Magneto-optic material with low loss and high Faraday coefficient is the key.
Experiment plan
  Find out the right sputtering and annealing recipe for Ce:YIG
    Film characterization by X-ray diffraction
  Fabricate waveguides on SOI by E-beam lithography (2-layer litho)
    Single ring with Through Port
  Permanent magnets are here.