## Slide 1: Si/Ge PD v.2 process flow
6/2/11

## Slide 2: Hard mask deposition
Clean, then deposit 100nm SiO2 in PECVD
Then 60nm Cr in Ebeam 1
Si
Ge
250 nm SiO2
60 nm Cr

## Slide 3: HM patterning
Stepper: SPR 220-3
Etch in ICP 2 (Coldren recipe for the CR)
Remove PR
Ben’s recipe in ICP2 (as vertical as SiOvert, less damage to Ge, but sometimes PR ends up everywhere when a Cr mask isn’t used)
Si
Ge
250 nm SiO2
Ge
Ge
SiO2
SiO2
Ben’s
SiO vert
60 nm Cr
Si
Ge
250 nm SiO2
PR
60 nm Cr

## Slide 4: Mesa etch
Strip Cr, then
Etch in ICP 2 (standard Si photonics WG etch recipe)
Si
Ge
250 nm SiO2

## Slide 5: Passivation deposition
Strip hardmask
Clean thoroughly then deposit in PECVD: 500nm SiO2+250nm SiO2 + 250nm SiN
Si
Ge
750 nm SiO2
250 nm SiN

## Slide 6: Via etch
Pattern PR (SPR 220-3)
Dry etch to last 100nm
Wet etch remaining 100nm
Si
Ge
PR
PR

## Slide 7: Pre-metal
Strip PR, pre-metal clean, deposit 5nm SiO2
Si
Ge

## Slide 8: Thin metal
2-layer resist (LOL2000+nLOF2020), etch thin SiO2 in dilute HF, deposit 30nm Ni/50nm Ti/400nm Au
Si
Ge
PR
PR
PR

## Slide 9: SU8
Spin and pattern
Si
Ge
Si
PD area
Pad area
SU8

## Slide 10: SU8 sticking layer
Positive resist liftoff – 25nm IBD SiN
Si
Ge
Si
PD area
Pad area
SU8
Si
Ge
PR
PR
PR

## Slide 11: Probe metal
w/rotation for sidewall coverage (resist not shown)
Si
Ge
Si
PD area
Pad area
SU8
Si
Ge