## Slide 1: Si Photonics Meeting - Isolator
Jason
1/19/2010

## Slide 2: Outline
Optical isolator literature review
  Faraday rotation
  Nonreciprocal phase shift and optical loss
Optical isolator design based on ring resonators

## Slide 3: Conventional optical isolator
With magnetic field parallel to the light propagation direction, right-hand and left-hand circular polarized light has different propagation constants, and thus the polarization rotates. This is so called Faraday rotator. The rotation direction is independent of propagation direction, which is always counterclockwise (or clockwise).
Placing the two polarizers in 45 degree with a 45-degree Faraday rotator in-between, only one direction of light can pass.
Magneto-optic material
(polarization rotates 45 degree)
Light propagation direction
B

## Slide 4: Nonreciprocal phase shift and optical loss
Propagation direction
Magnetic field
αeff
neff
M=0
M≠0 for backward and forward light
Magnetic field transverse to the light propagation direction
  Nonreciprocal phase shift
    Different propagation constant sfor forward and backward light
  Nonreciprocal optical loss
    Different absorption coefficients for forward and backward light

## Slide 5: Nonreciprocal propagation constant
z
y
x
Magnetic field in y-direction
Magnetic field in x-direction
Propagation direction

## Slide 6: Literature example
Lateral magnetic field
TM-polarized light has nonreciprocal phase shift
Interferometer structure
  Forward: construction interference
  Backward: destructive interference
Different directions of magnetic fields on both arms shorten the required length to half
Yokoi, et. al., Applied Optics, 2003

## Slide 7
Yokoi, et. al., Applied Optics, 2000

## Slide 8: Literature of nonreciprocal loss
Shimizu, et. al., JLT, 2006

## Slide 9: Summary of nonreciprocal propagation
The 3 right configurations all have opposite propagation constant shift compared to the original one
Propagation direction
Propagation direction
Propagation direction
Magnetic field
Propagation direction
Magnetic field
z
y
x
Magnetic field
Magnetic field
θF Can be parallel or antiparallel to the magnetization

## Slide 10: Concept of isolators based on ring resonators
B
x
y
z
Single ring
Double ring
Nonreciprocal phase shift
  Magnetic field transverse to the propagation direction
  Light propagating in clockwise (CW) and counterclockwise (CCW) directions has different propagation constants
  Optical input with resonance wavelength will be blocked while the other direction input will not.
Q of the ring: 106
κ1 =κ2=3γ, κ_ring=4 γ

## Slide 11: Nonreciprocal propagation constant in ring resonators
B
YIG
Si
BOX
Si
I
YIG
Metal wire
B
Top view
Cross-section
y
x
Radial magnetic field direction toward the center of the ring (or outward)
Propagation constant change is proportional to field intensity difference at the boundary of the YIG layer
y0
y1
y0 and y1 are the bottom and top boundary of the YIG layer

## Slide 12: Nonreciprocal propagation constant in ring resonators
Input
output
B
Si
BOX
Si
MO
B
x
y
x0
x1
x0 and x1 are the left and right boundary of the YIG layer
Magnetic field direction has to be perpendicular to the wafer (the device)
Propagation constant change is proportional to field intensity difference at the boundary of the YIG layer

## Slide 13: Maximize the propagation constant difference
Larger Faraday rotation (θF)
Place the YIG layer in the region where field intensity is maximal
Double magneto-optic layers (+θF & -θF)
Wallenhorst, et. al., JAP, 1995

## Slide 14: YIG/nitride waveguide design
W=1um
H=0.4um
SiO2
YIG
nitride

## Slide 15: SOI rib waveguide with YIG on the sidewall
W=0.5um
H=0.7um
Slab height
YIG
MO material : Ce:YIG
  refractive index =2.22
  Loss: 20 cm-1
  thickness: 200nm

## Slide 16: SOI rib waveguide design
W=0.3um
W=0.4um
W=0.5um
W=0.6um
W
H=0.7um
Slab height
YIG
MO material : Ce:YIG
  refractive index =2.22
  Loss: 20 cm-1
  thickness: 200nm

## Slide 17: Single mode condition for rib waveguides
W
H=0.7um
Slab height
Single mode
Multi-mode
Soref, et.al., JQE, 1991
Single mode condition

## Slide 18: Coming next
Design resonator & waveguide
Material preparation
  Ce:YIG (CeY2Fe5O12)
  BIG (Bi3Fe5O12)
Process flow based on silicon or silica waveguides