## Slide 1: Grating Analysis 2010-12-01
Jock Bovington
Wenzao Li
Jared Bauters

## Slide 2: Outline
Experiment design with Process flow
Brief summary of AFM analysis
Characteristic SEM images
Dose/Duty Cycle analysis

## Slide 3: Experiment design with Process flow
Two initial calibration samples were run
  InP Epi (epump2) with IBD SiO2 (88nm)
    11nm Au Thermal Evaporated
    Developed
    ICP #2 (Oxide Etch)
    AFM
    RIE #2 (InP/SL Etch) - Thanks Mike and Jared
    AFM
  SOI (700nm Si, 1um BOx)
    11nm Au Thermal Evaporated
    Developed
    AFM (~393+/-7nm)
    Deep Si RIE “Bosch” (Si Etch) - Thanks Jason
    AFM
Calibration includes dose and duty cycle splits

## Slide 4: Grating Analysis
with assistance from Bill Michell, Jared and Wenzao

## Slide 5: AFM Analysis
AFM gives valuable information about the quality of a grating, but can only take a small snap shot.

## Slide 6: SOI AFM Analysis
390nm
425nm
Before Etch
After Etch
fd

## Slide 7: InP AFM Analysis
~350nm
~347nm
Before Etch
After 20s Oxide Etch
~344nm
~317nm
After 40s Oxide Etch
After 105s Oxide Etch

## Slide 8: InP AFM Analysis
~181nm
Before Etch
After Strip & 52s InP Etch
~317nm
~189nm
After Strip, 52s InP Etch, H2SO4

## Slide 9: SEM Analysis
Top down SEM is an excellent way to gain understanding about gratings.
  Dose
  Proximity Effects
  Duty cycle
  Qualitative information about pattern distortion

## Slide 10: Low Dose, Proximity Effects

## Slide 11: Higher Dose, Uniform Gratings

## Slide 12: SOI Image Analysis Results

## Slide 13: SOI Image Analysis Results

## Slide 14: SOI Image Analysis Results

## Slide 15: SOI Image Analysis Results

## Slide 16: SOI Image Analysis Results

## Slide 17: InP Image Analysis Results

## Slide 18: InP Image Analysis Results

## Slide 19: InP Image Analysis Results

## Slide 22: InP Image Analysis Results

## Slide 23: Conclusion
Nearly half of the gratings were under exposed.
No gratings were overexposed
In general cleanest of the gratings had smaller patterns than those in the mask, which is counter to the underlying assumption of the pattern bias design of the DC split. Possible explanations include:
  A programming error
  Thick resist
  Dose is too low to see backscattering effect.

## Slide 24: Next EB Litho Run
Sweeper – ~5 characteristic patterns from first mask with thinner resist over 5-8 doses. 50% DC pattern repeated with different pattern bias
  Total: ~100 gratings
InP & GaAs Grating Coupler – We were happy with the results of the initial calibration. Next will be a dry run of the first mask with different lengths and flip-chip bonding alignment marks.