## Slide 1: Phasor amplifier design
Awfang, hwchen, jbovington, jebowers

## Slide 2: Amplifier Requirements
Gain
  ~ 16 dB based on hui-wen’s Calculations
    Also design for 25 dB
  25 mW (maybe twice this)
  18 dBm saturation power (demonstrate second rev)

## Slide 3: Previously demonstrated
Demonstrated on SEL platform
  1 dB gain, 11 dBm saturation power
Strong saturation at higher current due to poor thermal impedance, and high series resistances.
Gen 2 lasers (same structure) showed improved high current behavior
g = golog(J hi/Jtr)
  go = 972 cm-1
  Epump 1 hi = .4
  Jtr = 310.8

## Slide 4: Structural improvements/Changes
We expect an improvement in current injection.
  hi ~ 70%
  Latest gene
  Also, we have new structures for improved thermal impedance. (30% theoretical Zt improvement)
Confinement factor will be increased from 3.4% to 8.2%

## Slide 5: Amplifier Optimization
Assuming:
  hi = 70%
  8.2% confinement factor
Length optimization for minimum power dissipation
  ~500 micron for 16 dB on chip gain
  ~ 840 micron for 25 dB