## Slide 1: WGUTC process flow

## Slide 2: Starting wafer
Si
BOX
Handle wafer
Device layer

## Slide 3: Implant alignment etch
SiO2 mask from Si thinning by wet oxidation - ~1um thick
Mask used for standard Cl/BCl3 ICP etch – alignment marks only in corners of die
Not removed after etch
Si
BOX
Alignment marks
Most areas

## Slide 4: N++ implant
SiO2 mask from Si thinning by wet oxidation - ~1um thick
Si
BOX
Alignment marks
Device areas
PD layout – top view
N++

## Slide 5: N implant
New PECVD SiO2 mask
Followed by:
Strip SiO2, clean, dep 50nm SiO2, 5’ RTA at 900C in graphite susceptor
Then Ge growth
Si
BOX
Alignment marks
Device areas
PD layout – top view
N++
N

## Slide 6: Material after growth
Si
BOX
Ge
Device area
Elsewhere
Doped Si
PD layout – top view
N++
N

## Slide 7: P-metal
Single layer liftoff
Si
BOX
Ge
Device area
Elsewhere
PD layout – top view

## Slide 8: Waveguide etch
WG etch (SF6/O2 in ICP1 with Cr/SiO2 hardmask)
Etch 300nm into Si
Final WG dimensions achieved using this process have already been verified
Si
BOX
Device area
WG
PD layout – top view
Optical input

## Slide 9: Deep etch
Deep etch (self-aligned to previous step - similar to what Hui-Wen used to do)
Without this step, minimum bend radius becomes huge, MMI design becomes difficult
Si
BOX
Device area
WG
PD layout – top view
No change in PD area

## Slide 10: Mesa wet etch
I have an OK wet etch for this (heated H2O2), would like a faster one
I have qualified the undercut for both H2O2 and dilute SC1 etches, it’s ~700nm for an 800nm deep etch – this is OK for me (only undercuts from the input, not from the side or back)
Si
BOX
Device area
WG
PD layout – top view

## Slide 11: Passivation dep/via etch
500nm to protect waveguides and passivate PD sidewalls, via etch to open n-contacts
Si
BOX
Device area
WG
PD layout – top view
3 rectangles: 2n, 1p

## Slide 12: Heater metal dep
Only shown on this slide
Si
BOX
Device area
WG
PD layout – top view
No change in PD area

## Slide 13: N-metal
Thick (~700nm) (want to level with p-metal)
Forms ground plane for microstrip lines
Si
BOX
Device area
WG
PD layout – top view

## Slide 14: Cap deposition
Liftoff process in ALD/Ebeam for dielectric/metal
Shown on this slide only
MIS caps – preferred due to lower surface roughness on semiconductor – but raises difficulties with contacting
  If cap shorts, it is not so bad – it just means I have to bias PDs in coherent receiver at -2V
Via is “large” because it goes past the edge of the p-metal by 2.5um (whereas it is typically the same size as the p-metal)
Si
BOX
Cap area
P-metal
N-metal
Large* via

## Slide 15: Post dep
Post dep (~3um tall x 2um wide, 1um minimum spacing)
Design rules from Rodwell group – probably fine
Posts on n-type material are far from PD
Si
BOX
Device area
WG
PD layout – top view
Posts
here
Posts
here
Posts
here

## Slide 16: BCB/planarization
2.5um final height (measured from top of n-metal)
  Given post height and spun BCB height, this may take two coats
Preceded by sticking layer deposition (blanket)
Si
BOX
Device area
WG

## Slide 17: Probe metal
Preceded by blanket sticking layer deposition and etching (both) sticking layer(s) around posts
Si
BOX
Device area
WG
PD layout – top view

## Slide 18: Final cross-sections
WG
WG w/ heater
Si
PD

## Slide 19: Final cross-sections
Si
capacitor
Probe pad (signal)
(slightly different for coherent receivers due to wirebonding-related concerns)
Probe pad (ground)
Transmission line
Ge
Si

## Slide 20: Total mask layers (lithographies)
Implant alignment
N++ implant
N implant
- Ge growth -
P-metal
Trench
Deep Si etch
Mesa
Heater metal
Via etch (to n-contacts and p-contact metal)
N-metal
Capacitor (incl. top metal)
Post dep
BCB (not actually a lithography)
(re-do post litho for etch)
Probe metal
11 layers, probably 12-14 lithographies total (may need to do mesa and capacitor twice)
Only P-metal, trench, via, and post lithographies need good alignment, everything else is +/- at least 1um