## Slide 1: DUV Stepper Waveguides Si Dummy Run
Jock Bovington
&
Jared Hulme

## Slide 2: Overview
Design of Experiment
Device Layout
SEM Results
Conclusions

## Slide 3: Design of Experiment
Jock Bovington

## Slide 4: Design of Experiment
Using (3) Si wafer (NOT SOI)
  Split DBARC bake temperature (160,170,180C)
  Split dose energy (16,17,18…31mJ/cm2)
  Hold focus (-0.15um)
  Etch 250s
Run (1) SOI wafer given the results

## Slide 5: Process Follower
Clean Wafers
  Nano Strip, DI rinse, BHF, Di rinse, SRD
Dehydration bake (132C, >1min)
Spin DBARC (5krpm, 30s)
Hot plate bake temp = XC, 60s
Spin UV210 (5krpm, 30s)
Soft bake temp = 132C, 60s
DUV stepper exposure (YmJ/cm2, -0.15m)
Post exposure bake (132C, 90s)
Develop 300MIF (120s, minimal agitation)
PEII O2 Descum (100W, 300mT, 30s)
Si Deep RIE “Bosch” single step etch BOV_J_01 (250s, ~250nm)
Dektak step height
Gasonics Strip (recipe #7, 120s, 1-3 repeats)
Dektak step height
SEM

## Slide 6: Device Layout
Jared Hulme

## Slide 7: Device Layout – Dose Energy
26 | 27 | 28 | 29 | 30
25 | 24 | 23 | 22 | 21
16 | 17 | 18 | 19 | 20

## Slide 8: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 9: SEM Results
Jared Hulme

## Slide 10: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
.15um
.3um
12um
2.55um
.15um

## Slide 11: SEMs – 160C Bake time
Die 26
Die 27
Die 28
Die 29

## Slide 12: SEMs – 170C Bake time
Die 24
Die 25
Die 28

## Slide 13: SEMs – 180C Bake time
Die 25
Die 26
Die 27
Die 28

## Slide 14: SEMs – 180C Bake time
Die 29

## Slide 15: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
12um
3um
1.425um
.15um
.15um
.15um

## Slide 16: SEMs – 160C Bake time
Die 26
Die 27
Die 28
Die 29

## Slide 17: SEMs – 170C Bake time
Die 24
Die 25
Die 26

## Slide 18: SEMs – 180C Bake time
Die 25
Die 26
Die 27
Die 28

## Slide 19: SEMs – 180C Bake time
Die 29

## Slide 20: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
.6um
.6um
.28um

## Slide 21: SEMs – 160C Bake time
Die 26
Die 27
Die 28
Die 29

## Slide 22: SEMs – 170C Bake time
Die 24
Die 25
Die 26
Die 27

## Slide 23: SEMs – 180C Bake time
Die 25
Die 26
Die 27
Die 28

## Slide 24: SEMs – 180C Bake time
Die 29a
Die 29b

## Slide 25: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 26: SEMs – 160C Bake time
Die 26
Die 27
Die 28
Die 29

## Slide 27: SEMs – 170C Bake time
Die 24
Die 25
Die 26

## Slide 28: SEMs – 170C Bake time
Die 27a
Die 27b

## Slide 29: SEMs – 180C Bake time
Die 25
Die 26
Die 27
Die 28

## Slide 30: SEMs – 180C Bake time
Die 29

## Slide 31: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 32: SEMs – 160C Bake time
Die 26
Die 27
Die 28
Die 29

## Slide 33: SEMs – 170C Bake time
Die 24a
Die 24b
Die 25

## Slide 34: SEMs – 180C Bake time
Die 25
Die 26
Die 27
Die 28

## Slide 35: SEMs – 180C Bake time
Die 29

## Slide 36: Conclusions
Jared Hulme & Jock Bovington

## Slide 37: Si Litho Conclusions – Bad News
It appears that at low DBARC bake temp (160C) there is often severe undercut during development which destroys fine features.
For gratings and narrow gaps high DBARC bake temp (180C) leaves webbing which partially masks these area.
All wafers have residue that was not removed after 3x Recipe#7 in Gasonics.
  Follow-up Experiment
    (1) 30min Piranha 100C
    (1) 30min Nanostrip Dip
    (1) HOLD most dissimilar wafer
    SEM both cleaned wafers

## Slide 38: Si Litho Conclusions – Good News
DUV Stepper SOI should be set around
  25mJ/cm^2
  170C DBARC Bake Temp
Run (1) SOI wafer with Focus/Energy array to measure offsets for all patterns
  Energy: 23, 24, 25, 26, 27
  Focus: -0.35, -.25, -0.15, -0.05, 0.05

## Slide 39: DUV Stepper Waveguides SOI Test Run
Jock Bovington
&
Jared Hulme

## Slide 40: Overview
Design of Experiment
Device Layout
SEM Results
Conclusions

## Slide 41: Design of Experiment
Jock Bovington

## Slide 42: Design of Experiment
Using (3) Si wafer (NOT SOI)
  Split DBARC bake temperature (160,170,180C)
  Split dose energy (16,17,18…31mJ/cm2)
  Hold focus (-0.15um)
  Etch 250s
Run (1) SOI wafer given the results

## Slide 43: Process Follower
Clean Wafers
  Nano Strip, DI rinse, BHF, Di rinse, SRD
Dehydration bake (132C, >1min)
Spin DBARC (5krpm, 30s)
Hot plate bake temp = XC, 60s
Spin UV210 (5krpm, 30s)
Soft bake temp = 132C, 60s
DUV stepper exposure (YmJ/cm2, -0.15m)
Post exposure bake (132C, 90s)
Develop 300MIF (120s, minimal agitation)
PEII O2 Descum (100W, 300mT, 30s)
Si Deep RIE “Bosch” single step etch BOV_J_01 (250s, ~250nm)
Dektak step height
Gasonics Strip (recipe #7, 120s, 1-3 repeats)
Dektak step height
SEM

## Slide 44: Device Layout
Jared Hulme

## Slide 45: Device Layout – Dose Energy
 | 23 | 24 | 25 | 26 | 27
-.35 |  |  |  |  | 
-.25 |  |  |  |  | 
-.15 |  |  |  |  | 
-.05 |  |  |  |  | 
0.5 |  |  |  |  | 

## Slide 46: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 47: SEM Results
Jared Hulme

## Slide 48: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
.15um
.3um
12um
2.55um
.15um

## Slide 49: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
12um
3um
1.425um
.15um
.15um
.15um

## Slide 50: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips
.6um
.6um
.28um

## Slide 51: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 52: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 53: Conclusions
Jared Hulme & Jock Bovington

## Slide 54: SOI Test Conclusions – Bad News

## Slide 55: SOI Conclusions – Good News