## Slide 1: Sweeper Processing Issues
March, 2012

## Slide 2: Post Anneal Observations

## Slide 3: Sweeper Chip E Post 1050C Anneal
Nomarski Image of Dope area
Same area normal view
Hard to see Dope windows after 1050C anneal but faint outline can be seen under Nomarski.

## Slide 4: Sweeper Chip E Post 1050C Anneal
Eight large particles seen post anneal. An ISO soak with U/S at 5/5/High for 3 min and DI for 2 min was used to remove them.

## Slide 5: Sweeper Chip E Post 1050C Anneal
Nomarski view. Streaks extend to edge of wafer in all cases. Seen in differenct densities but similar to this in five spots around circumference of the chip. Not sure if present preanneal
Same image under normal view, streaks not noticed.

## Slide 6: Stripping Issues at Post SiN Hardmask Etch
13.2. SiN deposition |  |  |  |  |  | 
13.2.1. Dehydration bake 5 min @ 150 C |  |  |  |  |  | 
13.2.2. Deposit 3000A of SiN |  |  |  |  |  | 
13.3. Mesa litho (Mesa Def mask) |  |  |  |  |  | 
13.3.1. Sample prep |  |  |  |  |  | 
13.3.1.1. Acetone 3 min / Isopropyl alcohol (IPA) 3 min / DI rinse 3 min |  |  |  |  |  | 
13.3.1.2. Dry with N2, dehydration bake 3 min 120 C |  |  |  |  |  | 
13.3.1.3. PE2 O2 descum 300 mT, 100 W, 1 min |  |  |  |  |  | 
13.3.1.4. Dehydration bake 5 min, 150 C |  |  |  |  |  | 
13.3.2. Spin resist |  |  |  |  |  | 
13.3.2.1. Blow sample with N2 |  |  |  |  |  | 
13.3.2.2. Dispense HMDS, 30 sec @ 3K |  |  |  |  |  | 
13.3.2.3. Blow sample with N2 |  |  |  |  |  | 
13.3.2.4. Dispense nLOF 5510, 30 sec @ 3K |  |  |  |  |  | 
13.3.2.5. Soft bake 1 min, 90 C |  |  |  |  |  | 
13.3.3. Expose in stepper 0.25 sec, offset: -1 |  |  |  |  |  | 
13.3.4. Post bake 1 min, 110 C |  |  |  |  |  | 
13.3.5. Develop AZ300MIF, 1 min |  |  |  |  |  | 
13.3.6. Inspect: If bent tapers -> try a longer descum in next step to etch some of PR. |  |  |  |  |  | 
13.3.7. PE2 O2 descum 300 mT, 100 W, 1 min |  |  |  |  |  | 

## Slide 7: Test Piece
Residue on SiN
Wispy blobs

## Slide 8: Chip C1
Large Resist blobs
Resist

## Slide 9: Chip A2 Left Die
Pits all over, mostly on left die

## Slide 10: Other Projects Mesa Process
2010_04_28 Slotline
  Positive resist 955 0.9, RIE 3 etch, Developer strip but not very effective
2008_10_03 Self Align Process
  Positive resist 955 0.9, RIE 3 etch, 1165 Strip but still residue