## Slide 1: DUV positive/negative PR metal liftoff

## Slide 2: Recipe – Negative PR
DBARC
  5k, 30 s
  170C, 60 s
UVN 2300-0.5 (this recipe comes from UVN 30-0.5 spec sheet)
  3k, 30 s (550 nm thick)
  110 C, 60 s
  Expose (~25 mJ/cm2, -0.15 focus, NA=0.63, annular σ=0.4/0.8)
  105 C, 60 s
  AZ300MIF, 60 s
Descum
  30 s, 100 W
Metal dep (E-Beam 1)
  100 nm, 1 Å/s with occasional spike at 2 Å/s
Liftoff
  1165, 30 min, sonication

## Slide 3: SEMs

## Slide 4: Recipe – Positive PR
DBARC
  5k, 30 s
  170C, 60 s
UV 210-0.3
  1k, 30 s (~500 nm according to spec sheet)
  135 C, 60 s
  Expose (~25 mJ/cm2, -0.15 focus, NA=0.63, annular σ=0.4/0.8)
  135 C, 90 s
  AZ300MIF, 45 s
Descum
  15 s, 100 W
Metal dep (E-Beam 3)
  20/80 nm (Ti/Au)
Liftoff
  1165, 30 min, sonication

## Slide 5: Optical microscope