## Slide 1: DUV Stepper Waveguides
Jock Bovington
&
Jared Hulme

## Slide 2: Overview
Design of Experiment
Device Layout
SEM Results
Conclusions

## Slide 3: Design of Experiment
Jock Bovington

## Slide 4: Design of Experiment
Using 3 Si wafer (NOT SOI)
  Split DBARC bake temperature (160,170,180C)
  Split dose energy (16,17,18…31mJ/cm2)
  Hold focus (-0.15um)
  Etch 250s

## Slide 5: Process Follower
Clean Wafers
  Nano Strip, DI rinse, BHF, Di rinse, SRD
Dehydration bake (132C, >1min)
Spin DBARC (5krpm, 30s)
Hot plate bake temp = XC, 60s
Spin UV210 (5krpm, 30s)
Soft bake temp = 132C, 60s
DUV stepper exposure (YmJ/cm2, -0.15m)
Post exposure bake (132C, 90s)
Develop 300MIF (120s, minimal agitation)
PEII O2 Descum (100W, 300mT, 30s)
Si Deep RIE “Bosch” single step etch BOV_J_01 (250s, ~250nm)
Dektak step height
Gasonics Strip (recipe #7, 120s, 1-3 repeats)
Dektak step height
SEM

## Slide 6: Device Layout
Jared Hulme

## Slide 7: Device Layout – Dose Energy
26 | 27 | 28 | 29 | 30
25 | 24 | 23 | 22 | 21
16 | 17 | 18 | 19 | 20

## Slide 8: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 9: SEM Results
Jared Hulme

## Slide 10: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 11: SEMs

## Slide 12: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 13: Vertical Gratings
.15um
.3um
12um
2.55um

## Slide 14: SEMs – 160C Bake time
Die 21
Die 22
Die 23
Die 24

## Slide 15: SEMs – 160C Bake time
PR for Vertical gratings can peel away easily.

## Slide 16: Horizontal Gratings
12um
3um
1.425um
.15um

## Slide 17: SEMs – 160C Bake time
Die 21
Die 22
Die 23
Die 24

## Slide 18: SEMs – 160C Bake time
Die 21
Die 22
Die 23
Die 24

## Slide 19: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 20: SEMs

## Slide 21: Pattern Layout
PTPNSL-EPhi1.2_DUV2.gds
EPhi 1.2 points of interest
  Coupler gaps
  300nm period gratings
  Star Coupler points
  Taper Tips

## Slide 22: SEMs

## Slide 23: Conclusions
Jared Hulme & Jock Bovington

## Slide 24: Conclusions