## Slide 1
Trying to get feature sizes smaller than a fraction 0.5 to 1 of the resist thickness is challenging. 0.9um resist  0.5um is the limit.
SPR955

## Slide 3
Accuracy – Sputter(~5nm)>PECVD(10-15nm)>Thermal- dry(10-20nm).

## Slide 4
CEM - Sputter

## Slide 5
CEM - Thermal

## Slide 6
SPR - Sputter

## Slide 7
SPR - Thermal

## Slide 8
CEM
SPR
Resist profile
Oxide profile
Silicon profile
w
w
w + 200nm
w’
w’ + 150nm
w’
w’ + 180nm
w’’
w’’ + 110 +/- 10 nm
w’’ + 110 +/- 10 nm
w’’
35 +/- 10 nm
Marginally better sidewalls for CEM – comparing slides 4&7
248 +/- 5 nm