## Slide 1: Grating Analysis Update 2011-03-01
Jock Bovington
with assistance from
Wenzao Li

## Slide 2: Outline
Grating Fabrication
  PULSAR Gratings
  SWEEPER Gratings
Grating SEM Gallery
Image Processing Tool*
  Attainment of nm resolution measurement accuracy for understanding dose and proximity effects
  Applications in fully controlled apodization of kappa with duty cycle…and later other parameters
*Thanks to Wenzao for building this tool with me

## Slide 3: Experiment design with Process flow
Two initial device samples were run
  PULSAR (GaAs) Epi with IBD SiO2 (55nm)
    11nm Au Thermal Evaporated
    Developed
    ICP #2 (Oxide Etch)
    AFM
    ICP #1 (GaAs Etch)
    AFM
    SEM
  Sweeper SOI (500nm Si, 1um BOx)
    2 patterned die, 2 unpatterned
    11nm Au Thermal Evaporated
    Developed
    AFM (~393+/-7nm)
    Deep Si RIE “Bosch” (Si Etch) - Thanks Jason
    AFM
    SEM

## Slide 4: Grating Analysis

## Slide 5: PULSAR AFM Analysis
with ~55nm SiO2 Hardmask

## Slide 6: Sweeper AFM Analysis
Final etch height (no hard mask)

## Slide 7: SEM Analysis
Top down SEM is an excellent way to gain understanding about gratings.
  Dose
  Proximity Effects
  Duty cycle
  Qualitative information about pattern distortion

## Slide 8: Understanding the grating

## Slide 9: Edge Detection Program

## Slide 10: InP Image Analysis Results

## Slide 11: PULSAR Grating SEMs

## Slide 12: Sweeper Grating SEMs

## Slide 13: Sweeper Grating SEMs

## Slide 14: Conclusions
Honed in on the best Ebeam writing conditions for large pitch gratings ~500-700nm
Characterized etches for these gratings for:
  GaAs
  Si/SOI
  InP (Working on a polymerization issue with the MHA etch, next will try GaSonics. Pietro, Sweeper has a solution with the RIE#2)
Grating Development To-Do-List:
  Cross section POR gratings to fully qualify etches
  Characterize etch rate v. pattern size