## Slide 1: Isolator update
Jason Tien
3/1/2011

## Slide 2: Device Structure
B
Ce:YIG
Top view
Input
(a)
(b)
Magnet
SGGG sub.
Ce:YIG (0.5μm)
1.6mm
0.4 mm
Silicon waveguides
Magnetic field flux from a cylinder magnet

## Slide 3: 295 nm thick Si layer
TE
ng=3.85
YIG
BOX
GGG
ng=3.88
TM
WG: 600 nm x 295 nm
Intensity distribution
ng=4.68
TM
TE
ng=3.97
Air
BOX

## Slide 4: 295 nm thick Si layer
WG: 600 nm x 295 nm
TM mode Hx field
YIG
GGG

## Slide 5: NRPS calculation
Si waveguide thickness: 300 nm
Ce:YIG thickness: 500 nm
BOX
Ce:YIG
SGGG
Si
Air
Air
Hx field profile for 600 nm x 300 nm waveguide

## Slide 6: NRPS calculation
Si thickness: 200nm
Narrower waveguides confine less power at the Si-garnet interface

## Slide 7: NRPS calculation
Si thickness: 300nm
Narrower waveguides have larger filed intensity in Si-garnet interface

## Slide 8: Design plot for coupling gap
900um ring to straight waveguide coupling design
295 nm thick SOI

## Slide 9
FSR (TM) ~ 84pm (ng~5)

## Slide 10: Tunable magnetic optical filter
Ring radius: 900um
Coupling gap: 192nm
Extinction ratio: 9 dB
TM mode

## Slide 11: Ring isolator
Ring radius: 900um
Waveguide dimension: 600 nm x 300 nm
Ce:YIG: 0.5um
Isolation ratio ~ 9dB
TM mode
Magnetic field intensity ~ 200 Gauss
Near field IR image

## Slide 12: Summary
Resonance wavelength is tunable by applying different magnitudes of magnetic fields
Inward and outward radial magnetic fields show different resonance wavelengths with half of FSR of shift.
9dB of isolation with TM input
Better isolation can be achieved in critical coupling region.
Smaller ring isolator can be realized with a smaller permanent magnet or micro-electromagnet.
Drop port isolation, circulators…