## Slide 1: SOA EPI Design
Yongbo
12/16/2011

## Slide 2: III/V epi design
 |  | revised design (0711281-9) |  | Note
(No.) | Material | Height | Doping (cm-3) | 
0 | n-InP substrate | 350 um | Up to grower | 
1 | u-InP buffer | 0.5 um | - | Landmark suggestion
2 | p-InGaAs | 30 nm | Up to grower | etching stop layer
3 | p-InP | 20 nm | Up to grower | InGaAs protection layer (Too thick affects implantation uniformity due to the undercut)
4 | p-InGaAs | 0.2 um | >1E19 | for etch-back tolerance (p-contact)
5 | p-InP | 1.5 um | 1E18 | 1.0 um - 0.3 um - 0.2 um with decreasing doping levels? To be decided (waiting for Landmark’s standard epi)
6 |  |  |  | 
7 |  |  |  | 
8 | p-InAlGaAs | 125 nm | 1E17 | Current SOA EPI (waiting for Landmark’s standard epi)
9 | u- 8x InAlGaAs (+0.85%) u- 9x InAlGaAs (-0.55%) | 7 nm / 10 nm (1545 nm) | nid | 
10 | n-InAlGaAs | 125 nm | 1E17 | 
11 | n-InP | 0.11 um | 1E18 | Standard Design
12 | 2x n-InGaAsP / 2x n-InP | 7.5 nm / 7.5 nm | 1E18 | 
13 | n-InP | 10 nm | 1E18 | 
14 | n-InGaAs | 0.2 um | 1E18 | 

## Slide 3: Electron Blocking layer
EBL after the well rather than the barrier
  Confine the electron in the well rather than the barrier region
EBL improves confinement of the electron
  better high temperature performance
  Lower threshold
  Improved quantum efficiency (sharp slope)

## Slide 4: Etch Stop layer/Current channel
Add an etch stop layer above upper SCH
Under-cut to define the current channel
  No proton implantation for lasers/no harm to the active region
  Smaller differential resistance/tolerance for via opening
  Thin layer will not affect the optical mode (TE) too much
  It always reduces the capacitance of the modulator using undercut.
  Current non-uniformity (need simulation)
  How thin it could be for under-cut
  One more step but compatible if we add etch stop layer
  Repeatability using wet etching
  Slightly direction-dependent but it could be OK
What kind of material?
InP/InGaAsP/InP?
What kind of Etchant?
H2SO4 : H2O2 : H2O?

## Slide 5
Backup: current EPI design

## Slide 6: One version of Landmark’s EPI (1550)
200μm
700μm
FP Lasers’ performance
From Zheng’s thesis
ASE’s peak @~1540.6nm, red-shift with pump current increased

## Slide 7: Andy’s EPI (1310)

## Slide 8: AW Fang(1550)

## Slide 9: Phaser EPI (1550)
SCH: 1.3um 125nm/p-1e17
Well: InAlGaAs 8x 7nm +0.85%
Barrier: InAlGaAs 9x 10nm -0.55%
SCH: 1.3um 125nm/n-1e17