## Slide 1: Mesa Sidewall Profile
June 14, 2011

## Slide 2: Mesa Lithography
Chip 1 Photoresist on SiN/Au
Chip 3 Photoresist on SiN
No image of Chip 2 Photoresist on SiN

## Slide 3: Mesa Post SiN Etch Post First 1165 Strip
Chip 1 RIE SiN on Au
Chip 2 RIE SiN on InP
Chip 3 ICP SiN on Au

## Slide 4: Mesa Post InP Etch
Chip 1 RIE SiN on Au
Chip 2 RIE SiN on InP
Chip 3 ICP SiN on InP
Angled area rougher than straight areas. Chip 2 also has incomplete RIE 3 resist strip causing masking

## Slide 5: Mesa Post InP Etch
Chip 1 RIE SiN on Au
Chip 2 RIE SiN on InP
Chip 3 ICP SiN on InP

## Slide 6: Mesa Post SiN Etch Post First 1165 Strip
Chip 1 RIE SiN on Au
Chip 2 RIE SiN on InP
Chip 3 ICP SiN on Au

## Slide 7: Observation and Notes
RIE 3 Etch Time (CF4/02) is 17 minutes for InP pieces. Etch rate for 10 minutes is 210-240nm on Test Silicon piece
ICP 2 Etch time (CHF3) is 1 min 11 seconds for the InP piece. Etch for 45 seconds is 240-250nm for Test Silicon piece
Post SiN etch was done for 15 min soaked in 1165 stripper. Pieces were horizontal and stripper container was in 80C water bath.
Resist residue on top of SIN and on sides typical after one soak in 1165. Usually a light swab with additional soak is needed to remove standard RIE dry etch of SiN and may need to be repeated with plasma. Residue is still often present after additional 1165 soaks, Plasma, and swabbing. A 5-10 sec DI:HCL 1:10 dip will often remove the residue. Both RIE etches have much more residue than the ICP which looked relatively clean.
SEM images were difficult to image due to charging and angle
RIE 2 etch time was set to 35 min which caused the etch depth to be 2X more than target. Target is 1.5 um. Dektak depths measured are 3.2 to 3.6 um.

## Slide 8: Additional Images Taken
See following slides

## Slide 9: Chip 1 Photoresist on SiN/Au

## Slide 10: Chip 3 Photoresist on SiN

## Slide 11: Chip 1 RIE SiN Etch Post Strip on SiN/Au

## Slide 12: Chip 2 RIE SiN Etch Post Strip

## Slide 13: Chip 3 ICP SiN Etch Post Strip

## Slide 14: Chip 1 RIE SiN-Au Mesa Post InP Etch

## Slide 15: Chip 1 RIE SiN-Au Mesa Post InP Etch

## Slide 16: Chip 1 RIE SiN-Au Mesa Post InP Etch

## Slide 17: Chip 2 RIE SiN Mesa Post InP Etch

## Slide 18: Chip 2 RIE SiN Mesa Post InP Etch

## Slide 19: Chip 2 RIE SiN Mesa Post InP Etch

## Slide 20: Chip 2 RIE SiN Mesa Post InP Etch

## Slide 21: Chip 3 ICP SiN Mesa Post InP Etch

## Slide 22: Chip 3 ICP SiN Mesa Post InP Etch

## Slide 23: Chip 3 ICP SiN Mesa Post InP Etch

## Slide 24: Chip 3 ICP SiN Mesa Post InP Etch

## Slide 25: Chip 1 RIE SiN Etch Post Strip on SiN/Au

## Slide 26: Chip 2 RIE SiN Etch Post Strip

## Slide 27: Chip 3 ICP SiN Etch Post Strip
InP appears golden in color but actually grayish like Chip 2.