## Slide 2
c)
f1
f2
f3
f4
fc
a)
SOA1
SOA2
SOA3
SOA4
f1
f2
f3
f4
fc
AWG
b)

## Slide 5
Chart: Wavelength [nm]
9 dB
3.5 dB

## Slide 6
2125 A/cm^2
(FP data)

## Slide 8
35 dB

## Slide 9
Chart: Current [mA]
| 101.2 | 103.4 | 105.6 | 107.80000000000001 | 110 | 112.19999999999999 | 114.4 | 116.6 | 118.8 | 121 | 123.2 | 125.4 | 127.6 | 129.80000000000001 | 132 | 134.20000000000002 | 136.4 | 138.6 | 140.80000000000001 | 143 | 145.19999999999999 | 147.4 | 149.60000000000002 | 151.79999999999998 | 154 | 156.20000000000002 | 158.4 | 160.6 | 162.80000000000001 | 165 | 167.2 | 169.4 | 171.6 | 173.8 | 176 | 178.2 | 180.4 | 182.60000000000002 | 184.79999999999998 | 187 | 189.20000000000002 | 191.4 | 193.6 | 195.8 | 198 | 200.2 | 202.4 | 204.6 | 206.8 | 209 | 211.2 | 213.4 | 215.60000000000002 | 217.79999999999998 | 220
Ch. 3 | 0.10819 | 0.12939 | 0.15485 | 0.18678 | 0.23189 | 0.30947 | 0.6725 | 1.4466 | 2.3552 | 3.2085 | 4.0064 | 5.8624 | 7.1351 | 7.8334 | 9.1576 | 10.244 | 9.8234 | 10.3819 | 10.7941 | 10.8977 | 11.6221 | 12.1819 | 13.0424 | 15.6909 | 17.4924 | 18.1465 | 18.9485 | 19.1767 | 19.1407 | 20.2865 | 20.0653 | 20.7358 | 18.7222 | 18.6949 | 19.5676 | 21.5173 | 23.579 | 23.9851 | 24.261 | 24.384 | 25.041 | 24.8994 | 24.7752 | 24.6289 | 24.6759 | 23.2033 | 23.1685 | 26.0763 | 26.1674 | 26.8487 | 26.1201 | 26.0924 | 26.3393 | 26.2096 | 25.6966
b)
a)

## Slide 10
500 ps
a.u.

## Slide 11
a)
b)
N-InP
N-contact
Si
Si
Si
SiO2
SiO2
QW
SCH
P-contact
SCH
Si
P-InP
SU-8

## Slide 12
7.7 dB
a.u.
200 ps

## Slide 13
HR
MMI
SOA
Mod
MMI
SOA
Mod
AWG
…
AR

## Slide 14
Layer | Material | Doping | Thickness
Substrate | InP | S-Doped | 350 μm
Buffer | InP | Undoped | 200 nm
Contact | In0.53Ga0.47As | P – 1E19 | 100 nm
Cladding | InP | P – 1E 18 | 1.5 μm
SCH | AlGaInAs | P – 1E17 | 125 nm
QW | AlGaInAs (well) (8x) AlGaInAs (barrier) (9x) | Undoped | 7 nm 8 nm
SCH | AlGaInAs | N – 1E17 | 125 nm
Contact | InP | N – 1E18 | 110 nm
Superlattice | In0.85Ga0.15As0.327P0.773 (2x) InP (2x) | N – 1E18 N – 1E18 | 7.5 nm 7.5 nm
Bonding | InP | N – 1E18 | 10 nm
Cap | In0.53Ga0.47As | N – 1E18 | 200 nm

## Slide 15
Layer | Material | Thickness
Contact | In0.53Ga0.47As | 100 nm
Cladding | InP | 1.5 μm
SCH | Al0.131Ga0.34In0.528As | 125 nm
Quantum wells/barriers | Al0.089Ga0.461In0.45As (well) (8x) Al0.055Ga0.292In0.653As (barrier) (9x) | 7 nm 8 nm
SCH | Al0.131Ga0.34In0.528As | 125 nm
Contact | InP | 110 nm
Superlattice | In0.85Ga0.15As0.327P0.773 (2x) InP (2x) | 7.5 nm 7.5 nm
Bonding | InP | 10 nm
Waveguide | Si | 700 nm
Buried Oxide | SiO2 | 1 μm
Substrate | Si | 600 μm