## Slide 1: Sweeper Processing Issues
March, 2012

## Slide 2: Post Anneal Observations

## Slide 3: Sweeper Chip E Post 1050C Anneal
Nomarski Image of Dope area
Same area normal view
Hard to see Dope windows after 1050C anneal but faint outline can be seen under Nomarski.

## Slide 4: Sweeper Chip E Post 1050C Anneal
Eight large particles seen post anneal. An ISO soak with U/S at 5/5/High for 3 min and DI for 2 min was used to remove them.

## Slide 5: Sweeper Chip E Post 1050C Anneal
Nomarski view. Streaks extend to edge of wafer in all cases. Seen in differenct densities but similar to this in five spots around circumference of the chip. Not sure if present preanneal
Same image under normal view, streaks not noticed.

## Slide 6: Stripping Issues at Post SiN Hardmask Etch
13.2. SiN deposition |  |  |  |  |  | 
13.2.1. Dehydration bake 5 min @ 150 C |  |  |  |  |  | 
13.2.2. Deposit 3000A of SiN |  |  |  |  |  | 
13.3. Mesa litho (Mesa Def mask) |  |  |  |  |  | 
13.3.1. Sample prep |  |  |  |  |  | 
13.3.1.1. Acetone 3 min / Isopropyl alcohol (IPA) 3 min / DI rinse 3 min |  |  |  |  |  | 
13.3.1.2. Dry with N2, dehydration bake 3 min 120 C |  |  |  |  |  | 
13.3.1.3. PE2 O2 descum 300 mT, 100 W, 1 min |  |  |  |  |  | 
13.3.1.4. Dehydration bake 5 min, 150 C |  |  |  |  |  | 
13.3.2. Spin resist |  |  |  |  |  | 
13.3.2.1. Blow sample with N2 |  |  |  |  |  | 
13.3.2.2. Dispense HMDS, 30 sec @ 3K |  |  |  |  |  | 
13.3.2.3. Blow sample with N2 |  |  |  |  |  | 
13.3.2.4. Dispense nLOF 5510, 30 sec @ 3K |  |  |  |  |  | 
13.3.2.5. Soft bake 1 min, 90 C |  |  |  |  |  | 
13.3.3. Expose in stepper 0.25 sec, offset: -1 |  |  |  |  |  | 
13.3.4. Post bake 1 min, 110 C |  |  |  |  |  | 
13.3.5. Develop AZ300MIF, 1 min |  |  |  |  |  | 
13.3.6. Inspect: If bent tapers -> try a longer descum in next step to etch some of PR. |  |  |  |  |  | 
13.3.7. PE2 O2 descum 300 mT, 100 W, 1 min |  |  |  |  |  | 

## Slide 7: Test Piece
Residue on SiN
Wispy blobs

## Slide 8: Chip C1
Large Resist blobs
Resist

## Slide 9: Chip A2 Left Die
Pits all over, mostly on left die

## Slide 10: Other Projects Mesa Process
2010_04_28 Slotline
  Positive resist 955 0.9, RIE 3 etch, Developer strip but not very effective
2008_10_03 Self Align Process
  Positive resist 955 0.9, RIE 3 etch, 1165 Strip but still residue

## Slide 11: Mesa Etch Strip Issues
September 22, 2011

## Slide 12: Process
Two Bonded Chips
  Chips 1 and 2
    Mesa Metal Pd/Ti/Pd/Au EBeam 3
    300nm SiN PE-CVD
    Mesa Lithography (Positive Resist 1.8um)
    Plasma (PE-II) 30 sec 100W
    Chip 1 Only
    RIE2 SiN Etch CF4/O2, 20 sccm/1.8 sccm, 10 mT, 250 V, 17 minutes
    RIE 2 O2 clean 20 sccm, 10mT, 250V, 5 minutes
    Chip 2 Only
    ICP2 SiN Etch CHF3 , 40 sccm, 0.5 Pa, SRC Forward 900W, Bias 200W, 1 minute 12 seconds
    Plasma (PE-II) 2 minutes 100W
    Chips 1 and 2 Strip
    Solvent soak 1165 at 80C
    Plasma 2 min at 200W PE-II. Improvement seen on ICP Chip but still residue left.
    Acetone, ISO, and DI. No improvement seen.

## Slide 13: RIE2 17 min CF4/O2 SiN Etch
Post 2 hour 80C 1165 Strip
Post 2 hour 80C 1165 Strip and 2 min 200W O2 Plasma
Particle on Mask
Post 2 hours 80C 1165 Strip, 2 min 200W O2 Plasma, and Acetone-Iso

## Slide 14: ICP 72 Seconds CF4/O2 SiN Etch
Post 2 hour 80C 1165 Strip
Post 2 hours 80C 1165 Strip and 2 min 200W O2 Plasma
Post 2 hours 80C 1165 Strip, 2 min 200W O2 Plasma, and Acetone-Iso

## Slide 15: Notes
Newer Process (DQPSK, MZM, and EAM) has a different ICP etch recipe and stripping process but there is often resist remaining after the strip in this process flow also.
Developer MF726 Time: ~40 sec
Flood exposure Time: 1 min
O2 descum 300 mT/100W Time: 20 sec
ICP2 SiN PATTERNING
SiN etch #181 GC-SiN O2 : 5 sccm, CF4 : 50sccm Pressure: 2 Pa RF Power: 500 W, Bias:25W Time : 2 min 30 sec
Strip PR in AZ726MIF Time: 1 min
ACE/ISO/DI Clean
O2 descum 300 mT/100W
Other Strip/clean processes:
Light swabbing. This was often used in the past but trying to stay away from this due to possible damage to the taper tips. This would get rid of the bulky heavy resist but some would remain near the sidewalls.
Diluted HCL:DI dip for 10-30 sec. This would often clean up residue but underetching of the Mesa metal would be an issue.
Gasonics: This helps but equipment is down often.
Repeating strip process after plasma (solvent soak, plasma, repeat as necessary)