## Slide 1: Isolator update
Jason Tien
12/13/2010

## Slide 2: Outline
Material properties
  Magnetization
  X-ray diffraction
Experimental measurement of asymmetric MZI isolator
  IR camera image
  Transmission spectra
  Temporal response

## Slide 3: Magnetization of Ce:YIG
Magnetization of Ce:YIG and GGG substrate
Magnetization of Ce:YIG only (subtract GGG contribution)
RT sputtered Ce:YIG (0.2um) on GGG (5mm by 5mm) and 900C 10min RTA
Measured by SQUID at room temperature (in-plane direction)
Ce:YIG thin film saturates at external magnetic field of 10 gauss
Paramagnetic GGG

## Slide 4: Magnetization of Ce:YIG
0.5um Ce:YIG from Mizumoto’s group
0.2um Ce:YIG grown at UCSB
Saturation H-field ~50 Oe
Saturation H-field ~10 Oe
Measured by SQUID at room temperature (in-plane direction)

## Slide 5: X-ray Diffraction of Ce:YIG
XRD resolution: 0.01 deg
Ce:YIG (444)
SGGG (444)
Kα1
Kα2
0.5um Ce:YIG from Mizumoto’s group
0.2um Ce:YIG grown at UCSB

## Slide 6: Transmission spectra of MZI
TL
Lensed fiber
Magnetic field direction
MZI
Power meter
When input wavelength is fixed, the transmitted power difference between positive and negative magnetic field is about 3~5 dBm
Wavelength split (0.1nm) is much smaller than calculated value (0.4nm).
TM
TE

## Slide 7: IR image at MZI output
TL
CCD
polarizer
objective
Lensed fiber
Magnetic field direction
positive magnetic field
Negative magnetic field
No magnetic field
MZI

## Slide 8: Temporal response of MZI
TM
TE
1520.05 nm
25C
Surface magnetic field of electromagnet: 200~300 Gauss at 3A input current
1 sec
Positive magnetic field
Negative magnetic field

## Slide 9: Summary
Asymmetric MZI with bonded Ce:YIG (from Mizumoto) shows nonreciprocal effects
  Smaller wavelength shift than expected
    Could be air gap between the Ce:YIG and Si waveguides assuming the material is no problem
The ring resonators on the same chip doesn’t show any resonance behavior due to offset Ebeam calibration after replacing the filament.
Next
  Recalibrate the gap between the ring and the straight WG
  Bond Ce:YIG onto only one arm of the MZI

## Slide 10: MZI-type Isolator
B field
Comparison is based on the same Faraday coefficient (Δn=1e-4)
ΔL=343um
B field
ΔL=343um
Ce:YIG
Ce:YIG