## Slide 1: AWG
awfang

## Slide 2
Alignment markers.
  Relative to center
  -3800,3800
  3800, 3800
  -3800,-3800
  3800,3800
  Die size = 8100 x 8100.
  Shift into Mask
  x = 4200, 4200
  = -8000, -8000
  = -400, -8000
  = -8000, -400
  = -400, -400

## Slide 3: Two ways to process
1) Keep III-V covered entiredly and then do selective removal during N-layer removal
  Pro
    Simpler Fab
    Do not need to “protect” silicon from SiN etching
  Con
    Any III-V breakage puts Silicon in risk
2) Remove III-V everywhere except “device” region, and protect Silicon
  Pro
    Silicon is protected from the beginning
  Con
    More complicated process.
3) Passivate III-V regions anyways, and remove in the end
  Pro
    Lower risk passivation problems
    Simpler than 2

## Slide 4: Epi Structure
 |  | Doping
P-InGaAs | 100nm | 10^19
P – InP Cladding | 1.5 micron | 10^18
InGaAsP SCH | 120 nm | Top 30 nm – 5 10^17
7 InGaAsP Wells | 6.5 nm well / 8 nm barrier | 
N – InP | 110 | 10^18
InGaAsP/InP SL | 7.5/7.5 2X | 10^18
N –InP bonding Layer | 10 nm | 10^18