## Slide 1: Taper Tip Reduction in the Autostepper Process Development
Jock Bovington

## Slide 2: Outline
Goal: The DUV stepper will not be online until next year at the earliest. Therefore, a <200nm taper tip process must be developed with the Autostepper.
Tried 3 process concepts to reduce taper tip width
  BHF wet etch of SiO2 hardmask
    Dry etch followed by wet etch
    Wet etch only
  Over exposure of P resist mask
  PMGI/SPR bi-layer pattern reduction with DUV flood exposure

## Slide 3: Aside: Hard Mask Choice and Thickness
PlasmaTherm PECVD - SiO2
  If left after etch will not disturb Si3N4 waveguide mode
  Consistent deposition rate
  Isotropic wet etch in BHF (~100nm/min)
  High selectivity with Cl based dry etch of GaAs
    Selectivity to be confirmed in RIE#5
  Thickness could be determined to improve line edge roughness due to standing wave patterns.
    285nm thick mask in i-line(365nm) Autostepper with single PR layer
      t = n* λ /2 (assumes n = 1.56283, check this. Thermal oxide ~1.47454)
    Jon Peter says that the post exposure bake smoothes the PR mask pattern more than the oxide thickness

## Slide 4: BHF wet etch of SiO2 hardmask

## Slide 5: Dry etch plus BHF wet etch of SiO2 hardmask
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
PR
Bond
PECVD Hardmask
Positive Resist
Std. Lithography
HM Dry Etch
BHF Wet Etch
Strip & III-V Dry Etch
BHF HM Removal

## Slide 6: Dry etch plus BHF wet etch of SiO2 hardmask
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
PR
Bond
PECVD Hardmask
Positive Resist
Std. Lithography
HM Dry Etch
BHF Wet Etch
Strip & III-V Dry Etch
BHF HM Removal

## Slide 7: Dry etch plus BHF wet etch of SiO2 hardmask
ACE,ISO,DI,PEII(O2 Plasma)
Deposit oxide hardmask in PlamsaTherm PECVD - 285nm
ACE,ISO,DI,PEII(O2 Plasma)
Dehydration bake 110 1min
Spin HMDS (3krpm, 30sec)
  NOTE: Did not wait after pipetting or bake after spinning
Spin SPR955.9 (3krpm, 30sec)
Pre-exposure bake 95C, 90s
Autostepper Exposure=0.424s, Focus=0
Post exposure bake 125C, 90s
40s Develop in MIF726
O2 plasma 30s 300W 100mT to clean surface
ICP#2 (recipe #104)
  CF4/CHF3/O2 5/40/5sccm, 400/40W ICP/CCP, 6min 40sec
BHF wet etch (varied etch time)
RIE#5 GaAs Etch
  Process abandoned because of poor adhesion of resist
Completed Pending Abandoned

## Slide 8: Adhesion Problems
Following oxide dry etch wrinkles appeared in the PR pattern indicative of poor resist adhesion to the oxide hardmask

## Slide 9: BHF wet etch only of SiO2 hardmask
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
Bond
PECVD Hardmask
Positive Resist
Std. Lithography
BHF Wet Etch
Strip
III-V Dry Etch
BHF HM Removal

## Slide 10: BHF wet etch only of SiO2 hardmask
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
Bond
PECVD Hardmask
Positive Resist
Std. Lithography
BHF Wet Etch
Strip
III-V Dry Etch
BHF HM Removal

## Slide 11: BHF wet etch only of SiO2 hardmask
ACE,ISO,DI,PEII(O2 Plasma)
Deposit oxide hardmask in PlamsaTherm PECVD - 285nm
ACE,ISO,DI,PEII(O2 Plasma)
Dehydration bake 110 1min
Spin HMDS (3krpm, 30sec)
  NOTE: Did not wait after pipetting or bake after spinning
Spin SPR955.9 (3krpm, 30sec)
Pre-exposure bake 95C, 90s
Autostepper Exposure=0.424s, Focus=0
Post exposure bake 125C, 90s
40s Develop in MIF726
O2 plasma 30s 300W 100mT to clean surface
BHF wet etch (varied etch time)
RIE#5 GaAs Etch
  Process abandoned because of poor adhesion of resist
Completed Pending Abandoned

## Slide 12: Accelerated Etching
After 6 minute of BHF wet etching the entire taper tip appears undercut and mesa is half gone. This seems rapidly accelerated given the assumed 225nm/min etch rate of PECVD.

## Slide 13: Adhesion Problems
After 3 minute of BHF wet etching entire structures have lifted off indicative of poor adhesion of the resist even without dry etching. Revisiting the HMDS primer process is recommended for future development, however this result caused me to abandon the wet etch reduction process in search for another process.

## Slide 14: Conclusions BHF wet etch of SiO2 hardmask
Adhesion is the main issue with the current process.
Future processes should investigate longer wait times after pippetting the HMDS and a post spin bake of the HMDS to increase it’s capacity to act as a primer on top of oxide hardmasks.
Primer adhesion optimization is important many steps in the process not just for tapers and will be investigated.

## Slide 15: Over-exposure of positive resist taper pattern

## Slide 16: Over-exposure of positive resist taper pattern
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
Bond
PECVD Hardmask
Positive Resist
Over-exposed Lithography
HM Dry Etch
Strip
III-V Dry Etch
BHF HM Removal

## Slide 17: Over-exposure of positive resist taper pattern
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PR
Epi
HM
Si or SiO2 WG Layer
Si
PR
Bond
PECVD Hardmask
Positive Resist
Over-exposed Lithography
HM Dry Etch
Strip
III-V Dry Etch
BHF HM Removal

## Slide 18: Over-exposure of positive resist taper pattern
ACE,ISO,DI,PEII(O2 Plasma)
Deposit oxide hardmask in PlamsaTherm PECVD – 200nm
ACE,ISO,DI,PEII(O2 Plasma)
Dehydration bake 110 1min
Spin HMDS (3krpm, 30sec)
  Wait 60s after pipetting or 105C, 2min bake after spinning (improved adhesion)
Spin SPR955.9 (3krpm, 30sec)
Pre-exposure bake 95C, 90s
Autostepper Exposure=Variable, Focus=0
Post exposure bake 125C, 90s
40s Develop in MIF726
O2 plasma 30s 300W 100mT to clean surface
ICP#2 (recipe #104)
  CF4/CHF3/O2 5/35/10sccm, 500/50W ICP/CCP, 0.5Pa, 2min 30sec
RIE#5 GaAs Etch
Completed Pending Abandoned

## Slide 19: Over-exposure Focus = 0 100x Visible Microscope
Note the sharpening, retraction, & rainbow thin fill effect that occurs with increased exposure of the pattern.
0.4sec
0.55sec
0.7sec
0.85sec
1.0sec
1.6sec

## Slide 20: Over-exposure Focus = 0 100x DUV Microscope
Note the sharpening, retraction, & rainbow thin fill effect that occurs with increased exposure of the pattern.
0.4sec
0.55sec
0.7sec
0.85sec
1.0sec
1.6sec

## Slide 21: Over-exposure Focus = 0 100x DUV Microscope
Note the sharpening, retraction, & rainbow thin fill effect that occurs with increased exposure of the pattern.
0.4sec
0.55sec
0.7sec
0.85sec
1.0sec
1.6sec

## Slide 22: Residual PR Films at Taper Tip
As the over-exposure is increased the pattern retracts and thins at the tip. This sharpens the tip, however it leaves a film or resist visible in the microscope which is not expected to withstand oxide dry etching.

## Slide 23: Conclusions Over-exposure of positive resist taper pattern
Some reduction is clearly visible and should be investigated as a change in the current Si Hybrid process.
I suggest a simulation of 300-500nm taper tips transmission as a function of alignment offset.
<200nm tapers don’t seem possible in this process because of the thinning of the tips into residual PR films which will adversely effect consistency and line edge roughness.
There is also the unmeasured parameter of consistency. This is predicted to decrease with higher over exposure doses.

## Slide 24: PMGI/SPR bi-layer pattern reduction with DUV flood exposure

## Slide 25: PMGI/SPR bi-layer pattern reduction with DUV flood exposure
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
Bond
PECVD Hardmask
PMGI & Positive Resist Bi-layer
Std. Lithography
DUV Exposure & Develop
Strip
III-V Dry Etch
BHF HM Removal

## Slide 26: PMGI/SPR bi-layer pattern reduction with DUV flood exposure
Epi
HM
Si or SiO2 WG Layer
Si
Epi
Hardmask
Si or SiO2 WG Layer
Si
Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
III-V Epi
Si or SiO2 WG Layer
Si
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
Epi
HM
Si or SiO2 WG Layer
Si
PMGI
PR
Bond
PECVD Hardmask
PMGI & Positive Resist Bi-layer
Std. Lithography
DUV Exposure & Develop
Strip
III-V Dry Etch
BHF HM Removal

## Slide 27: PMGI/SPR bi-layer pattern reduction with DUV flood exposure
ACE,ISO,DI,PEII(O2 Plasma)
Deposit oxide hardmask in PlamsaTherm PECVD – 200nm
ACE,ISO,DI,PEII(O2 Plasma)
Dehydration bake 110 1min
Spin SF-11 (4krpm, 30sec)
Reflow Bake (200C, 2min)
Spin SPR955.9 (3krpm, 30sec)
Pre-exposure bake 95C, 90s
Autostepper Exposure = 0.42s, Focus = +10
Post exposure bake 110C, 90s
40s Develop in MIF726 (May be longer)
DUV flood expose (varied time)
Develop (101A, 1min) (repeated variable number of times)
ACE soak 5min - to strip SPR955.9
  i-line flood expose and 1-2min Develop in MIF726 was found to attack exposed PMGI
O2 plasma 30s 300W 100mT to clean surface
ICP#2 (recipe #104)
  CF4/CHF3/O2 5/35/10sccm, 500/50W ICP/CCP, 0.5Pa, 2min 30sec
RIE#5 GaAs Etch
Completed Pending Abandoned

## Slide 28: SPR 955 0.9 pattern before PMGI exposure and development

## Slide 29: Repeated DUV Exposure/Develop Process

## Slide 30: Repeated DUV Exposure/Develop Process
 | 1x | 2x | 3x | 4x | 5x | 6x
2min Exposure 60s Develop | Under developed | Under developed | Under developed | Developed | Developed | Developed
4min Exposure 60s Develop | Under developed | Under developed | Developed |  |  | 
6min Exposure 120s Develop | Under developed |  |  |  |  | 
8min Exposure 2min Develop | Under developed |  |  |  |  | 
10min Exposure 2min Develop | Under developed |  |  |  |  | 
12min Exposure 2min Develop | Under developed |  |  |  |  | 
It appears that a single exposure and development is difficult to achieve. Further investigation will be done in this area to improve consistency of the process.

## Slide 31: PMGI Taper Tip Patterns
Once the PMGI has been fully exposed and developed, even over exposed and repeatedly developed the patterns show the most significant and repeatable reduction in taper size and have tips <200nm meeting the objective of the PULSAR process requirements.
3x4min Exposure, 60s Develop, 5min Acetone, 30s PEII O2 descum

## Slide 32: Residual PR Films at Taper Tip
As with the i-line over-exposure process It is possible with too many repeat exposure development cycles to wear down the tip. However the patter does not seem to suffer as drastic an effect.
6x2min Exposure, 60s Develop, 5min Acetone, 30s PEII O2 descum

## Slide 33: Conclusions
BHF hardmask wet etching must overcome adhesion issue to be a viable option.
SPR 955 0.9 over-exposure process seems limited by the wavelength of the i-line lithography tool and the residual films at pattern edge, development will continue as it is a simpler process, however it is a second option at this point.
Currently, the PMGI/SPR bi-layer pattern reduction with DUV flood exposure process appears to show most promise for delivering <200nm taper tips using the Autostepper.
Recommendation: I recommend that the Si hybrid group investigated with simulations taper tip reduction trade-offs with alignment offset to improve taper performance
Acknowledgements: Thanks to Brian Thibeault and Ning Cao for discussions and recommendations to improve these processes.

## Slide 34: Next steps
Hard mask etches and III-V etches must be completed to finalize the decision of the taper process most appropriate for PULSAR.
Continuing Development
  Thermal study of GaAs bonded epi
    PL Study is nearly complete
    Contact anneal study is starting this week
  Top cladding/via process development
    BCB and SOG will be attempted
    Ti/Pt/Au P/Probe metal process attempted over the next few weeks
Pulsar Taper Mask
  Taped out all but the P/Probe metal and Via mask, which are pending process development