## Slide 1: BCB Planarization Process
Jared Hulme
4/9/12

## Slide 2: Hard Mask Dep & Lithography
Hard Mask Deposition
  Clean - ACE/ISO/DI
  Deposit Oxide
    PlasmaTherm PECVD 400nm
Lithography
  Clean
    ACE/ISO/DI
    O2 Decsum 30s, 300mT, 100W)
    Dehydration bake: Hotplate 150C, 2-5min
  Spin HMDS (5000rpm, 30s) (let sit for 30s on chip before spinning)
  Spin AZ4210 (4000rpm, 30s)
  Pre-Exposure Bake (95C, 1min)
  Lithography - Pattern a window in the deep etch region
    Litho Tool: GCA Stepper / Autostepper / I-Line filtered contact aligner
    Exposure: 3sec / 1sec / 13sec
    Focus Offset: 0 / 0 / NA
    NO POST-EXPOSURE BAKE
    Develop (AZ400K 1:4 diluted, 70sec) (actual is more like 2 min 20 sec)
    DI Rinse
  Inspect in microscope
  Dektak height: = ______nm
Si Substrate
286um
Si Substrate
SiO2
Si Substrate
SiO2
Resist
Si Substrate
SiO2
Resist
Si Substrate
SiO2

## Slide 3: Etch and Inspect
Hardmask Etch - SiO2 Etch target 400nm
  Etch Tool: ICP#2
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers Sioxvert etch # 101, 5min (CHF3 etch so check gases)
  Etch(Recipe, Rate): (Bowers Sioxvert etch # 101, 250nm/min = 4.16nm/s) over etch by 20% => Etch for 2’
Inspect in microscope
Dektak height: = ______nm
Strip PR
  ACE/ISO/DI Rinse
  1165 Soak at 80C in covered bath - 10min
  ISO/DI Rinse
  PEII - O2 Descum (100W, 300mTorr, 60-120sec)
Dektak height: = ______nm
Si Etch target 2um
  Etch Tool: ICP#2 or Deep Si RIE
  Clean: O2 Clean, 5min
  Season (Recipe, Time): Bowers si etch # 127, 5min - Note: Trenching > .4 um
  Etch (Recipe, Rate): (Bowers si etch # 127, 4nm/s) : 2 um / (4 nm/s) = 500s = 8’ 20” => Etch for 8’ 30”
    Selectivity - 1:10 (SiO2:Si)
Inspect in microscope
Dektak height: = ______nm
Remove Oxide
  BHF dip (100 nm/min) : 400 nm / (100nm/min) = 4 min => Dip for 5’
  DI Rinse
Inspect in microscope
Deposit Nitride or Oxide PlasmaTherm PECVD 40nm
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate

## Slide 4: BCB Application and Cure
BCB application
The ‘Blue Oven’ must be at room temperature 25_C or less before beginning
– Otherwise, BCB will bubble during the cure and the sample will be ruined
NOTE: there must not be any stops in the steps from sample surface preparation to loading the spun sample w/ BCB into the Blue oven
– Any delays will allow increased surface oxide to regenerate on the semiconductor, increasing leakage currents
– Oxygen contaminates BCB and prolonged exposure will compromise the cure and ruin the sample
Prepare the ‘Blue Oven’ – run N2 through chamber at 100%
Place Aluminum Baking Table in ‘Blue Oven’
Solvent clean sample (if necessary), PEII 30s
Coat wafer with BCB 3022-46 – let sit on surface for 30 sec
Spin BCB 500 rpm, ramp 100, 5 sec
Spin BCB 1500 rpm, 150rpm/s ramping, 30 sec – BCB thickness _ 3-4 μm
BCB Cure
Place sample(s) on Aluminum Baking Table
Reduce N2 flow to 60% after 3 min
Load and run Program 5 (confirm in case it has been altered)
Program sequence for HARD CURE (Total time in oven: 6-7 hours)
  (a) 5 min ramp to 50_C, 5 min soak
  (b) 15 min ramp to 100_C, 15 min soak
  (c) 15 min ramp to 150_C, 15 min soak
  (d) 60 min ramp to 250_C, 60 min soak
  (e) Natural cool down (NOTE TIME OF COOL DOWN: about 3.5 Hours)
  (f) Oven off
Remove sample and inspect under the microscope
Turn off the ‘Blue Oven’
Si Substrate
BCB

## Slide 5
Wafer planarization etch back
  Clean carrier wafer in Panasonic ICP (Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 5 min
  (a) Load sample on carrier wafer, BCB ICP etch (Recipe 308: CF4/O2 50:200 sccm, 40 Pa, 1000W) 5 min
    Ash rate ~ 400nm/min (it does take some time to heat up the sample before the full rate kicks in)
  (b) Inspect sample in Microscope/Dektak/FEI SEM to see if both large and small mesas and are exposed
  Repeat the above etch (1 min increments) and inspection until all mesas are exposed (note: uniformity of BCB should be under 150nm)
    Be sure to run the wafer clean program in between each etch cycle
  Repeat the BCB passivation and Wafer planarization etch back step for further sample planarization
Remove Oxide/Nitride if needed
  BHF dip
  DI rinse
  Bake 110˚C / 2min
BCB Etch
Si Substrate
Si Substrate

## Slide 6
P-metal Lithography
  Clean
    ACE/ISO/DI (ultrasonic for ACE/ISO)
    O2 Decsum 60s, 300mT, 100W)
    Dehydration bake: Hotplate 150C, 2-5min
  Spin on resists
    PMGI SF-11: 4000rpm/1 min
      Bake 170C/1min
    PMGI SF-11: 4000rpm/1min
      Bake 170C/2min
    AZ-NLOF 2020 Resist: 3000rpm/30sec
    Bake 110C/1min
  Autostep 200 Expose .14sec
  Post-Exposure Bake 110C/1min
  Develop Resist
    AZ-MIF300 developer 40sec
    DI Rinse
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 70sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  DUV Expose SF-11: 300sec/1000W
    Develop in SAL101 60sec
  Inspect in microscope
  Repeat DUV and develop as needed
P-Metal Lithography
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate
Si Substrate

## Slide 7
Pre-metal clean
  O2 Decsum 60s, 300mT, 100W)
E-beam metal deposition
  Ti: 50Å @.2Å/min
  Pt: 200Å @ .5Å/min
  Au: 1.5um @ 2/5/30 Å/min for 200/600/remainder
Liftoff
  1165 soak @ 80˚C for 20min
  Gently agitate with pipette
  ISO/DI rinse
Inspect in microscope
Repeat liftoff steps as needed
P-Metal Deposition
Si Substrate
Si Substrate
Si Substrate

## Slide 8
Pre-metal clean
  O2 Decsum 60s, 300mT, 100W)
RTA
  360˚C / 30s
Inspect in microscope
P-Metal Anneal

## Slide 9: Results
Ash rate ~ 400nm/min
Uniformity < 150nm
BCB withstood 360˚C without any noticable change
Run 2 | Wafer 2 | Sample 3 | Ashed 5'20" | 
 | Measured heights between mesa and bcb |  |  | 
 | Measurements in nm |  |  | 
Die 1 | Small | Large | Large S | Small S
Average | 542.375 | 517.0161 | 566.5929 | 548.74
Minimum | 505 | 437.1 | 504 | 528.8
Maximum | 595.4 | 630.8 | 706.6 | 568.2
Overall Min | 568.2 |  |  | 
Overall Max | 706.6 |  |  | 
Uniformity | 138.4 |  |  | 

## Slide 10: Next Steps
Redo metal deposition
  Half N-layer metal
  Half P-layer metal
Continue uniformity measurements
Attempt a vertical ash