## Slide 1
POEM v1.0 Process Flow
08/13/2012
Yongbo Tang

## Slide 2: Overview
SOI
  500nm/1000nm Si/SiO2
  250nm half etching
EPI
  1465nm PL
  Old standard epi structure
    No InGaAs/InP protecting layer above 100nm InGaAs

## Slide 3: Check wafer quality
SOI surface cleaning
SOI wafer
  check: surface roughness < 1 nm RMS

## Slide 4: Hardmask deposition
Deposit PECVD oxide 275nm

## Slide 5: SOI waveguide litho
SPR955CM 0.9 (negative mask/Positive PR/Etch->hole)
Spin at 3k RPM for 30s
Used CEM
Exposure needs optimization

## Slide 6: Hardmask etch
ICP2 SIOVert

## Slide 7: Strip resist
Resist difficult to remove –
Solution: Use Piranha/BHF

## Slide 8: SOI waveguide etch
Etched 254nm +/-4nm across 4x3 die array

## Slide 9: Remove hardmask

## Slide 10: VC litho
No Hard mask??
(negative mask/Positive PR/Etch->hole

## Slide 11: Strip resist
Resist difficult to remove
Solution: Use Piranha/BHF

## Slide 12: III/V wafer bonding
NH4OH vapor was removed from process. Bond yield was very high.
No additional InGaAs/InP protecting layer

## Slide 13: III/V substrate removal
HCl:H2O=3:1
InGaAs layer exposed! (Affect the P-contact)
Goto next step ASAP.

## Slide 14: P-mesa hardmask deposition
PECVD 300nm of SiN (twice)

## Slide 15: P-mesa litho
SPR955CM 0.9 at 3kRPM (800nm thick)
  positive mask/positive PR/Etch-> Mesa
Use CEM!
0.4s exposure
HMDS issue had large impact on this step

## Slide 16: P-mesa hardmask etch
Overetch attacks Si in failed bond regions

## Slide 17: P-mesa etch
Etch into top SCH/ partly into the QW
Uniformity was under 50nm across chip

## Slide 18: SCH litho
Used SPR955 1.8, spun at 2.5k (3k left taper tip uncovered)
  Pos Mask/Pos PR/Etch->Mesa
Increased exposure time to 0.5s for optimum resolution

## Slide 19: SCH etch
(MUST DO: 2 minutes O2 descum in PE2 before wet etch! PR must be hydrophilic or etch will not occur)???
Wet etch 15/5/1 H2O/H2O2/H3PO4. Did 30-40s, should be clear when etch is complete (exposed n-layer is pink, VCs clearly visible)

## Slide 20: Strip p-mesa hardmask
10 sec BHF dip to remove polymer!
CF4 etch in ICP2???(keep SiN?)
Attacks Si in failed bond region A LOT – exposed passive devices destroyed by this step

## Slide 21: N-InP hardmask deposition
One chip used SiO2 from sputter 4 for this step, no adverse effect
500A SiN

## Slide 22: N-InP lithography
SPR955CM 1.8, spun at 2.5k, expose for 0.5s
  Pos Mask/Pos PR/Etch -> Mesa

## Slide 23: Pattern hardmask
Etch in ICP2. Devices using SiO2 hardmask required O2 ashing to remove PR (gasonics was down)
Strip PR

## Slide 24: N-InP etch
Use etch monitor. Stop immediately when curve flattens.

## Slide 25: N-InP metal litho
Use single layer of SF-15, spun at 2.5k. Dektak imaging resist before developing underlayer, then dektak total height after developing underlayer. Underlayer height must be 2x metal height (2um for 1um of metal) or more
Which PR??? nLoF2020?

## Slide 26: N-metal hardmask open
Etch in ICP2 using 181 for SiN or SiOVert for SiO2. Polymerization did not affect liftoff.

## Slide 27: N-metal sac-layer etch
MUST DO: 2 minutes O2 descum in PE2 before wet etch! PR must be hydrophilic or etch will not occur
Use 15/5/1 H2O/H2O2/H3PO4 for 30s, same as QW etch.
Take microscope before/after, less obvious when etch is complete than QW etch.

## Slide 28: N-metal deposition
Use E-beam 4 to reduce bat ears
Ni/Ge/Au/Ni/Au (50A/300A/300A/200A/6000A)

## Slide 29: N-metal lift-off

## Slide 30: Nitride sticking layer
Used 20nm PECVD SiN. Might be better to use thick (200+nm) oxide as waveguide cladding since BCB/SU8 both fall apart when polishing

## Slide 31: BCB
See process by J. Hulme for details

## Slide 32: BCB ash
How to identify whether SiN is still there
If SiN is still there, PE2 required or keep in mind for SiN removal before p-metal.
If not, be careful with the leakage along the side wall.
Make sure no leakage along sidewall

## Slide 33: BCB/revised
300nm SiN sticking layer.

## Slide 34: P-metal litho
  Used 1 layer SF 11(15???) spun at 2.5k and baked at 180C
    Positive Mask/Negative PR/Liftoff->Mesa
SiN removal by PE2 (need a way to check whether it is gone)

## Slide 35: P-metal liftoff
thin p-metal deposition to ensure that the final probe metal is on the highest surface.
Pd/Ti/Pd/Au 30A/170A/170A/1000A

## Slide 36: Anneal
RTA 30s@360C

## Slide 37: Impl. Litho
AZ4210+2 layer SF11 (Neg Mask/Pos PR/Etch->Hole)

## Slide 38: Impl.
send out for impl. /7C

## Slide 39: InGaAs removal for isolation
SiN removal PE2
H2O:H2O2:H3PO4=38:1:1 for 75sec
PR strip off

## Slide 40: Via litho 1
Via only for N metal
  Positive Mask/Positive PR/etch -> Hole
SiN removal by PE2

## Slide 41: Via etch 1
SiN removal
Use BCB ashing recipe in ICP1
SiN removal
PR strip

## Slide 42: TLM testing

## Slide 43: Pad litho

## Slide 44: Metal dep. and lift off
Ti/Au: 250A/20000A.