## Slide 1
SOI wafer after roughness inspection
Hardmask – SiO2
Thermally grown
PECVD/Sputter
Sputter because PECVD has thickness variation?
OR
Blank etch till 280nm of hardmask is left
SPR955-0.9, 3000rpm, to try out CEM
SiO vert – CHF3 40sccm. Will copy paste the entire recipe window, to be checked before etch.
SiO2 thickness >280nm
How often do we calibrate focus/time?
Expose, Reflow?
Filmetrics, Descum (ICP leaves polymer residue)
Flood exposure, UV lamp power >~6.7

## Slide 2
Hardmask etch
Silicon etch
Check recipe
Descum, strip resist, dektak
Check recipe, BCl3+Cl2 (20:40sccm)
Dektak, SEM
Numbers I need after every run.
Dektak height after silicon etch.
Rib widths at all levels, see fig.
oxide and rib height (#2,#3 - will have to cleave sample which people do not like, include a dummy all the time?)
Trench widths
Loss measurements from testing phase if possible.
The excel file will then calculate the two deltas, ideally both zero.
Silicon
SiO2
W1
W3
Desired length + constant variation (Δ) + random variation(δ).
W2
Flood exposure?

## Slide 3
Splits | 
Waveguide width (um) | Trench width (um)
0.7 | 0.7
1 | 1
1.5 | 1.5
2 | 2
2+{3*(0.7+1+1.5+2)+12*0.7}+{3*(0.7+1+1.5+2)+12*1}+{3*(0.7+1+1.5+2)+12*1.5}+{3*(0.7+1+1.5+2)+12*2}+2 = 130um
500um